# PE Plastic Biodegradation by Microbial Communities

## Introduction

Plastic pollution has become a global environmental challenge, with over 400 million tons of plastics produced annually and a large fraction of this waste accumulating in landfills and natural ecosystems[1][2]. Polyethylene (PE), a polyolefin polymer composed of long hydrocarbon chains, is the single most widely used plastic – accounting for ~38% of plastic demand – found in products from packaging films and bags to containers[3]. PE’s popularity stems from its durability, hydrophobicity, and chemical inertness, but these same properties make it highly recalcitrant to biodegradation[4][5]. Unlike natural organic waste, PE cannot be readily broken down by microbes, leading to persistent litter that can persist for decades or even centuries in the environment[2][6]. Indeed, the estimated half-life of PE in certain conditions ranges from decades to hundreds of years[2][6]. Over time, environmental weathering (UV exposure, mechanical abrasion) may fragment PE into microplastics, but these tiny particles are still chemically intact and can disperse globally – even being detected in remote regions like Arctic snow[7][8]. The accumulation of PE debris poses risks to wildlife and raises concerns about long-term ecosystem impacts.

In this context, there is intense interest in developing biodegradation strategies for PE waste, harnessing microbes that can metabolize or mineralize the polymer. Compared to incineration or mechanical recycling, biodegradation under mild conditions could offer a more eco-friendly solution[9][10]. However, PE’s simple carbon–carbon backbone lacks the easily hydrolysable bonds present in other plastics (like the ester linkages in PET), making it an exceptionally challenging substrate for microbial enzymes[11][12]. Early studies reported only negligible weight loss of polyethylene after years of burial in soil[13][14]. To date, no single microbe or enzyme has been shown to achieve complete PE mineralization on a practical time scale[15][16]. Nevertheless, a growing body of research has documented partial biodegradation of PE by certain bacteria and fungi, especially after pretreatments or over very long incubations[8][17]. These observations have spurred efforts to identify new PE-degrading organisms, understand the degradation mechanisms, and enhance these processes through bioengineering.

Crucially, recent studies suggest that microbial communities (consortia), rather than isolated strains, may be key to more efficient PE biodegradation[18][19]. In natural settings, diverse microbes colonize plastic debris (the so-called “plastisphere” biofilms) and may act in concert to break down polymers[20][21]. Harnessing such synergistic interactions – either by enriching natural consortia or constructing synthetic ones – is an emerging strategy in plastic bioremediation[22][23]. This review provides a comprehensive overview of PE biodegradation by microbial communities. We first discuss the inherent challenges of PE biodegradation and the known microbial and enzymatic mechanisms. We then compare the abilities of various bacteria and fungi to attack PE, highlighting the roles of multispecies consortia and biofilms in enhancing degradation. Next, we examine approaches for developing effective PE-degrading microbial communities, from environmental enrichment (“top-down”) to assembling defined mixtures (“bottom-up”), including cross-kingdom consortia. We also address controversies and knowledge gaps – such as how to distinguish true biodegradation from mere surface deterioration – and the need for standardized methods in this field. Finally, we offer a forward-looking perspective on how advanced tools (e.g. genomics, enzyme engineering, and synthetic biology) could accelerate progress in the next 5–10 years toward sustainable biological mitigation of PE pollution.

## Characteristics of Polyethylene and Biodegradation Challenges

PE is a long-chain hydrocarbon polymer, typically synthesized via ethylene polymerization, that can be linear or branched (e.g. high-density PE versus low-density PE)[24][6]. Its molecular structure – a backbone of carbon–carbon single bonds with hydrophobic methylene groups – is extremely chemically stable. Unlike natural polymers (cellulose, proteins, etc.), PE lacks reactive functional groups for enzymes to attack[4]. It is also generally solid and crystalline (especially HDPE), limiting microbial access to its interior. These features explain why PE is often considered non-biodegradable under ambient conditions. For example, intact PE sheets showed only trace deterioration (0.2% weight loss) even after a decade in soil[14]. Key factors impeding biodegradation include:

- Hydrophobicity and size: PE’s water-insolubility and high molecular weight prevent microbes from directly taking up the polymer[25][26]. Microbes must first adhere to the plastic surface, and even then only surface layers are accessible.

- Crystallinity: The tightly packed crystalline regions of PE are impermeable and resistant to enzymatic attack. Degradative action usually initiates in amorphous regions or at defects[27][28].

- Lack of functional groups: Most biodegradation enzymes (e.g. hydrolases) target specific bonds like esters, amides or glycosidic bonds. PE’s C–C bonds have high bond dissociation energies and no good leaving groups, making typical enzymatic cleavage very difficult[29][12]. Only oxidative enzymes or radicals can appreciably attack the C–H/C–C bonds in PE.

- Additives and weathering products: Commercial PE contains additives (antioxidants, fillers, plasticizers) that may either hinder microbial attack or confuse the analysis by being preferentially consumed[30][31]. Moreover, environmental weathering can oxidize PE surface to create carbonyl groups – paradoxically, while oxidation can promote biodegradability, it also embrittles the plastic into microplastics that disperse widely[32][33].

Given these challenges, microbial degradation of PE is inherently a slow, multi-step process. In the environment, abiotic factors like UV radiation and heat often initiate degradation by introducing oxygenated functional groups into the polymer (a process known as oxidative pretreatment or abiotic deterioration)[32][25]. These oxidative cracks and bonds (e.g. formation of carbonyls, hydroperoxides) reduce PE’s molecular weight and generate “entry points” that microbes can further act upon[34][35]. Without such pretreatment, pure microbial action on pristine PE is extremely limited. Thus, research in PE biodegradation often involves some pretreatment (UV exposure, thermal aging, addition of pro-oxidant additives) to accelerate subsequent bio-fragmentation[36][14]. Still, distinguishing true biodegradation (conversion to biomass or CO₂/CH₄) from mere depolymerization or disintegration is critical. One major issue in the literature is the lack of a uniform definition and quantitative criteria for PE biodegradation[37][38]. Reported weight loss or CO₂ evolution can vary widely depending on experimental setups, and incomplete oxidation of PE might yield micro-fragments that escape detection[39][40]. As a result, establishing standardized methods (e.g. using radiolabeled PE or clear mineralization tests) is a priority for this field[41][42].

In summary, the recalcitrance of PE arises from its stable hydrophobic polymer structure. Any successful biodegradation approach must overcome the initial barriers (surface adherence and oxidation) and then deal with a mixture of intermediate byproducts. The following sections describe how certain microbes – especially in cooperative communities – are capable of initiating and completing different stages of this process.

## Mechanisms of Microbial PE Biodegradation

Biodegradation of PE by microbes generally proceeds through a series of sequential stages, each mediated by specific biological activities[43][25]. Figure 1 illustrates these stages in an idealized biodegradation scenario for polyethylene.

Figure 1: Schematic overview of the polyethylene biodegradation process by microbes (adapted from Zhang et al. 2023[44]). In stage (i) colonization, microbes attach to the PE surface often via biofilm formation, aided by secreted extracellular polymeric substances (EPS) or biosurfactants that help them adhere to the hydrophobic plastic[45]. Stage (ii) biodeterioration involves surface damage as attached microbes grow and secrete enzymes or acids that cause pitting, crack formation, or swelling in the polymer matrix[46]. Filamentous fungi and actinomycetes can physically penetrate the plastic with hyphae, exacerbating the surface erosion[47]. In stage (iii) biofragmentation, extracellular depolymerases (oxidases, oxygenases, etc.) cleave the long polymer chains into shorter oligomers, dimers and monomers[48]. This step is crucial since intact PE is too large to uptake – microbes require the polymer to be depolymerized to fragments roughly C_10–C_50 in size before assimilation[26]. Stage (iv) assimilation refers to the uptake of soluble oligomers/monomers into microbial cells and their incorporation into central metabolic pathways[49]. Finally, stage (v) mineralization is the complete oxidation of the carbon fragments to inorganic end-products (CO₂ under aerobic conditions, or CO₂/CH₄ under anaerobic conditions)[50]. Each stage may involve distinct members of a microbial community acting in concert.

It is important to note that initial colonization and biofilm formation on PE are prerequisites for efficient degradation[45][51]. Many PE-degrading microbes secrete sticky EPS or even biosurfactants to help them attach to the inert plastic surface. This not only concentrates cells on the substrate, but the biofilm microenvironment can facilitate localized polymer oxidation. Studies have shown that biofilm formation can introduce hydrophilic functional groups onto PE and create surface roughness, effectively “priming” the plastic for subsequent fragmentation[45][52]. For example, certain bacteria produce surfactants that reduce water contact angle on PE, while fungi secrete hydrophobic proteins (hydrophobins) that allow their hyphae to strongly adhere to plastic[53][54]. Biofilms can also retain extracellular enzymes in proximity to the polymer. Thus, the earliest stage of colonization is not merely passive attachment – it actively contributes to polymer weathering and the introduction of reactive sites.

Following colonization, biodeterioration describes the superficial breakdown of polymer integrity driven by microbial growth and metabolites. Bacteria on PE have been observed to secrete oxidative enzymes (like dehydrogenases and lipases) that initiate bond scission or modify the polymer chemically[46]. The metabolic byproducts (acids, peroxides) can further chemically etch the plastic[55]. Filamentous organisms (e.g. Streptomyces or fungi) physically disrupt the polymer by growing through it, leveraging mechanical forces in addition to enzymatic action[47]. This stage typically results in visible changes – increased surface roughness, small cracks or pits, and the appearance of carbonyl groups (detected by FTIR) on the PE surface[56][57]. However, the polymer chains may still largely remain high-molecular-weight at this point, meaning true depolymerization has yet to occur in bulk.

The critical step of biofragmentation is the actual cleavage of the long PE chains into smaller units. Microbes capable of attacking PE employ oxidative enzymatic mechanisms, since hydrolysis (used for polyesters like PET) is ineffective on the C–C backbone[11][12]. Enzymes implicated in PE fragmentation include oxidoreductases such as laccases and peroxidases (which generate reactive radicals that can abstract hydrogens from the polymer)[58][59], and oxygenases such as alkane monooxygenases that can insert oxygen into C–H bonds of alkane-like substrates[12][60]. Free radical oxidation (e.g. via Fenton chemistry or UV-activated processes) can also play a role in concert with biotic processes[32][61]. The outcome of fragmentation is a mixture of lower-molecular-weight compounds: short hydrocarbons, oxidized oligomers (with alcohol, carbonyl or acid end-groups), and even monomeric units like ethylene glycol or fatty acids, depending on how far oxidation progresses[60][62]. Notably, studies indicate PE must be depolymerized to oligomers roughly <600 Da (around C_20 fragments) for microbes to assimilate them through the cell membrane[63]. Achieving this depolymerization is often the rate-limiting step in PE biodegradation. For instance, Rhodococcus ruber C208 was shown to oxidize PE, reducing its average molecular weight by ~20% when supplemented with copper to induce a laccase enzyme[64][56]. Such partial oxidation “softens” the plastic, yielding fragments that can be further metabolized.

After fragmentation, assimilation and mineralization proceed via conventional microbial metabolism. Once the PE is broken into small enough molecules (e.g. fatty acids, short-chain alkanes or alcohols), these molecules can be transported into microbial cells[49]. There they enter catabolic pathways – for example, fatty acids undergo β-oxidation, alkanes/alcohols are funneled into central metabolism as acetyl-CoA or other intermediates[65][66]. Ultimately, with sufficient oxidative steps, the carbon from PE is converted to CO₂ (under aerobic conditions) or a mix of CO₂ and methane (if anaerobic archaea are involved)[49]. Mineralization indicates complete biodegradation, though in practice many experiments stop short of demonstrating full mineralization, instead reporting intermediate byproducts (e.g. detection of oxidized fragments by GC-MS)[62][67]. Confirmation of true mineralization typically requires respirometric tests (measuring ^14CO₂ from radiolabeled PE, for example) or long-term monitoring of gas production.

In real-world environments, these stages are often distributed among different members of a microbial community. One organism might be proficient at the initial surface oxidation, while another can metabolize the byproducts. This division of labor is a key rationale for using microbial consortia, as discussed later. It is also noteworthy that environmental factors (temperature, oxygen availability, UV exposure) can dramatically influence these biodegradation stages. For instance, sunlight-driven photooxidation can accelerate the biodeterioration and fragmentation phases, essentially collaborating with microbial action[61][33]. In summary, PE biodegradation is a complex, stepwise process requiring initial oxidative attack and subsequent co-metabolic handling of breakdown products. The following sections examine what microbes and enzymes carry out these steps.

## Microorganisms Involved in Polyethylene Degradation

### Bacteria

A variety of bacteria have been reported to colonize and partially degrade polyethylene, especially when the plastic is pre-weathered or incubated for long periods. Many of these bacteria are environmental isolates from plastic-contaminated sites (soil, landfills, marine debris) where they likely adapted to use polymer fragments or associated additives as carbon sources[68][69]. Biofilm-forming bacteria are frequently observed on PE surfaces in nature[70][71], suggesting an inherent ability to attach and perhaps secrete the enzymes needed for polymer breakdown. Some of the commonly reported PE-degrading bacterial genera include Bacillus, Pseudomonas, Arthrobacter, Rhodococcus, Acinetobacter, Enterobacter, and Brevibacterium, among others[72][73]. For example, strains of Bacillus and Pseudomonas – which are well-known hydrocarbon degraders – have repeatedly been isolated from plastic waste and shown to cause weight loss or surface erosion of PE films[74][75]. Bacillus species appear to be ubiquitous in plastic debris; one study found a Bacillus strain could degrade not only PE but also other plastics like PET and polyurethane[76]. Pseudomonas, likewise, are versatile degraders: Pseudomonas aeruginosa E7 was shown to utilize low-molecular-weight PE (obtained by thermal degradation of PE) as a carbon source by means of an alkane hydroxylase system (discussed in Enzymes section)[12][77].

Soil bacteria from extreme environments have also demonstrated PE-degrading capabilities. Thermophiles (heat-loving bacteria) and acidophiles/halophiles have been tested on PE under conditions that mimic harsh environments. For instance, a thermophilic Brevibacillus borstelensis strain isolated from desert soil showed ~11% weight reduction of LDPE film after 30 days at 50 °C[78]. Likewise, an acid-tolerant Pseudomonas sp. was found to achieve ~6% PE weight loss in 30 days at pH 5 and 44 °C[79]. These levels of degradation are modest but significantly higher than what most single strains achieve under ambient conditions, highlighting that stress conditions or prolonged incubations can augment certain bacteria’s activity[80]. Still, even the best-performing isolates tend to yield only single-digit percentage weight losses over month-long scales, indicating that complete degradation is not attained. Often, bacteria may only attack the amorphous portion of PE, leaving behind a more crystalline residue.

A special group of bacteria worth noting are the actinomycetes – filamentous bacteria such as Rhodococcus, Streptomyces, and Nocardia. Actinomycetes share some traits with fungi (e.g. branching hyphae) and are known for producing diverse extracellular enzymes. Several studies suggest actinomycetes play a disproportionate role in polymer degradation. Rhodococcus ruber strain C208, for example, can grow on a polyethylene film as a sole carbon source and produces an extracellular laccase enzyme that oxidizes PE[58][59]. Santo et al. (2013) showed that inducing this laccase with copper ions increased PE degradation significantly, as evidenced by molecular weight reduction and carbonyl formation[81][56]. Streptomyces species have also been isolated from plastic-contaminated sites and found to cling to and embrittle PE films[82]. Actinomycetes’ ability to form biofilms and secrete potent oxidative enzymes likely underpins their effectiveness. They produce sticky exopolysaccharides (rich in N-acetylglucosamine) that help them adhere to plastic surfaces[51][83], and many are known to degrade tough natural polymers (like lignin), so they have the enzymatic machinery for attacking stable carbon bonds. Indeed, genomic studies of PE-colonizing actinomycetes have identified genes for alkane monooxygenases, catalases, and other oxidative enzymes potentially involved in polymer breakdown[60][65]. In summary, across the bacterial domain, Gram-positive spore-formers (Bacillus, actinomycetes) and Gram-negative opportunists (Pseudomonads, etc.) appear most frequently in reports of PE degradation[72][76]. They tend to share traits of robust metabolism, biofilm formation, and production of oxygenase or peroxidase enzymes.

### Fungi

Fungi are increasingly recognized as important agents in plastic biodegradation. In terrestrial ecosystems, fungi are primary decomposers of recalcitrant organic matter (like wood), and they possess powerful oxidative enzymes and extensive mycelial networks[84][85]. These capabilities make them well-suited to tackle stubborn polymers such as PE. A key advantage of fungi is their growth form – filamentous fungi produce hyphae that can physically penetrate into polymer matrices, accessing interior surfaces that bacteria might not reach[86][87]. Fungal hyphae can wedge into microscopic crevices on a plastic surface, prying it apart as the colony expands. In addition, many fungi secrete hydrophobins and other proteins that improve attachment to hydrophobic materials[88][89]. These proteins coat the fungal mycelium and the plastic surface, effectively “gluing” the fungus to the PE and increasing the contact area. This strong adhesion allows fungi to colonize PE even more readily than bacteria in some cases[90][91].

Several fungal genera have shown the ability to grow on and degrade polyethylene. Common examples include Aspergillus, Penicillium, Fusarium, Cladosporium, and Mucor species[92][93]. Many of these are soil fungi or plant litter decomposers that likely encounter polyethylene mulch or waste in the environment. Aspergillus in particular has multiple reported strains capable of deteriorating PE films. For instance, Aspergillus niger and Aspergillus terreus isolates were found to colonize LDPE and cause surface cracking and weight loss over a few months of incubation (often after UV pretreatment of the plastic)[94][95]. Penicillium simplicissimum from soil was shown in one study to reduce the tensile strength of PE films by ~30% after several weeks, indicating polymer chain scission[94][96]. Fusarium species have also been reported to form biofilms on PE and contribute to its breakdown[92][93]. Typically, fungi do not fully mineralize PE on their own, but they excel at the initial oxidative attack and depolymerization.

Fungi produce an arsenal of extracellular oxidative enzymes that are believed to drive PE fragmentation. Chief among these are laccases and peroxidases (such as lignin peroxidase and manganese peroxidase), which are the same enzymes fungi use to degrade lignin in wood[92][97]. These enzymes generate free radicals capable of abstracting hydrogen atoms from the PE chain, leading to oxidative chain cleavage. Indeed, multiple studies have detected laccase activity in cultures of fungi grown with PE, and addition of laccase in vitro can increase the carbonyl index of PE (a sign of oxidation)[58][59]. White-rot fungi (e.g. Phanerochaete chrysosporium, Trametes versicolor) that are prolific lignin-degraders have been tested on polyethylene with some success – they cause surface oxidation and slight weight loss of PE films, presumably via their secreted peroxidases[98][99]. However, fungi often work slowly on PE; significant degradation may require several months of incubation. In one report, Pleurotus ostreatus (oyster mushroom) grew on PE strips over 90 days and produced detectable oxidation products, though complete polymer breakdown was not achieved[100][101]. Notably, fungi can act in synergy with bacteria: fungal hyphae can precondition the plastic, and also serve as highways for bacteria to spread (bacteria can travel along hyphae to colonize new areas of the plastic)[102][103]. This cross-kingdom collaboration is an intriguing approach to PE biodegradation (discussed more under consortia).

In summary, fungi bring unique capabilities to PE degradation: penetrative growth, production of powerful oxidative enzymes, and tolerance of low-nutrient environments (like a plastic surface). Genera such as Aspergillus and Penicillium have repeatedly shown potential to biodeteriorate polyethylene[104][105]. While fungi alone may not completely mineralize PE, they can significantly accelerate the initial breakdown, making the resulting fragments more accessible to other microbes. Harnessing fungal enzymes (e.g. through enzyme cocktails or engineered microbes expressing fungal genes) is considered a promising strategy to improve PE biodegradation rates[29][106].

### Other Organisms

Besides bacteria and fungi, some algae and even animal gut microbiota have been implicated in polyethylene degradation. Certain photosynthetic microbes (algae and cyanobacteria) can colonize plastic surfaces in aquatic environments as part of biofilms, though their direct role in degradation is less clear. There is some evidence that algal metabolites (like oxygen radicals produced during photosynthesis) might contribute to polymer oxidation in sunlit waters[107][108], but systematic studies of algae degrading PE are limited. More attention has been given to the microbiomes of plastic-ingesting invertebrates. For example, the larvae of wax moths (Galleria mellonella, commonly called “waxworms”) can chew and ingest polyethylene films. It has been discovered that waxworm gut microbial communities play a role in breaking down the ingested plastic[109][110]. In experiments where waxworms were fed exclusively on PE, researchers isolated gut bacteria and yeasts that could grow on polyethylene. A notable case is a consortium of Serratia marcescens (a bacterium) and Meyerozyma sp. (a yeast) from waxworm intestines: this bacterium-fungus pair was able to degrade ~16% of a PE film’s weight in one month, significantly higher than either organism alone[111][112]. Gas chromatography identified various oxidative metabolites (alkanes, alcohols, acids) in the worm frass, indicating active breakdown of the polymer[113][114]. Similarly, Tenebrio (mealworm) larvae have gut microbes that can depolymerize styrofoam and may have some activity on PE. These findings suggest that nature may have evolved “digestive” consortia in some insects that facilitate plastic degradation – effectively using a combination of mechanical grinding by the insect and biochemical attack by gut microbes[115][116]. While insects are not practical agents for large-scale waste treatment, their microbial symbionts (and even their enzymes, such as a recently discovered waxworm saliva enzyme that oxidizes PE[117]) provide valuable leads for biotechnological exploitation.

In summary, a diverse cast of microorganisms – from common soil bacteria and fungi to extremophiles and symbionts – has demonstrated some ability to attack polyethylene. No single microbe is a silver bullet for complete biodegradation; rather, each contributes part of the solution. This diversity underpins the idea of microbial communities as the most effective approach, wherein different members can carry out different steps of the degradation process. In the next section, we delve into the specific enzymes these microbes use to depolymerize and consume PE.

## Enzymatic Strategies for Polyethylene Depolymerization

Enzymes are the molecular workhorses behind microbial polyethylene degradation. Given PE’s chemically inert structure, the enzymes capable of attacking it are typically those that generate highly reactive species or perform oxidation of strong C–H bonds. Hydrolytic enzymes (like many cutinases or lipases) that easily cleave ester bonds in bioplastics are ineffective on PE, because PE has no such bonds[11]. Therefore, PE depolymerization relies on oxidative and oxygenase enzymes. Research in the past decade has begun to identify and characterize several classes of enzymes involved:

- Laccases (multicopper oxidases): Laccases are copper-dependent oxidases that reduce oxygen to water while oxidizing a substrate (often generating a radical). In the context of PE, laccases can abstract hydrogen atoms from the polymer chain, creating carbon-centered radicals that lead to chain scission or introduction of oxygen (forming carbonyl groups)[58][59]. The earlier-mentioned Rhodococcus ruber laccase is a prime example: it caused measurable reduction in PE molecular weight and increased carbonyl index when incubated with PE films[118][56]. Fungal laccases are also suspected contributors in many systems where fungi degrade PE, as laccases are commonly secreted during wood decay and can act on a broad range of polymers[58][59]. For instance, a recent study of an Antarctic bacterium (Psychrobacter) discovered a cold-adapted laccase that could oxidize polyethylene at low temperatures, significantly enhancing weight loss of PE over controls[119][120]. Laccases often work in tandem with mediators (small molecules that extend their oxidative range), which could further improve their effect on a hydrophobic solid like PE.

- Peroxidases: Enzymes such as manganese peroxidase (MnP) and lignin peroxidase (LiP), mostly from white-rot fungi, generate potent oxidizing agents (e.g. Mn^3+-chelates or free radicals) capable of attacking tough organic substrates. Fungal degradation of PE has been correlated with the expression of these peroxidases[92][97]. For example, transcriptomic analysis of a marine fungus Alternaria growing on PE found upregulation of genes encoding MnP and LiP, among many other oxidative enzymes[106][121]. These peroxidases likely help break the long PE chains into oxygenated fragments. However, peroxidases require hydrogen peroxide (H₂O₂) to function, which might be supplied by other enzymes like oxidases in the community or through abiotic means.

- Alkane hydroxylases (oxygenases): Perhaps the most significant enzymes for actually cleaving the PE backbone are the alkane monooxygenases, often referred to as the AlkB family (and related cytochrome P450s). These enzymes normally catalyze the subterminal or terminal hydroxylation of alkanes in oil-degrading bacteria[60][65]. Polyethylene can be thought of as a long saturated alkane. When external forces (heat, oxidation) break PE into smaller wax-like fragments, alkane hydroxylases can then act on those. Pseudomonas aeruginosa E7, for example, was shown to use an alkane monooxygenase system (comprising an alkane hydroxylase plus rubredoxin and rubredoxin reductase) to degrade low-molecular-weight PE wax[12][77]. Jeon and Kim (2016) characterized two alkane monooxygenase isozymes (AlkB1 and AlkB2) in this strain and found AlkB2 had higher activity on a ~C_30 polyethylene fragment than AlkB1[77][122]. This indicates some alkane hydroxylases may be specifically adapted or inducible for longer-chain substrates. Genomic surveys have detected alkB-like genes in many PE-enriched communities and isolates[60][123]. For instance, metagenomic sequencing of a marine plastisphere biofilm enriched on PE revealed enrichment of alkane degradation genes (like alkB) over time[124][125]. Similarly, multiple PE-degrading Rhodococcus and Bacillus strains have been found to harbor cytochrome P450 enzymes that can oxidize hydrocarbons[126][127]. Once an alkane hydroxylase converts a chain end to an alcohol, subsequent enzymes (alcohol dehydrogenases, aldehyde dehydrogenases) can further oxidize it to fatty acids[66][128]. Those fatty acids can enter β-oxidation, as illustrated in Figure 2.

Figure 2: Proposed pathway for microbial oxidation of PE-derived alkane fragments (simplified from Zhang et al. 2023[126][129]). Long-chain segments of PE (which may be generated by prior abiotic or enzymatic fragmentation) are first oxidized at the chain end by alkane hydroxylase enzymes (AH, such as AlkB monooxygenases or P450s), yielding primary alcohols. These alcohols are then converted to aldehydes by alcohol dehydrogenase (ADH) and further to fatty acids by aldehyde dehydrogenase (ALDH)[66][128]. Depending on whether the initial oxidation is terminal or sub-terminal, the products can be even-chain or odd-chain acids. Some enzymes like Baeyer–Villiger monooxygenases (BVMO) might also act on secondary oxidation to form esters which then hydrolyze to acids[66]. The resulting fatty acids enter the microbial β-oxidation cycle, being stepwise shortened to acetyl-CoA units that feed into the tricarboxylic acid (TCA) cycle for complete mineralization. Through this cascade, the carbon from PE fragments is gradually funneled into normal metabolism[60][65].

- Auxiliary enzymes: In addition to the primary depolymerases mentioned above, microbes utilize various supportive enzymes during PE degradation. Dehydrogenases, oxidoreductases, and even esterases can play roles in downstream processing of oxidized fragments. For example, once a long alkane is oxidized to a fatty acid, beta-oxidation enzymes take over, but certain unusual intermediates might require specific enzymes (like a Baeyer–Villiger monooxygenase to cleave a ketone to an ester)[66][129]. Catalases and superoxide dismutases are also important since the oxidation processes generate reactive oxygen species that microbes must tolerate. Some bacteria upregulate stress response genes when growing on PE, indicating the metabolism of PE fragments can be toxic or challenging[130][131].

Despite these advances in identifying enzymes, it remains true that no dedicated “polyethylene depolymerase” (analogous to PETase for PET) has been found yet[15][37]. Instead, the breakdown of PE seems to involve a combination of generalist enzymes from hydrocarbon and lignin degradation pathways. This suggests that improving PE biodegradation might require engineering enhanced enzymes. For instance, protein engineering of laccases to increase their redox potential could make them more aggressive oxidants against PE. Similarly, directed evolution of alkane monooxygenases might yield variants that can bind and attack higher molecular weight substrates (mimicking a PE chain). Recent work has also explored enzyme cocktails: Magnin et al. (2019) showed that combining two enzyme types (an esterase and an amidase) synergistically enhanced polyurethane degradation[132][133]. A similar combinatorial approach could be applied to PE – e.g. a laccase to do initial oxidation, plus an alkane hydroxylase to further degrade the oxidized chain ends. Some studies have reported increased PE degradation when adding purified enzymes to microbial cultures or when co-culturing different enzyme-producing microbes[12][77]. As enzyme discovery continues (especially via metagenomic mining of plastisphere communities[124][130]), we can expect a growing toolkit of biocatalysts that, individually or together, target different steps of PE depolymerization.

In summary, the enzymatic attack on PE relies on oxidative enzymes – chiefly laccases, peroxidases, and alkane hydroxylases – to overcome the inertness of the polymer. These enzymes convert parts of the polyethylene chain into more reactive or smaller molecules that standard metabolic enzymes can then assimilate. Unlocking faster PE biodegradation likely hinges on enhancing these initial oxidative steps, either by discovering novel enzymes from extremophiles, genetically improving known enzymes, or assembling multi-enzyme systems that can progressively disassemble the polymer. With the enzymatic basis laid out, we now turn to the concept of using microbial consortia to exploit multiple enzymes and metabolic capabilities in parallel.

## Biodegradation by Microbial Consortia

### Advantages of Microbial Consortia over Single Strains

Isolated bacteria or fungi often show only limited ability to degrade polyethylene, as discussed above. Microbial consortia – communities of multiple interacting microorganisms – can outperform single strains on such complex tasks[134][135]. In natural environments, biodegradation of persistent pollutants typically results from synergistic actions of diverse microbes, each contributing different enzymes and metabolic pathways. There are several compelling reasons why consortia are advantageous for PE degradation:

- Enzymatic diversity: A consortium inherently hosts a broader range of enzymes than any single organism. Degrading PE is a multi-step process (oxidation, depolymerization, assimilation, mineralization) that likely requires different enzyme sets. In a community, one microbe might secrete a potent oxidase, while another produces an efficient alkane hydroxylase, together achieving what neither could alone[134][136]. Indeed, mixed cultures have been shown to yield more complete breakdown of plastics, as complementary enzymes act sequentially[137][138].

- Metabolic cooperation and division of labor: In consortia, microbes can partition the metabolic workload. One group might specialize in using the initial breakdown products, preventing accumulation of those potentially inhibitory byproducts[139][135]. This division of labor reduces metabolic burden on each strain and minimizes feedback inhibition. For example, in a PE-degrading consortium, early degraders generate fatty acids which are promptly consumed by other community members, keeping concentrations low and driving the equilibrium toward further polymer breakdown[140][135].

- Intercellular signaling and reduced competition: Microbes in communities communicate via quorum sensing and other signals to coordinate activities. This can regulate enzyme production and growth so that competition is reduced and synergy is enhanced[141][142]. Some consortium members might even suppress undesirable microbes or cross-feed essential nutrients/vitamins to others, stabilizing the community function.

- Biofilm formation and habitat creation: As noted, certain strains excel at forming biofilms on PE, even if they do not degrade PE well themselves. In a consortium, these “pioneers” can create a biofilm scaffold that other less surface-adherent but more degradative microbes can join[143][144]. For instance, a non-degrading strain might produce a sticky matrix allowing a degrader to firmly attach and colonize the plastic. Such facilitation is absent in a pure culture.

- Broader substrate range: Environmental plastic waste is rarely pure; PE waste may be mixed with other plastics, dyes, and additives. A single strain usually metabolizes a narrow set of substrates, but a multi-species community can collectively attack a mix of polymers and chemicals[19][145]. One strain might degrade polypropylene, another tackles polyethylene, etc., making the community effective on heterogeneous waste streams.

- Resilience and robustness: Consortia tend to be more resilient to environmental fluctuations. If conditions change (pH, temperature, contaminants), some members can survive and maintain function where a single strain might fail. The presence of redundant or stress-resistant members buffers the community. Experiments have shown that mixed cultures maintain degradation activity over a wider range of conditions than isolated strains[146][147].

These advantages have been demonstrated in several studies. For example, Skariyachan et al. (2016) isolated a group of five bacterial strains from a garbage dump; individually they had modest PE-degrading ability, but together as a consortium they achieved significantly higher depolymerization of LDPE films[148][149]. In another case, a two-member consortium of Bacillus and Paenibacillus (both isolated from landfill soil) degraded ~14.7% of added PE micro-particles within 60 days, whereas either strain alone had much lower activity[150][151]. This mixed culture likely benefited from Bacillus producing oxidative enzymes while Paenibacillus perhaps metabolized the oxidation byproducts[150]. Cross-kingdom consortia also show clear benefits: Esmaeili et al. (2013) demonstrated that combining a fungus (Aspergillus niger) with a bacterium (Lysinibacillus) led to faster polyethylene film degradation than either alone[152]. The fungal hyphae may have served as a platform for the bacteria to spread and also initiated the breakdown, which the bacteria then furthered[102][103]. Such fungus–bacterium consortia leverage both robust biofilm formation (from fungi) and efficient metabolic throughput (from bacteria).

It should be noted that not all combinations of microbes work well – antagonism can occur, and some strains might out-compete or inhibit others, reducing overall performance[153][154]. Designing effective consortia thus requires identifying strains that are compatible and complementary. Modern omics tools are aiding this process, as discussed later. Overall, however, the evidence is strong that consortia offer a more effective and holistic approach to PE biodegradation than single organisms, by uniting multiple biochemical talents in one system[134][136].

### Approaches to Constructing PE-Degrading Consortia

Researchers follow two general strategies to obtain functional microbial consortia for PE degradation: “top-down” enrichment and **“bottom-up” assembly[23][155]. These approaches can also be combined for optimal results.

Top-down approaches start with a complex environmental community and selectively enrich it for PE-degrading activity. This often involves taking a sample from a site likely to contain polymer degraders (soil from a plastic waste dump, ocean plastic biofilms, landfill leachate, etc.) and cultivating it in the lab with polyethylene as the primary carbon source[23][155]. Over successive sub-culturing (and sometimes adjusting conditions to favor certain microbes), one aims to obtain a simplified community highly adapted to degrading PE. Top-down enrichments have yielded impressive outcomes. For instance, Joshi et al. (2022) obtained a marine consortium by enriching coastal seawater samples with LDPE as sole carbon; this consortium was able to reduce the weight of LDPE films by ~47% in 120 days[156][157] – a remarkably high degradation extent, likely reflecting a cooperative community of marine bacteria specialized to utilize plastic[156][158]. Similarly, enrichments of landfill soil communities have produced consortia that form dense biofilms on PE and slowly but steadily oxidize and depolymerize it[159][160]. The advantage of top-down is that nature’s “pre-evolved” interactions are kept intact – the microbes already know how to work together. However, the composition of such consortia can be complex and include unculturable members[159][160]. To harness them effectively, one may need to sequence the community DNA to identify key players (metagenomics) and possibly simplify the consortium by isolating core strains.

Bottom-up approaches involve mixing known isolates (which may be pure cultures or engineered strains) to create a new consortium from scratch[23][161]. Here, one selects strains that each bring a desired function – e.g. one good at biofilm formation on PE, another with strong oxidative enzymes, another that consumes intermediates – and co-cultivates them under conditions where they can cooperate. Bottom-up construction allows precise control over the membership and potentially the use of genetically modified microbes with enhanced traits. Researchers have tried various combinations. For example, Park & Kim (2019) combined two soil isolates (a Bacillus and a Paenibacillus) to exploit their complementary degradation pathways, as mentioned above[150]. Skariyachan et al. (2021) formulated a consortium of Enterobacter and Pseudomonas strains derived from cow dung, achieving significantly higher PE and polypropylene degradation than any single strain and observing that PE films were attacked more readily than pellets (due to larger surface area)[162][163]. In another creative bottom-up approach, Lou et al. (2022) took two effective waxworm gut isolates – a yeast and a bacterium – and recombined them into a defined two-member consortium, which as noted degraded nearly 16% of a PE sample in a month[164][62]. This demonstrated that even a minimal synthetic community (just two species) could outperform each alone, validating the bottom-up design principle.

The challenge with bottom-up is identifying the right mix of strains and conditions to avoid antagonism and ensure stability. Often trial-and-error is needed, as mixing arbitrary isolates can lead to one overgrowing the others or production of inhibiting compounds. Additionally, laboratory isolates might lack the robustness of environmental consortia. On the other hand, bottom-up consortia can be optimized (through adjusting inoculum ratios, tweaking nutrients, or even genetic engineering of members to remove incompatibilities) and are easier to reproduce and scale once established.

Increasingly, researchers advocate a hybrid approach: use top-down enrichment to find a good community, then characterize it (via metagenomics, 16S/ITS sequencing, etc.) to identify key degraders, and finally reassemble a simpler synthetic consortium (bottom-up) containing those key players[165][166]. This way, one captures the synergy of the natural community but reduces complexity to a manageable level. For example, Gao & Sun (2021) enriched a marine bacterial community on a mixture of PE and PET and identified three core strains responsible for most of the degradation; they then isolated those strains and recombined them into a simplified consortium that retained the original community’s degradation performance[167][168]. Such rational design of consortia is greatly aided by high-throughput sequencing and meta-omics, which allow us to map community composition and function in detail.

A notable insight from plastisphere studies is that hydrocarbon-degrading bacteria (HCB) often dominate enriched PE consortia[169][170]. This is not surprising since PE is chemically similar to long-chain hydrocarbons. Alcanivorax, Marinobacter, Pseudoalteromonas in marine settings, or Sphingomonas, Burkholderia in soil, are examples of hydrocarbonoclastic genera that proliferate in the presence of polyethylene, potentially utilizing leaked additives or the small fraction of oxidized chain ends as growth substrates[125][171]. Their presence is often a good sign that the community is headed toward breaking down the polymer.

Despite successes, current consortia constructions still face bottlenecks. It is not always clear which genes or metabolic interactions are truly responsible for PE degradation, making rational improvement difficult[153][154]. Sometimes consortia that work in the lab are unstable over time; one member might mutate or get overtaken by “cheaters” that benefit without contributing. Moreover, many environmental microbes cannot be cultured, so top-down enrichments might never yield them in isolation[159][160]. This is where advanced omics and modeling come in, helping to guide the assembly of robust consortia.

### Role of Omics and Bioinformatics in Consortium Design

To better harness microbial communities for PE biodegradation, researchers are leveraging genomics, metagenomics, transcriptomics, and proteomics to dissect what happens in these consortia at the molecular level[172][173]. By sequencing the DNA or RNA of enrichment cultures (the metagenome/metatranscriptome), one can identify the enzymes and pathways that are upregulated during PE degradation and the organisms that host them. For example, Pinto et al. (2022) performed metagenomic analysis on a seawater-derived consortium enriched on LDPE for 2 years; they observed that genes for alkane degradation became dominant, and they pinpointed an increase in the abundance of alkB (alkane monooxygenase gene) and other catabolic genes as the community adapted to using PE[124][125]. This highlights which enzymatic routes (in this case, terminal oxidation of alkanes) are crucial. Similarly, Hou et al. (2022) sequenced two Pseudomonas strains capable of degrading PE and found multiple putative PE-degrading enzyme genes in their genomes, as well as genes for exopolysaccharide production, suggesting a genetic basis for strong biofilm formation on plastic[174][171].

Transcriptomic studies (monitoring mRNA expression) provide insight into active metabolism. In a classic study, Gravouil et al. (2017) grew Rhodococcus ruber (the laccase-producing strain) on polyethylene and compared gene expression to growth on a control substrate; they found 158 genes upregulated on PE, with the most enhanced pathways being those for alkane degradation and fatty-acid β-oxidation[175][176]. This directly supports the notion that Rhodococcus uses an alkane-degrading mechanism to tackle PE, and it identifies which specific genes are involved. Armed with such data, researchers can then target those enzymes for purification, characterization, or overexpression in a production host.

Multi-omics on whole communities can reveal community dynamics and interactions. Metaproteomics might show which organism produces which enzyme in a mixed culture. For instance, one might detect that a Pseudomonas secretes an alkane hydroxylase, while an Arthrobacter in the same consortium produces an esterase that frees up nutrients from additives – each fulfilling a niche. Metabolomics can likewise monitor the consumption of intermediate metabolites to ensure no harmful build-up (which could stall degradation) occurs[177][178]. Altogether, integrating these omics data helps in identifying keystone species (the ones indispensable for degradation), elucidating metabolic pathways utilized by the community, and finding genetic markers (like alkB or laccase genes) to track or enhance the process.

This information loop greatly facilitates consortium design. For example, if metagenomics reveals that certain unculturable species carry vital genes, one could try to isolate them or engineer a surrogate strain to carry those genes. If transcriptomics shows that a community requires a particular vitamin or cofactor to express key enzymes, media can be supplemented accordingly. In one case, a consortium was improved by adding a strain that supplies biosurfactants after analysis showed low bioavailability of the hydrophobic substrate. In another, synthetic biology approaches have been suggested where gene circuits for communication (quorum sensing) are engineered into consortia members to maintain a desired ratio or state[141][142].

In summary, omics-driven insights are increasingly guiding the assembly and optimization of microbial communities for PE biodegradation. The ability to spy on the community’s genetic and metabolic network allows scientists to prune unnecessary members, add beneficial ones, and even predict outcomes of altering conditions. This will be crucial for moving from lab-scale demonstrations to field or industrial-scale applications, where one needs a consortium that is efficient, stable, and safe.

## The Plastisphere: Natural Microbial Communities on Plastic

When plastics enter the environment, they quickly become covered by microorganisms, forming a biofilm termed the “plastisphere.” This concept, first described by Zettler et al. (2013) for marine plastic debris, refers to the unique ecological community that develops on plastic surfaces[179][180]. The plastisphere consists of bacteria, archaea, fungi, protists, and even micro-invertebrates that colonize the polymer, often distinct from the free-living community in the surrounding environment[179][180]. Studying plastisphere communities is highly relevant to PE biodegradation, because these are essentially nature’s consortia that have adapted to survive on plastic – potentially including microbes that can utilize the plastic as a nutrient source.

Community composition: Plastisphere communities vary depending on the environment (marine vs. soil vs. freshwater) and the type of plastic. But common trends have emerged. In marine plastisphere samples, researchers often find a mixture of heterotrophic bacteria (e.g. Alteromonas, Vibrio, Corynebacterium), cyanobacteria, and diatoms attached to PE fragments[181][182]. There is usually a succession where early colonizers are fast-growing copiotrophs and phototrophs, while later a more stable community establishes. Notably, hydrocarbon-degrading genera (like Alcanivorax in oceans or Rhodococcus in soil) tend to be enriched on plastic surfaces, presumably feeding on leached additives or the small fraction of oxidized polymer[183][171]. In soil plastispheres (e.g. plastic mulch films in agriculture or landfill plastics), one often finds Actinobacteria (e.g. Nocardia, Microbacterium), Proteobacteria (e.g. Pseudomonas), and diverse fungi forming biofilms on PE[184][185]. Environmental factors like UV exposure can shape these communities – for example, more phototrophs (algae) on floating ocean plastics, versus more filamentous fungi on buried plastics with less light.

Biofilm development: The formation of a mature plastisphere biofilm is thought to facilitate degradation. As microbes attach and produce EPS, the plastic’s hydrophobicity is reduced and its surface chemistry is altered[186][187]. The biofilm matrix can trap particles and moisture, creating micro-niches. Interestingly, studies show that as the biofilm matures on plastic, species diversity often decreases – the community “selects” for those organisms best suited to long-term colonization of that substrate[188][189]. These late-stage colonists are likely the ones involved in slow breakdown of the polymer. Immature plastispheres might have many transient species that are simply using the surface as habitat without interacting with the plastic. Thus, a key area of research is distinguishing true degraders from mere colonizers. Multi-omics can help: if a microbe is abundant on plastic and also expresses alkane degradation genes, it’s a prime suspect as a degrader[175][176]. Some approaches involve comparing the plastisphere community on a degradable plastic vs. a non-degradable control; organisms specifically enriched on the degradable material are likely involved in breakdown.

Ecological interactions: Within the plastisphere, microbes engage in various interactions – competition for colonization space, predation (some protists graze on plastic-colonizing bacteria), and symbiosis. These interactions can influence degradation. For example, predation by protozoa might actually stimulate bacterial degraders by preventing any one species from overpopulating and by recycling nutrients (the “grazing hypothesis” for biostimulation)[190][182]. Conversely, certain biofilm-forming bacteria may exclude others, limiting community diversity to a few dominant species, which could either enhance focused degradation or eliminate helpful cooperation. There’s also interest in whether plastisphere microbes exchange genes (horizontal gene transfer) for degradation pathways. If plastic surfaces bring different species into close contact, they might swap plasmids carrying catabolic genes, accelerating the spread of plastic-degrading capability.

From a practical perspective, the plastisphere is essentially a natural enrichment of plastic-interacting microbes. By studying plastisphere samples from various sites, scientists hope to discover novel degraders or enzymes. For instance, metagenomic libraries constructed from plastisphere DNA have yielded clones that can degrade model substrates[179][191]. Enzymes uncovered this way might be new types of oxygenases or oxidases tailored to attack plastic. Plastisphere studies have already led to isolation of interesting strains: Ideonella sakaiensis (though for PET) was found in a bottle recycling plant, effectively a man-made plastisphere[192][193]. For PE, Rhodococcus C208 was originally enriched from weathered plastic in soil[194][195]. As another example, Delacuvellerie et al. (2022) examined plastisphere communities from river versus ocean plastics and identified certain Novosphingobium and Thalassospira strains present only on plastics, which are now being tested for degradation ability.

Harnessing the plastisphere for bioremediation could take two forms: (1) bioaugmentation, where a plastisphere-derived consortium is directly applied to plastic waste in hope it will continue its degradation activity, or (2) bioprospecting, where individual organisms or enzymes from plastisphere studies are isolated and then used in engineered systems. The former is tricky because environmental consortia may not thrive outside their native conditions. The latter is more feasible with current technology. Either way, the plastisphere is a rich source of biodiversity and biodegradation potential that is still being tapped. It also serves as a reminder that plastics, while persistent, are not completely inert to life – given enough time, nature is adapting and evolving microbes to tackle this novel substrate. Our job is to accelerate and enhance those natural processes in a safe, controlled manner.

## Current Limitations and Controversies in PE Biodegradation Research

Despite the progress in identifying microbes and devising consortia, the field of PE biodegradation faces several critical challenges and unresolved issues:

- Demonstrating complete mineralization: The ultimate goal is to break polyethylene down into CO₂ (or biomass) with no residual microplastic. To date, no study has conclusively shown 100% mineralization of PE by microbes[15][39]. Most report partial degradation – e.g. weight loss, formation of CO₂ amounting to a fraction of the carbon, or the generation of oxidized intermediates. It remains difficult to prove that what microbes leave behind isn’t just tiny plastic fragments. This is partly a measurement issue: how to detect residual polymer or confirm its absence. Respirometry (CO₂ evolution tests) can indicate mineralization, but if microbes convert PE mostly to biomass, CO₂ might underestimate degradation. On the other hand, weight loss can overestimate degradation if the loss is due to fragmentation (flakes breaking off and not accounted for) or loss of volatile additives. Standardized biodegradation assays (like ASTM D5338 for plastic composting) need to be adapted for PE and consistently used across studies[41][42]. Inconsistencies in past work make it hard to compare results and sometimes lead to over-optimistic claims.

- Distinguishing degradation from deterioration: As discussed, microbes can cause deterioration (surface embrittlement) without truly depolymerizing much of the plastic[8][14]. Some publications have equated formation of a biofilm or slight changes in polymer FTIR spectra with “biodegradation.” Critics point out that those changes could be superficial; real biodegradation should involve significant molecular weight reduction and carbon assimilation by the microbes[37][16]. The review by Montazer et al. (2020) emphasizes defining biodegradation in biochemical terms (like conversion to specified end-products) to avoid confusion[39][196]. Until uniform criteria are adopted (e.g. requiring evidence of mineralization or clear mass balance of carbon), reports of polyethylene “degradation” should be interpreted cautiously.

- Role of additives and pretreatments: Many experiments use pretreated PE (e.g. thermally oxidized, UV-weathered, or containing pro-oxidant additives) to enhance biodegradation[17][197]. While this makes sense to simulate environmental aging, it complicates interpretation. If degradation is observed, is it the additive that was degraded or the PE itself? There have been instances where microbes readily consumed pro-oxidant additives (like fatty acid salts or starch fillers in so-called “oxo-biodegradable” plastics) and produced CO₂, giving a false impression of polymer degradation[42][198]. Future studies are urged to remove additives (e.g. using solvent extraction) from test plastics to ensure that measured biodegradation truly reflects the polymer’s breakdown[42][199]. Conversely, some suggest incorporating specific additives to aid biodegradation – for example, blending PE with a biodegradable polyester so that microbes attacking the polyester leave pores in the PE structure, increasing access. But if not careful, microbes will just degrade the easy part (polyester) and ignore the PE.

- Toxic byproducts: The breakdown of PE can yield various oxidation products like long-chain aldehydes, ketones, and acids[200][113]. Some of these might be toxic to the degrading microbes themselves or to other organisms in the environment. For instance, certain oxidized oligomers could act as antimicrobial agents or induce stress responses that slow degradation. There is still limited knowledge of the toxicity and fate of intermediate products from PE biodegradation[201][202]. If a community suddenly stalls after initial depolymerization, it could be due to accumulation of a noxious intermediate. Comprehensive metabolic profiling and toxicity assays should be conducted on the media after biodegradation to identify any problematic compounds. This will also be important if biodegradation is integrated with downstream processes – knowing the byproducts informs how to further treat or valorize them.

- Slow rates: One of the biggest practical issues is simply that even when microbes can degrade PE, they do so very slowly. Incubation periods of 2–6 months are common in lab studies, often yielding <20% degradation[203][204]. In nature, the process likely takes years. Enhancing the rate is a major challenge. Some approaches to speed it up include providing periodic mild oxidation (e.g. low-dose UV or adding H₂O₂) to complement the biotic action, optimizing physical form (microplastic powder degrades faster than intact film due to higher surface area[205][206]), and ensuring optimal nutrients for the microbes so they aren’t carbon-limited. Yet, fundamentally, breaking C–C bonds is energy-intensive, and microbes won’t do it quickly unless there is a strong selective pressure and energetic benefit. Bioengineering might create strains that constitutively express high levels of needed enzymes or that channel more energy into polymer breakdown than growth, but those strains may have trade-offs in fitness.

- Scale-up and environmental deployment: Taking a lab consortium that works in a flask and using it in a real waste management setting presents multiple questions. How do we deliver the microbes? (In a composting facility? Sprayed onto landfill sites? In bioreactors treating shredded plastic?) Will they compete with native microbes or get outcompeted? There are also biosafety and regulatory concerns – releasing engineered microorganisms into the environment is tightly controlled. One possible route is contained bioprocessing: collect PE waste, pre-treat it, and feed it to a bioreactor with a specialized consortium. This would require the PE to be in small pieces and possibly a slurry, which is energy-intensive to prepare. Also, complete mineralization in a reactor needs capturing any evolved greenhouse gases (CO₂/CH₄), lest we solve one environmental problem but contribute to another.

- Microplastics focus: An area gaining attention is biodegradation of micro- and nano-plastics. These tiny fragments (which result from weathering of larger plastics or are directly released from products) are especially concerning because they can penetrate organisms and even cells. Ironically, their small size might make them more amenable to microbial attack (high surface area, potentially even ingestible by protozoa or small invertebrates). However, their dispersion and ubiquity in the environment make targeting them difficult[207][208]. Few studies have specifically examined microbes that degrade microplastic PE in natural settings – it’s hard to even recover the plastic for analysis. New methods (perhaps using fluorescently labeled model microplastics and tracking their breakdown in microcosms) will be needed. The goal would be to find if certain environmental conditions (like those in wastewater treatment plants or river biofilms) encourage biodegradation of microplastics and whether we can enhance that.

In summary, while the prospect of microbial PE degradation is exciting, one should remain aware of these limitations. Overcoming them will likely require interdisciplinary efforts – improved analytical techniques for tracking carbon flows, better bioreactor engineering for slow processes, and standardized protocols so that results from different studies can be meaningfully compared[41][209]. It’s also essential to manage expectations: biodegrading PE is inherently difficult, and it may be that biological methods are best used in concert with other approaches (like chemical recycling) rather than as a standalone solution for all PE waste.

## Future Perspectives (Next 5–10 Years)

### Enhanced Enzyme Discovery and Engineering

A major thrust in the coming years will be to discover or create faster, more efficient enzymes that can initiate PE depolymerization. Researchers will continue scouring diverse environments (especially extreme ones like Antarctic soils, hot springs, oil reservoirs) for microbes that attack hydrocarbons and plastics. Metagenomic screening of those samples could yield novel oxygenases, oxidases, or even entirely new classes of enzymes capable of breaking the PE backbone. For example, the recent finding of a waxworm saliva enzyme that can oxidize PE at room temperature[117] hints that untapped enzymatic activities exist in nature. Enzymes from insects, marine fungi, or anaerobic consortia might broaden the arsenal beyond the usual laccases and AlkBs. Once candidates are found, protein engineering will accelerate improvements. Techniques like directed evolution and rational design (aided by AI-based protein modeling) could modify enzyme active sites to better accommodate long hydrocarbon chains. One could imagine engineering an alkane monooxygenase to have a larger hydrophobic tunnel, capable of binding a 100-carbon chain (mimicking a segment of PE) and hydroxylating it. Similarly, improving laccase thermostability and redox potential could allow it to generate stronger radicals to attack PE more aggressively[118][56]. Another concept is to create fusion enzymes or enzyme cascades: for instance, a laccase domain linked to an alkane monooxygenase domain, so that one enzyme complex both oxidizes the polymer surface and immediately hydroxylates chain ends – a multi-step depolymerase in one package.

Gene editing tools (like CRISPR) will also enable the metabolic engineering of known PE-degrading strains. We might see Rhodococcus or Pseudomonas strains engineered to overexpress multiple relevant enzymes (e.g. a strain with a bacterial AlkB, a fungal laccase, and a chloroperoxidase all encoded in its genome). By removing regulatory bottlenecks, these “super” strains could constitutively produce a cocktail of enzymes on encountering PE. Synthetic biology might even create designer microbes that sense the presence of polyethylene oligomers and respond by upregulating degradation pathways (a programmed circuit). The challenge will be to ensure that engineered strains remain safe and effective in complex environments, but in contained settings like a bioreactor, this is feasible. Within 5–10 years, it’s plausible we will have one or more optimized enzyme systems that can depolymerize a significant fraction of PE in days rather than months, at least in vitro. The translation of that to in vivo (within a microbial cell or community) will be the next step.

### Integrated Chemical-Biological Upcycling

Complete mineralization of PE to CO₂ is not necessarily the most sustainable outcome – it simply returns carbon to the atmosphere. A forward-looking trend is upcycling: converting plastic waste into useful chemicals or materials. In the future, biodegradation might be coupled with chemical catalysis in hybrid processes. For instance, a mild thermocatalytic step could break PE into a mixture of long-chain hydrocarbons, which microbes then ferment into high-value products (rather than fully oxidizing to CO₂)[210][211]. Recent research is exploring microbes that can transform alkane breakdown intermediates into bioproducts like biosurfactants, bioplastics (PHA), or even drop-in fuels[212][213]. One vision is a biorefinery for plastic waste: PE is depolymerized to C_15–C_20 alkane oils (via oxidation or pyrolysis), then a microbial community or engineered strain converts those into, say, lipids or long-chain alcohols that can be used in cosmetics or as bio-lubricants. Such an approach both disposes of the plastic and creates economic incentives (value-added products)[214][215].

In the next decade, we anticipate development of consortia tailored for upcycling. For example, a consortium might be engineered where one microbe specializes in depolymerizing PE to hexadecanoic acid (palmitic acid), and another microbe consumes palmitic acid to produce a biodegradable polymer or a specialty chemical. The key will be combining polymer degradation pathways with biosynthesis pathways in a single process. With advances in metabolic pathway engineering, microbes could be re-programmed to funnel carbon from polyethylene β-oxidation into specific products (e.g. ethanol, wax esters, acetone, etc.) rather than fully respiring it. Multi-omics-guided design will help optimize these pathways and maximize carbon flux towards the desired product[216][217]. There is also interest in integrating electrobiotechnology – using microbial electrochemical systems where microbes degrade plastic and the released electrons go into electrical current or hydrogen production. While still far-off, these creative couplings could make plastic bioprocessing economically viable.

### Focus on Microplastics and Environmental Deployment

In the coming years, research will likely pivot to more environmentally relevant scenarios. This means studying how consortia operate in natural matrices (soil, sediment, compost) and how to stimulate in situ biodegradation of dispersed microplastics. One approach is bioaugmentation of contaminated sites with plastic-degrading consortia. For example, adding a specialized consortium to a landfill bioreactor or to agricultural soil after film mulch removal, to accelerate breakdown of residual PE fragments. Field trials will be necessary to evaluate if introduced microbes can compete and persist. Another approach is adjusting environmental parameters to favor native degraders – essentially biostimulation. This could be as simple as adding nutrients or electron acceptors to a soil to encourage growth of the plastisphere community, or spraying a solution of harmless surfactants to help microbes access plastic particles. For marine microplastics, perhaps floating bioreactors or “bio-booms” could be deployed: devices that capture microplastics and have biofilms of degrading consortia on them, concentrating the plastic and degrading it in situ. While conceptually intriguing, such interventions will require careful impact assessment to avoid harming ecosystems.

Microplastic degradation in wastewater treatment plants (WWTPs) is another area of interest. WWTPs collect microplastics from urban runoff and could serve as controlled points for biodegradation. Researchers might develop biofilter units coated with PE-degrading biofilms that intercept microplastics in the waste stream and break them down before discharge. Over the next decade, we might see demonstration projects where engineered biofilms in reactors significantly reduce microplastic load in effluents.

Public and regulatory acceptance of microbial solutions will depend on proving that no harmful residues are left and that engineered microbes do not escape or upset natural microbial balances. Thus, expect future efforts to include containment strategies for GMOs (like using auxotrophic strains that cannot survive outside of a reactor) and thorough life-cycle analyses to ensure the process doesn’t inadvertently cause more issues (e.g. excessive greenhouse gas emissions, or incomplete degradation leaving toxic debris).

### Combining Top-Down and Bottom-Up – The Best of Both Worlds

As highlighted in this review, a promising path forward is combining the top-down knowledge from natural plastispheres with bottom-up construction using synthetic biology[218][219]. In the next 5–10 years, we foresee the identification of core microbial communities – minimal sets of species (maybe 3–10 strains) that can be assembled to degrade PE efficiently. These would be derived from repeatedly observed plastisphere consortia in different environments (if multiple independent communities share some common degrader taxa, those are likely key). By harnessing computational models, one could predict how to stabilize such mini-consortia and even enhance them (for example, by adding a “helper” organism that doesn’t degrade PE but provides a necessary vitamin or consumes an inhibitory byproduct).

Adaptive laboratory evolution might also be applied: taking a consortium and passaging it through increasingly challenging conditions (higher plastic concentrations, shorter cycle times) to select for faster degraders. This could effectively breed communities for better performance. Any genetic changes conferring improved degradation could then be pinpointed via genome resequencing of the evolved strains, giving targets for further engineering.

In short, the future likely holds tailored microbial solutions for plastic waste, each optimized for a niche: one consortium for aqueous environments, another for soil, a high-temperature one for industrial reactors, etc. These solutions will be backed by a deep mechanistic understanding (thanks to omics) and possibly augmented by machine learning that helps predict the best community composition or process parameters. Computational models of community metabolism (akin to genome-scale metabolic models, but for multi-species systems) could allow in silico experimentation before wet-lab trials.

### Concluding Outlook

PE plastic biodegradation is transitioning from observational science (cataloging which microbes can eat plastic) to an engineering discipline (designing microbes and processes to deal with plastic). In the next decade, we expect breakthroughs on several fronts: discovery of more potent enzymes and microbes, demonstration of pilot-scale bioreactors converting PE waste to useful outputs, and perhaps in situ treatments for plastic-polluted sites. While it’s unlikely that microbes will entirely solve the plastic problem (especially given the ever-growing volume of waste), they will become an integral part of a multi-pronged approach. This approach includes improved recycling, smarter plastic design (for degradability), and chemical methods – with microbial communities filling the crucial role of dealing with dispersed, hard-to-recover plastic and ensuring complete breakdown of what cannot be otherwise recycled[220][221]. The field is rapidly evolving from “Can anything eat PE?” to “How can we make them eat it faster and beneficially?”. By embracing the complexity of microbial communities and using cutting-edge tools to direct them, scientists and engineers are pushing the boundaries of what’s possible in biodegradation. The hope is that in 5–10 years, bio-augmented remediation of plastic waste will move from lab curiosity to practical reality, contributing to a more sustainable management of plastics and mitigation of environmental pollution.

## References

- Purohit, A., et al. (2025). “Polyethylene biodegradation: A multifaceted approach.” Biotechnology Advances 82:108577. DOI:10.1016/j.biotechadv.2025.108577 – Comprehensive review discussing strategies for developing microbial consortia and engineered enzymes to degrade polyolefins.

- Zhang, C., et al. (2023). “Assembly strategies for polyethylene-degrading microbial consortia based on the combination of omics tools and the ‘Plastisphere’.” Frontiers in Microbiology 14:1181967. DOI:10.3389/fmicb.2023.1181967 – Review covering current knowledge of PE biodegradation stages, key microbes/enzymes, and proposals for top-down & bottom-up consortium design.

- Montazer, Z., et al. (2020). “Challenges with verifying microbial degradation of polyethylene.” Polymers 12(1):123. DOI:10.3390/polym12010123 – A critical review addressing the experimental pitfalls in claiming PE biodegradation and the need for standardized definitions and methods.

- Chamas, A., et al. (2020). “Degradation rates of plastics in the environment.” ACS Sustainable Chemistry & Engineering 8(9):3494–3511. DOI:10.1021/acssuschemeng.9b06635 – Comprehensive review of literature data on environmental lifetimes of various plastics, noting PE’s extremely long half-life (decades to centuries).

- Lucas, N., et al. (2008). “Polymer biodegradation: Mechanisms and estimation techniques.” Chemosphere 73(4):429–442. DOI:10.1016/j.chemosphere.2008.06.064 – Explains general mechanisms (biodeterioration, depolymerization, assimilation, mineralization) for polymer biodegradation and how to evaluate them.

- Restrepo-Flórez, J. M., Bassi, A., & Thompson, M. R. (2014). “Microbial degradation and deterioration of polyethylene – A review.” International Biodeterioration & Biodegradation 88:83–90. DOI:10.1016/j.ibiod.2013.12.014 – Summarizes microorganisms reported to degrade PE and the proposed degradation pathways up to 2014.

- Santo, M., Weitsman, R., & Sivan, A. (2013). “The role of the copper-binding enzyme – laccase – in the biodegradation of polyethylene by the actinomycete Rhodococcus ruber.” International Biodeterioration & Biodegradation 84:204–210. DOI:10.1016/j.ibiod.2012.03.001 – Demonstrates that laccase production by R. ruber (enhanced by copper) leads to significant oxidation and molecular weight reduction of PE.

- Taghavi, N., et al. (2021a). “Degradation of plastic waste using simulated and naturally occurring microbial strains.” Chemosphere 263:127975. DOI:10.1016/j.chemosphere.2020.127975 – Study on using both acclimated environmental consortia and individual isolates (including fungi) to degrade various plastics including PE.

- Jeon, H. J., & Kim, M. N. (2016). “Functional characterization of alkane monooxygenases (AlkB1 and AlkB2) in Pseudomonas aeruginosa for low-molecular-weight polyethylene degradation.” International Biodeterioration & Biodegradation 115:141–146. DOI:10.1016/j.ibiod.2016.08.024 – Finds that AlkB2 plays a greater role than AlkB1 in degrading PE wax, providing insight into oxygenase contributions.

- Skariyachan, S., et al. (2021). “Novel consortia of Enterobacter and Pseudomonas formulated from cow dung exhibited enhanced biodegradation of polyethylene and polypropylene.” Journal of Environmental Management 284:112030. DOI:10.1016/j.jenvman.2021.112030 – Reports an enriched consortium from cow dung that achieved higher degradation of PE/PP films than pure cultures, highlighting synergy between strains.

- Park, S. Y., & Kim, C. G. (2019). “Biodegradation of micro-polyethylene particles by bacterial colonization of a mixed microbial consortium isolated from a landfill site.” Chemosphere 222:527–533. DOI:10.1016/j.chemosphere.2019.01.159 – Describes a two-member bacterial consortium that significantly degraded micro-PE particles over 2 months, with SEM evidence of surface erosion.

- Lou, H., et al. (2022). “Biodegradation of polyethylene by Meyerozyma guilliermondii and Serratia marcescens isolated from the gut of waxworms (Plodia interpunctella larvae).” Science of the Total Environment 853:158604. DOI:10.1016/j.scitotenv.2022.158604 – Demonstrates that a yeast–bacterium consortium from waxworm guts can synergistically degrade PE, identifying degradation products and gene expression changes in the process.

- Joshi, G., et al. (2022). “Unraveling the plastic degradation potentials of the plastisphere-associated marine bacterial consortium as a key player for low-density polyethylene degradation.” Journal of Hazardous Materials 425:128005. DOI:10.1016/j.jhazmat.2021.128005 – Shows that a marine consortium enriched from coastal plastic debris achieved nearly 50% LDPE weight loss in 4 months, and uses sequencing to profile the community and functional genes (including alkB) responsible.

- Zettler, E. R., Mincer, T. J., & Amaral-Zettler, L. A. (2013). “Life in the ‘Plastisphere’: Microbial communities on plastic marine debris.” Environmental Science & Technology 47(13):7137–7146. DOI:10.1021/es401288x – Pioneering study introducing the plastisphere concept, describing the diverse microbial ecology on floating ocean plastics (including PE) and suggesting some may contribute to plastic degradation.

[1] [2] [3] [4] [6] [9] [10] [11] [12] [18] [19] [20] [21] [22] [23] [24] [25] [26] [29] [30] [31] [32] [33] [36] [41] [42] [43] [44] [45] [46] [47] [48] [49] [50] [51] [52] [53] [54] [55] [58] [59] [60] [61] [63] [65] [66] [70] [71] [72] [73] [74] [75] [76] [77] [78] [79] [80] [82] [83] [84] [85] [86] [87] [88] [89] [90] [91] [92] [93] [97] [102] [103] [104] [105] [106] [109] [110] [121] [122] [123] [124] [125] [126] [127] [128] [129] [130] [131] [132] [133] [134] [135] [136] [137] [138] [139] [140] [141] [142] [143] [144] [145] [146] [147] [148] [149] [150] [151] [152] [153] [154] [155] [156] [157] [158] [159] [160] [161] [162] [163] [165] [166] [167] [168] [169] [170] [171] [172] [173] [174] [175] [176] [177] [178] [179] [180] [183] [184] [185] [186] [187] [188] [189] [191] [192] [193] [198] [199] [201] [202] [203] [204] [205] [206] [207] [208] [209] [210] [211] [212] [213] [214] [215] [216] [217] [218] [219] [220] [221] Frontiers | Assembly strategies for polyethylene-degrading microbial consortia based on the combination of omics tools and the “Plastisphere”

https://www.frontiersin.org/journals/microbiology/articles/10.3389/fmicb.2023.1181967/full

[5] [7] [8] [14] [15] [16] [17] [34] [35] [37] [38] [39] [40] [68] [69] [196] [197] Challenges with Verifying Microbial Degradation of Polyethylene

https://www.mdpi.com/2073-4360/12/1/123

[13] [27] [28] Biodegradation of polyethylene: a brief review | Applied Biological Chemistry | Full Text

https://applbiolchem.springeropen.com/articles/10.1186/s13765-020-00511-3

[56] [57] [64] [81] [118] [194] [195]  The role of the copper-binding enzyme - laccase - in the biodegradation of polyethylene by the actinomycete >Rhodococcus ruber> - Ben-Gurion University Research Portal

https://cris.bgu.ac.il/en/publications/the-role-of-the-copper-binding-enzyme-laccase-in-the-biodegradati

[62] [67] [111] [112] [113] [114] [164] [200] Biodegradation of polyethylene by Meyerozyma guilliermondii and Serratia marcescens isolated from the gut of waxworms (larvae of Plodia interpunctella) - PubMed

https://pubmed.ncbi.nlm.nih.gov/36089048/

[94] [95] [96] [98] [99] [100] [101] (PDF) Fungal bioremediation of polyethylene: Challenges and perspectives

https://www.researchgate.net/publication/352999270_Fungal_bioremediation_of_polyethylene_Challenges_and_perspectives

[107] Plastisphere microbiome: Methodology, diversity, and functionality

https://pmc.ncbi.nlm.nih.gov/articles/PMC10989970/

[108] The ecology of the plastisphere: Microbial composition, function ...

https://www.sciencedirect.com/science/article/abs/pii/S0043135421006266

[115] Harnessing and Degradation Mechanism of Persistent Polyethylene ...

https://pmc.ncbi.nlm.nih.gov/articles/PMC12388499/

[116] Evidence of Polyethylene Biodegradation by Bacterial Strains from ...

https://pubs.acs.org/doi/abs/10.1021/es504038a

[117] Wax worm saliva and the enzymes therein are the key to ... - Nature

https://www.nature.com/articles/s41467-022-33127-w

[119] Characteristics and polyethylene biodegradation function of a novel ...

https://www.sciencedirect.com/science/article/abs/pii/S0304389422014492

[120] Discovery of a polyethylene biodegradable laccase from ...

https://aiche.onlinelibrary.wiley.com/doi/10.1002/aic.70005

[181] [190] Plastisphere - Wikipedia

https://en.wikipedia.org/wiki/Plastisphere

[182] Life in the "plastisphere": microbial communities on plastic marine ...

https://pubmed.ncbi.nlm.nih.gov/23745679/