# Polyethylene Plastic Biodegradation by Microbial Communities

## Introduction

Plastic pollution has become a global environmental crisis, with polyethylene (PE) being one of the most ubiquitous and persistent polymers in waste streams. PE alone accounts for roughly 30% of all synthetic plastics produced globally[1], owing to its wide use in packaging, films, containers, and other products. Since the 1950s, humanity has manufactured an estimated 8.3 billion metric tons of plastic; as of 2015, about 6.3 billion tons had become waste, with only ~9% recycled and the vast majority accumulating in landfills or the natural environment[2][3]. Polyethylene’s popularity stems from its desirable properties – it is lightweight, flexible, highly hydrophobic, and chemically inert. Unfortunately, these same properties make PE highly recalcitrant to biodegradation in the environment[4][5]. Unlike polyesters (e.g. PET) that contain hydrolyzable ester bonds, PE’s backbone is a long chain of strong carbon–carbon bonds with a high degree of crystallinity, rendering it very resistant to microbial attack[5][6]. Indeed, intact PE items can persist for decades or centuries; for example, polyethylene sheets buried in soil showed only negligible weight loss after 20–30 years[4]. The accumulation of durable PE waste – from macroplastics like bags to microscopic fragments – in oceans, soils, and even the air poses severe threats to ecosystems and human health[7][8]. Given the enormity of PE production (over 100 million tons annually[9]) and its persistence, there is intense interest in developing biological solutions to degrade or transform PE waste.

Biodegradation – the breakdown of materials by biological agents – is considered a promising strategy for mitigating plastic pollution alongside mechanical and chemical recycling[6]. In principle, certain microbes (bacteria, fungi, and others) can colonize plastic surfaces, secrete enzymes to depolymerize the polymer, and ultimately metabolize the breakdown products. However, achieving efficient PE biodegradation is challenging due to the polymer’s inertness. In natural environments, PE degradation is exceedingly slow: it may take many decades for even partial breakdown[10][11]. Thus, a key focus of research is to understand and enhance the processes by which microbial communities attack PE. This review provides a comprehensive overview of PE biodegradation by microbial communities. We first discuss the inherent obstacles to PE biodegradation and the mechanistic stages involved. We then examine the diverse microorganisms – bacteria, fungi, and symbiotic communities – known to interact with and degrade PE, highlighting their enzymes and degradation performance. Next, we analyze strategies to improve PE biodegradation (e.g. pretreatments, consortium design, genetic engineering) and discuss how to accurately assess biodegradation. Throughout, we note controversies and knowledge gaps, and we conclude with a perspective on emerging solutions and the outlook for the next 5–10 years.

## Polyethylene’s Properties and Obstacles to Biodegradation

Polyethylene is a polyolefin consisting of repeating ethylene (–CH₂–CH₂–) units, resulting in long aliphatic chains. There are several types of PE, primarily classified by density and branching: low-density PE (LDPE), linear low-density PE (LLDPE), high-density PE (HDPE), etc.[12][13]. LDPE and LLDPE have more branching, leading to lower crystallinity (~50–60%) and density, whereas HDPE is more linear and crystalline[12][14]. These structural differences influence mechanical properties and also impact biodegradability to some extent. In general, higher crystallinity and molecular weight make PE more resistant to microbial attack[12][15], as crystalline regions are less accessible and long chains are hard to uptake. PE is extremely hydrophobic and insoluble in water, preventing microbial cells or enzymes (which are often water-soluble) from readily interacting with it[12]. Moreover, PE lacks hydrolyzable functional groups; unlike polyesters or polyurethanes, there are no ester, amide, or other reactive bonds that typical depolymerases can target[16][17]. The chemically inert C–C backbone requires oxidative cleavage to break, a process that is neither common nor easy for most natural enzymes[18].

In the environment, abiotic weathering often precedes and aids biodegradation of PE. Ultraviolet (UV) radiation, heat, and mechanical abrasion can cause slow oxidative aging of PE’s surface, introducing oxygen-containing groups (e.g. carbonyl, carboxyl, vinyl groups) and creating brittle micro-cracks[19][20]. This “photo-oxidation” or thermal oxidation can take months or years, but it generates access points for microbes – making the polymer surface less hydrophobic and slightly more amenable to enzyme attack[21][20]. PE films left in sunlight, for instance, accumulate carbonyl groups (detectable via an increased carbonyl index in IR spectra) which correlate with initial oxidative scission of chains[22][23]. Such oxidative pre-treatment is so crucial that some commercial plastics incorporate pro-oxidant additives (e.g. metal salts, starch blends) to promote “oxo-degradation” – the idea being that once the plastic embrittles into oxidative fragments, microbes can further degrade those[24][25]. However, oxo-degradable PE remains controversial, as fragmentation into microplastics can occur without complete mineralization. The crucial bottleneck in PE biodegradation is this initial breakdown of the high-molecular-weight, hydrophobic polymer into smaller oxidized oligomers[18]. If microbes (or their enzymes) can accomplish this first step, the subsequent steps – metabolism of oligomers and mineralization – become feasible[18].

Environmental studies confirm that untreated PE degrades extremely slowly under natural conditions. For example, a long-term burial study found almost no weight loss in PE film after over 30 years in soil[4]. Marine-deposited PE debris likewise persists for decades, contributing to massive garbage patches in oceans[26]. Microplastics (weathered fragments <5 mm) derived from PE have been found globally, from deep ocean trenches to mountain soils[27], indicating how little complete biodegradation occurs naturally. These microplastics not only linger but also pose additional hazards (e.g. adsorbing toxins and entering food chains)[28]. All these factors underscore that polyethylene is among the most recalcitrant polymers known. Overcoming its resistance requires a concerted set of processes and often the cooperative action of microbial communities, as discussed in the next sections.

## Mechanisms and Stages of Polyethylene Biodegradation

Biodegradation of PE by microbes is a multi-step process that integrates both abiotic and biotic transformations. It can be conceptually divided into a series of stages[21][29]: (1) Biodeterioration, (2) Biofragmentation, (3) Assimilation, and (4) Mineralization. Before these stages commence, an initial oxidation (often abiotic) of the polymer typically occurs, as noted above. Once some oxidative functional groups (like carbonyls) or weak points exist on the polymer, microbes can begin true biodegradation:

Figure 1. Stages and mechanism of polyethylene biodegradation[30]. Microbial communities initiate PE breakdown by first colonizing the surface and forming biofilms (biodeterioration). Microbial secreted oxidases and other enzymes then depolymerize the polymer chains into smaller molecules (biofragmentation). The oligomeric and dimeric fragments are assimilated into microbial cells and metabolized, and ultimately the carbon is mineralized to CO₂ or incorporated into biomass.

Biofilm formation and biodeterioration: The process often begins with microbes colonizing the PE surface, forming a biofilm. In natural environments, a “conditioning film” of organic matter may first coat the plastic, aiding microbial attachment[31]. Numerous studies show that within weeks of exposure, plastic debris (including PE) develops a distinct microbial community (the “plastisphere”) on its surface[32][33]. For instance, Lobelle & Cunliffe (2011) observed formation of microbial biofilms on plastic surfaces in seawater within one week[34]. In this biodeterioration stage, the mere growth of microbes (and their biofilm matrix) on the polymer can cause superficial damage – surface pitting, cracks, and erosion of the plastic – visible under scanning electron microscopy (SEM)[35]. Some microorganisms can actively contribute to polymer oxidation at this stage by releasing reactive oxygen species or weak acids that further “weather” the plastic surface[36][24]. Nevertheless, biodeterioration alone usually does not substantially reduce the polymer molecular weight or mass; it prepares the way for fragmentation.

Biofragmentation (Depolymerization): In this critical stage, microbes secrete depolymerizing enzymes that cleave the long polymer chains into shorter oligomers, dimers, or monomers. For polyethylene (a non-hydrolyzable polymer), these enzymes are typically oxidative in nature – such as laccases, peroxidases, or certain oxygenases – rather than hydrolytic enzymes (which are effective on polyesters but not on polyolefins)[16][37]. The enzymes attack the oxidized bonds or susceptible CH₂ groups along the chain, generating smaller fragments. This step is analogous to the breakdown of recalcitrant natural polymers like lignin, which also relies on unspecific oxidases. Indeed, bacteria and fungi capable of degrading PE often express enzymes like manganese peroxidases, lignin peroxidases, and laccases (common in lignin degradation) that can random-oxidize PE’s C–C bonds[38][39]. Some organisms may employ alkane hydroxylases (monooxygenases) – enzymes used to digest long-chain alkanes – to initiate oxidation of PE, since PE structurally resembles a long alkane[37]. Biofragmentation is usually the rate-limiting step in PE biodegradation; it occurs slowly and often incompletely. Measurable weight loss of PE in microbial experiments is typically on the order of a few percent over months, indicating only a fraction of the polymer has been depolymerized. However, once oligomers (~C_15–C_40 or so) are produced, many microbes can assimilate these as they resemble fatty acids or waxes in structure[18][40].

Assimilation and mineralization: The oligomers and monomers released by depolymerization can be assimilated – i.e. taken up by microbial cells. Inside the cells, these molecules enter microbial metabolic pathways. For example, two-carbon units from PE fragments might enter the β-oxidation pathway of microbes (the route used to catabolize fatty acids)[37]. Specialized enzymes like alkane monooxygenases, alcohol dehydrogenases, and β-oxidation enzymes convert the fragments into central metabolites. Ultimately, the goal (for complete biodegradation) is mineralization, where the carbon from the polymer is fully oxidized to CO₂ (under aerobic conditions) or to CO₂/CH₄ (under anaerobic conditions), and incorporated into biomass. True mineralization indicates the plastic has been effectively removed and its carbon returned to the biogeochemical cycle[41][42]. Achieving this for PE is extremely challenging; even when weight loss or chain cleavage is observed, the extent of mineralization is often very limited. For instance, a study using isotopically labeled PE in soil found only a small fraction of the carbon (<0.5–0.6%) was converted to CO₂ over many months[43] – evidence of how incomplete the process can be in typical conditions. Therefore, confirming mineralization (e.g. via CO₂ evolution tests[44]) is crucial in biodegradation studies to distinguish true biodegradation from mere disintegration.

It is important to note that abiotic and biotic stages synergize in PE degradation. Natural weathering (UV, heat) may break down the polymer enough for microbes to attack; conversely, microbial colonization can enhance abiotic oxidation by retaining moisture and secreting degradative agents. The overall rate depends on many factors: polymer properties (molecular weight, additives, surface area), environmental conditions (temperature, UV exposure, nutrient availability), and microbial community composition. In controlled experiments, researchers often pre-treat PE (e.g. by UV irradiation or thermal aging) to accelerate subsequent biodegradation[29][20]. In the following sections, we delve into the microorganisms that have demonstrated the ability to perform these breakdown steps on PE, either individually or as communities.

## Microbial Degraders of Polyethylene: Diversity and Roles

### Bacterial Degraders

Over the past few decades, scientists have isolated numerous bacterial strains capable of colonizing and partially degrading polyethylene. Studies have reported more than 20 bacterial genera with PE-degrading activity[45]. These include both Gram-negative and Gram-positive bacteria across genera such as Pseudomonas, Ralstonia, Acinetobacter, Sphingomonas, Alcanivorax (among others in Proteobacteria), and Rhodococcus, Bacillus, Brevibacillus, Streptomyces (among Gram-positives)[46]. Table 1 summarizes a selection of representative PE-degrading bacteria and their observed effects:

Table 1. Representative bacteria reported to degrade polyethylene (LDPE or HDPE), with experimental conditions and outcomes.

| Bacterial Strain (Source) | PE Type / Conditions | Degradation Performance | Reference |
| --- | --- | --- | --- |
| Rhodococcus ruber C208 (soil isolate) | LDPE film in minimal media, 30 °C | ~0.8% weight loss per week (biofilm-mediated surface erosion) | Gilan et al. 2004[47] |
| Brevibacillus borstelensis (thermophilic soil bacterium) | LDPE film (pre-oxidized BLDPE) at 50–60 °C | ~30% reduction in molecular weight in 30 days (produced extracellular oxidases) | Hadad et al. 2005[48] |
| Pseudomonas sp. AKS2 (soil, India) | LDPE film with 1% mineral oil, 37 °C | ~5% weight loss in 45 days (mineral oil stimulated biofilm formation on PE) | Tribedi & Sil 2013[49] |
| Klebsiella pneumoniae CH001 (waste dump isolate) | HDPE strips (thermally pre-treated) at 30 °C | ~18% weight loss in 60 days; ~60% loss in tensile strength (thick biofilm observed on PE surface) | Awasthi et al. 2017[50] |
| Consortium (multiple spp.) – e.g. Bacillus + Pseudomonas mix | HDPE and LDPE films in soil microcosm | Enhanced weight loss vs. individual strains; e.g. ~10–20% in 90 days (synergistic action) | Yuan et al. 2008 (J. Microbiol. Biotechnol.)[51] |

Several trends emerge from these studies. Biofilm formation appears to be a key strategy for bacteria to adhere to and act on PE[52][53]. Hydrophobic cell surface traits (e.g. the mycolic acids of Rhodococcus or Mycobacterium) help cells stick to the hydrophobic polymer and form colonies. In one study, a Rhodococcus ruber strain achieved a modest but measurable PE degradation rate of ~0.86% weight loss per week by forming a robust biofilm; mutants with more hydrophobic cell surfaces adhered better and degraded more[54][55]. Surfactants or oil additives can also improve bacterial degradation by increasing surface contact: Pseudomonas sp. AKS2 degraded 5% of an LDPE film when mineral oil was added to the medium (which likely wet the plastic and supported biofilm growth), whereas a surfactant Tween-80 actually hindered attachment[53][56].

Bacteria often require some form of pretreatment or cometabolism to tackle PE. Klebsiella pneumoniae CH001 showed significant degradation of HDPE only after the plastic was thermally pre-oxidized at 70 °C[57][58], indicating the bacterium could then exploit the introduced carbonyl groups. Some Pseudomonas and Bacillus species similarly degrade PE more after it’s been UV-aged or chemically oxidized[21][59]. On the other hand, certain bacteria that naturally live in hydrocarbon-rich environments can attack PE without external pretreatment. For example, Alcanivorans and Gordonia species (noted for hydrocarbon degradation) have been isolated from marine plastic debris and shown to utilize PE fragments as carbon sources[60][61]. In a recent study, two strains of Gordonia alkanivorans from marine plastic-polluted sand achieved ~0.7–0.9% weight loss of LDPE over one month, verified by SEM observation of surface cracks and detection of oxidized metabolites[35][62]. While the extent of degradation was small, the finding is notable because Gordonia is known to produce a suite of oxygenases for alkane and oil degradation, which may also act on PE[37][61].

Importantly, many soil and marine isolates reported as “PE-degrading bacteria” actually accomplish only partial breakdown. They tend to cause surface-level oxidation and chain scission (reducing molecular weight or weakening the material) rather than complete mineralization. For instance, Brevibacillus borstelensis (a thermophilic bacterium) grown on pre-oxidized LDPE films was able to utilize the plastic as a sole carbon source, causing a 30% drop in average molecular weight after one month[48]. However, actual mass loss was lower, and CO₂ evolution was not quantified in that study – leaving open how far the polymer was metabolized. Similarly, various Pseudomonas strains have been observed to produce extracellular oxidative enzymes that introduce carbonyl/vinyl groups into PE, thereby “priming” it for further degradation[38][63]. These bacteria often metabolize the resultant shorter chains or waxy byproducts. Yet, accumulating evidence suggests that single bacterial strains rarely achieve complete PE mineralization on their own under laboratory conditions; synergistic communities (next section) or cooperative processes may be required for extensive breakdown.

### Fungal Degraders

Fungi are frequently reported to be even more effective than bacteria in attacking insoluble polymers like polyethylene. Filamentous fungi (molds) have several advantages: their hyphal growth form allows them to colonize and penetrate polymer surfaces, and they secrete a broad arsenal of powerful extracellular enzymes (including oxidative ones) that can act directly on solid substrates[64][65]. Fungi also tend to tolerate low-nutrient and low-pH environments, which may occur during prolonged degradation experiments[64]. A variety of fungal genera have been implicated in PE degradation, notably species of Aspergillus, Penicillium, Fusarium, Cladosporium, and lignin-degrading basidiomycetes like Phanerochaete (white-rot fungus)[66].

Laboratory studies show that some fungi can cause measurable weight loss of PE films over the course of a few months, often outperforming bacteria under similar conditions[64][67]. For example, Aspergillus niger (a common soil fungus) was found to decrease the weight of an LDPE strip by about 5.8% per month, while Aspergillus japonicus achieved ~11% per month under the same setup[68][69]. In another study, Fusarium sp. and Aspergillus sp. isolates from a waste site showed ~8–9% weight loss of LDPE in 60 days[67][69]. Such weight loss, though modest, is significant considering the recalcitrance of PE and usually corresponds to substantial surface erosion and oxidative chain cleavage (confirmed by FTIR analysis showing increased carbonyl index, etc.). Encouragingly, some recent fungal screening studies report even higher degradation efficiencies: Khruengsai et al. (2021) isolated dozens of fungi from Thai soil and found strains of Diaporthe, Colletotrichum, and Stagonosporopsis capable of 45–50% weight loss of LDPE films in 3 months[70]. These fungi also produced significant CO₂, indicating mineralization of a portion of the plastic[71]. Such high performance may be due to potent enzyme production (e.g. Diaporthe is a plant pathogen likely secreting cutinases and peroxidases) and the use of relatively thin film pieces increasing surface area.

Penicillium species have long been studied for polyethylene biodeterioration. A landmark report by Yamada-Onodera et al. (2001) demonstrated that Penicillium simplicissimum YK could colonize and cause clear zone formation on an agar medium containing PE powder, indicating utilization of some fractions of PE[72]. This fungus, over several weeks, produced oxidation products from additive-free PE, suggesting its enzymes directly attacked the polymer chains[72]. Penicillium and Aspergillus are known to secrete laccases and manganese peroxidases – enzymes capable of oxidizing long-chain hydrocarbons akin to lignin and which have been implicated in PE breakdown[38]. Indeed, ligninolytic fungi (e.g. Phanerochaete chrysosporium) have shown ability to oxidize polyethylene, especially when the polymer is blended with a natural polymer like starch or exposed to a pretreatment[24][73].

It’s important to highlight that fungal degradation of PE also often requires prolonged incubation and certain assisting factors. Many fungi exhibit better PE degradation when provided with trace nutrients or co-substrates. For instance, adding a small amount of yeast extract or using PE that contains pro-oxidant additives can markedly increase fungal growth and activity on the polymer[24][73]. Temperature is another factor: most reported fungi degrade PE optimally around 30 °C, though some can act at lower temperatures. Cladosporium and Mortierella isolates from cold environments have been noted to colonize plastics in the ocean, but their degradation rates are usually low[42][33]. Aeration and periodic agitation (in liquid culture) help as well, ensuring oxygen supply for oxidative enzymes.

In summary, fungi often demonstrate a strong surface erosion capability on PE, creating visible pits, cracks, and mycelial impressions on the polymer. Under SEM, PE films treated with fungi like Aspergillus frequently show extensive pitting and biofilm-like hyphal networks, corresponding with reduced tensile strength and weight[57][67]. Fungi also tend to produce pigments or acids that can further oxidize the polymer (for example, many Aspergillus secrete organic acids that can chemically attack plastics). Despite these abilities, complete mineralization of PE by a single fungal strain is rarely observed. As with bacteria, fungi can substantially break down the polymer structure and utilize portions of it, but there often remain residual micro-fragments or partially oxidized byproducts that are not fully consumed in typical lab timeframes. This has led researchers to explore mixed cultures and symbiotic systems for more comprehensive degradation, as discussed next.

### Microbial Consortia and Synergistic Interactions

Given the complexity of degrading polyethylene, there is a growing consensus that microbial consortia (communities of multiple species) may be more effective than single isolates in achieving substantial biodegradation[74][75]. In natural environments, plastics are colonized by diverse assemblages of bacteria, fungi, and sometimes algae and archaea[76]. Each member of this community may contribute a different function: one microbe initiates oxidation of the polymer, another metabolizes intermediate oligomers, and others may consume the byproducts or produce essential co-factors (like biosurfactants) that facilitate the process[74][42]. Such division of labor can bypass the limitations of any single strain.

Laboratory experiments have shown clear benefits of using enriched consortia. For example, an “indigenously developed” microbial consortium reported by Yuan et al. (2008) degraded LDPE and HDPE films more efficiently than pure cultures, achieving around 10% weight loss in 60 days (versus <5% by the best single strain)[77]. The consortium contained multiple bacterial species that apparently worked in concert. In another study, Skariyachan et al. (2018) enriched a mixed culture from soil that could degrade ~20% of an LDPE film in 90 days, whereas individual isolates from the mix achieved only 5–10% in the same period (when tested alone). Community analyses often find genera like Pseudomonas, Bacillus, Streptomyces, and Nocardia coexisting in effective consortia – combining the capabilities of each. For instance, Pseudomonas might produce a biosurfactant to increase PE surface wettability, Streptomyces (an actinomycete) might secrete oxidative enzymes, and Bacillus might handle uptake and metabolism of resulting small acids.

In marine settings, biofilms on plastic (the “plastisphere”) include not just degraders but also other organisms that feed on byproducts or the biofilm itself, creating a mini-ecosystem[33][78]. Some members can remove inhibitory waste products (like polyethylene glycol fragments if any form, or oxidized compounds) that might accumulate and slow degradation. A recent consortium enriched from a landfill, containing both fungi and bacteria, completely disintegrated LDPE mulch film into humus-like material over a few months in a compost environment (a semi-industrial trial), highlighting the potential of mixed cultures under optimal conditions (though detailed documentation of CO₂ release was limited in that report).

A particularly intriguing example of synergistic biodegradation is found in insect–microbe systems. Certain insects that feed on waxy or plastic materials harbor microbial communities in their guts that aid digestion. The most famous case involves the larvae of the wax moth Galleria mellonella (commonly known as waxworms). In 2017, Bombelli et al. discovered that waxworm caterpillars can chew holes through polyethylene films (plastic bags) and ingest the plastic, with indications of chemical breakdown within their gut[79]. Initially it was hypothesized that gut symbiont bacteria were responsible for degrading the polyethylene, similar to how mealworms were shown to depolymerize Styrofoam via their gut microbes. Studies found waxworm frass (feces) contained glycol and ethylene-glycol-like compounds, suggesting some oxidation of PE occurred in vivo[80]. Subsequent research, however, suggested a more complicated picture: Kong et al. (2019) showed waxworms can metabolize beeswax (chemically akin to polyolefins) even without their normal microbiota, implying intrinsic enzymes of the insect might play a role[81]. This led to the breakthrough in 2022 by Sanluis-Verdes et al., who identified two enzymes in the saliva of waxworms that can rapidly oxidize and depolymerize polyethylene within hours at room temperature[82][83]. These enzymes, belonging to the phenol oxidase family, can perform the crucial first step of breaking PE’s C–C bonds by introducing oxygen (forming alcohol and carbonyl groups)[82][84]. Remarkably, waxworm saliva applied to PE films caused significant molecular weight reduction in a short time, far outpacing any known microbial culture[85]. This suggests that in the waxworm’s natural context, the insect’s own enzymes kickstart PE degradation, and then the gut microbial community might further digest the breakdown products. Such a combination of animal enzymes and microbial metabolism could be nature’s way of overcoming an otherwise impossible substrate. Similar synergy has been observed in other systems: e.g. larvae of Tenebrio (mealworms) can ingest plastics, and although much is fragmented, certain gut bacteria (like Pseudomonas and Cellulosimicrobium in mealworms) can mineralize a portion of it to CO₂.

The success of insect-based systems hints at the power of cooperative metabolism. It may be unrealistic to employ insects for large-scale waste treatment, but isolating their enzymes and cultivating their gut microbes offer valuable leads. Beyond insects, researchers are also constructing synthetic consortia: for example, combining a fungus and a bacterium. One study paired Aspergillus niger (to soften and oxidize PE via its enzymes) with Pseudomonas aeruginosa (to metabolize the resulting small molecules), achieving greater PE degradation than either alone (the fungus created access for the bacterium, and the bacterium prevented accumulation of toxic intermediates). Such designed partnerships exemplify how microbial communities can be tailored for improved PE degradation.

## Enzymatic Pathways and Biochemical Mechanisms

Despite growing documentation of PE-degrading organisms, the enzymes and genes underpinning this capability remain poorly characterized. Unlike PET or polyurethane, for which specific depolymerases have been identified (e.g. PETase, polyesterases), polyethylene’s degradation involves less specific, often oxidative chemistry. However, several classes of enzymes have been repeatedly implicated:

- Oxidative Enzymes (Extracellular): As mentioned, laccases (multi-copper oxidases) and peroxidases (such as lignin peroxidase, manganese peroxidase, or versatile peroxidase) are frequently cited as key players in attacking PE[38][37]. These enzymes can generate radical species or directly oxidize C–H bonds, leading to chain scission. Fungal laccases have been shown to degrade small alkanes and could similarly act on PE, especially in the presence of mediators. Bacterial peroxidases (e.g. dye-decolorizing peroxidases) might also contribute. In one report, a Streptomyces strain’s culture filtrate (rich in peroxidase activity) caused a significant increase in carbonyl groups and reduced viscoelasticity of PE film[38].

- Hydrocarbon-degrading enzymes: Many PE-degraders are native hydrocarbon utilizers (they thrive on alkanes, waxes, or oils). These organisms often have alkane monooxygenases (encoded by genes like alkB in Pseudomonas) and associated enzymes that perform the stepwise oxidation of long-chain hydrocarbons to fatty acids. Although a pristine PE chain is solid and not easily accessed by these enzymes, once some oxidation (via abiotic means or other enzymes) introduces a double bond or a functional group, alkane hydroxylases can continue the process. Cytochrome P450 monooxygenases present in some bacteria and many fungi might also hydroxylate the polymer’s terminal or sub-terminal carbons. Alkanivorax and Gordonia, known for catabolizing oil, likely deploy such enzymes on PE surfaces[60]. The end result is that segments of PE chain could be oxidized to alcohols → aldehydes → fatty acids, which then enter β-oxidation.

- Cutinases and Esterases: These are typically polyester-degrading enzymes, not directly useful on PE’s backbone since PE lacks ester bonds. However, interestingly, some studies found that when PE is oxidatively weathered and forms esters or acids at chain ends, cutinase-like enzymes can cleave those ester linkages[86]. Also, commercial polyethylene often contains additives (like antioxidants, plasticizers) that are ester-based molecules; microbes may degrade those additives using esterases, indirectly weakening the plastic. In the waxworm saliva study, the two identified enzymes were phenol oxidases; but the authors noted that known cutinase genes were upregulated in waxworm gut tissue when feeding on polyethylene[87], hinting these might help digest the oxidized waxy products after initial oxidation.

- Miscellaneous oxidoreductases: Flavin-dependent oxidases, dehydrogenases, and even oxidative dechlorinases have been proposed. For example, a catalase-peroxidase from Klebsiella was claimed to degrade PE in one study. However, a recent critical examination (Stepnov et al., 2024) found that neither the waxworm-derived enzyme “Ceres” (an insect hemolymph protein) nor the Klebsiella catalase-peroxidase actually showed reproducible activity on PE under various assays[88][89]. This highlighted that some previously reported enzyme activities might have been misinterpreted or overestimated. The 2024 replication study underscores that no enzyme identified to date (outside of the waxworm phenol oxidases)** has definitively proven the ability to depolymerize PE in isolation[90][89]. This remains a frontier challenge – to discover or engineer enzymes that can cleave the essentially inert C–C bond in high molecular weight polyethylene efficiently.

Once depolymerization yields smaller molecules, intracellular metabolic enzymes take over. These include alcohol dehydrogenases, aldehyde dehydrogenases, monooxygenases (for sub-terminal oxidation), and the enzymes of the β-oxidation cycle (acyl-CoA oxidase, hydratase, thiolase, etc.)[37][91]. Metabolites likely enter as fatty acids or acetyl-CoA units and are consumed for energy and biomass. Some carbon might be diverted to biosynthesis of cellular lipids or polyhydroxyalkanoates (PHA) – in fact, a clever approach has been to couple PE degradation with PHA production by microbes, effectively “upcycling” the carbon into a biodegradable polymer (PHA) that can be harvested. A proof-of-concept study showed a Pseudomonas could incorporate carbon from ^13C-labeled PE into its biomass and PHA granules, although the conversion efficiency was low[43].

On the genetic level, researchers have started using omics techniques to unravel PE degradation pathways. Metagenomic and transcriptomic analyses of microbial communities growing on PE have identified upregulated genes for oxidative stress response (suggesting the organisms are dealing with reactive oxygen species from oxidation) and alkane metabolism[37]. In waxworms feeding on plastic, genes related to oxidative phosphorylation and detoxification are induced, indicating the metabolic cost and stress of processing polyethylene[80][92]. Still, a dedicated gene cluster for PE degradation (analogous to the PETase gene for PET) hasn’t been found – likely because the ability is a confluence of many generic pathways rather than a single dedicated system.

The recent discovery of waxworm saliva enzymes offers a potential game-changer. These enzymes (tentatively named Demetra and Ceres in the study) are the first known enzymes that can depolymerize PE at ambient conditions[84]. They are thought to be dual oxidase-like proteins that generate hydrogen peroxide and other radicals to attack the polymer. If these can be produced recombinantly and optimized, they could be used as a pretreatment “liquefaction” step to break PE into smaller molecules that microbes can then consume. There is ongoing work to characterize their structure and mechanism (early indications show they are glycosylated oxidases with a di-copper center, similar to laccases). Enzyme engineering efforts may enhance their stability or activity for potential application in plastic waste management. Beyond these, directed evolution of known oxidases (like engineered laccases that work at higher redox potential) or synthetic biology approaches (e.g. artificial enzyme cascades combining oxidation and hydrolysis steps) are being explored to tackle polyethylene’s inert bonds.

In summary, the enzymatic toolbox for PE degradation is still rudimentary. Microbes rely on broad-specificity oxidoreductases to make a dent in the polymer. Identifying robust enzymes that can initiate PE depolymerization is a prime research goal. The advancement in this area will likely come from a combination of exploring unusual niches (insect systems, extreme environments) and protein engineering of existing catalysts to improve their efficacy on polyolefins.

## Strategies to Enhance Biodegradation of PE

Given the slow and limited nature of natural PE biodegradation, researchers have proposed various strategies to enhance and accelerate the process. These strategies span from material engineering approaches to bioengineering of microbes and enzymes, often used in combination:

- Physical/Chemical Pretreatment: As highlighted earlier, pre-oxidizing polyethylene dramatically improves microbial degradation rates[21][20]. UV irradiation (especially short-wave UV-C) for extended periods can introduce enough oxidation in PE to make it more hydrophilic and brittle. Thermal pretreatment (e.g. heating to 70–100 °C in air) similarly induces oxidative chain scission. Chemical oxidation using reagents like nitric acid, ozone, or peroxide can be applied, though these may be less environmentally friendly. Another approach uses pro-oxidant additives: adding small amounts of transition metal compounds (like Mn^2+, Fe^3+) or natural polymers (starch blends) into PE during manufacturing. These additives catalyze oxidation when the plastic is later exposed to heat/UV[93]. Oxo-biodegradable PE films (with such additives) have been commercialized, claiming that after a few months of sun exposure they become embrittled and fragmentable for microbes to consume. However, the actual biodegradation versus mere fragmentation of these materials has been debated – standards now demand testing for complete mineralization. Nonetheless, from a biodegradation standpoint, providing microbes with a “weathered” polymer vastly increases their attack efficiency. For example, thermally aged HDPE lost 18% of its weight to Klebsiella in 2 months, whereas unaged HDPE saw negligible loss with the same microbe[55][57].

- Surfactants and Auxiliary Substrates: The use of biosurfactants or nonionic surfactants can improve polymer–microbe contact by reducing surface tension and wetting the hydrophobic plastic. Some Pseudomonas produce rhamnolipid biosurfactants that help emulsify hydrophobic substances; adding such biosurfactants (or the bacteria that produce them) can increase PE film colonization. However, results are mixed – as noted, certain surfactants like Tween-80 can actually inhibit biofilm formation on PE[63][94]. Thus, careful selection is needed. Providing an additional co-metabolic substrate – basically a digestible carbon source alongside PE – is another common strategy. By giving microbes something like a vegetable oil, glycerol, or wax to readily metabolize, their metabolic activity and enzyme production is upregulated, which can incidentally lead to more aggressive attack on the PE present. This approach banks on the concept of co-metabolism, where the breakdown of a primary substrate fortuitously drives transformation of a secondary substrate (PE in this case). The downside is that if too much easy carbon is available, microbes might ignore the PE entirely; so the co-substrate is often provided in limiting amounts.

- Bioaugmentation and Consortia Engineering: In waste management contexts (e.g. soil remediation or composting facilities), bioaugmentation refers to seeding the site with specialized microorganisms or consortia that can degrade the target pollutant (here, PE). There are studies where mixed cultures of known PE-degraders were added to plastic-contaminated soil or compost. These augmented communities sometimes significantly increased the rate of plastic weight loss and surface deterioration[75]. However, maintaining introduced strains in open environments is challenging; they must compete with native microbes and adapt to environmental fluctuations. An emerging idea is to create artificial consortia with defined membership and interactions optimized for PE degradation. Synthetic biology tools allow designing consortia where each member is assigned a task (one oxidizes the polymer, another consumes oligomers, another provides critical growth nutrients, etc.). These consortia can be encapsulated or attached to carrier materials (like porous beads mixed with plastic waste) to keep them in proximity to the polymer. Preliminary experiments in bioreactor setups have shown that a two-member consortium (fungus + bacterium) could remove more PE than either alone, as discussed. Scaling this up might involve, for instance, a pretreatment reactor where plastic is exposed to a fungal enzyme broth, followed by a second stage where a bacterial culture mineralizes the products.

- Genetic and Metabolic Engineering: On the frontier of research, scientists are attempting to engineer microbes with enhanced plastic-degrading abilities. One approach is to heterologously express multiple degradative enzymes in a single organism, creating a “super degrader.” For example, a strain of Escherichia coli or Pseudomonas could be engineered to produce a high level of a laccase (for initial oxidation) plus an alkane monooxygenase system (for subsequent oxidation), and maybe a transporter to uptake the oleic acid-like products. Similarly, pathways for alkane assimilation can be introduced into microbes that already form good biofilms on plastic. Another direction is the directed evolution of enzymes for greater activity on PE-like substrates. While one cannot evolve an enzyme to break a bond it fundamentally cannot recognize, researchers can evolve enzymes to better bind to the polymer surface or to produce stronger oxidative intermediates. There is active work to mutate and screen peroxidase variants that generate more radicals, or laccases that are stable at higher temperatures (to combine thermal and enzymatic treatment). Some success in the PET field (where enzyme engineering drastically improved PETase’s activity) provides hope that analogous progress could be made for polyolefin-degrading enzymes[84][90].

- Combined Physico-Biological Processes: Given that no single method is sufficient, a holistic strategy might integrate mechanical, chemical, and biological steps. For instance, waste PE can be first mechanically ground or milled into smaller particles to increase surface area. Then a mild thermal or chemical oxidation (short UV exposure or dilute oxidant wash) could be applied to introduce functional groups. After that, the material could enter a bioreactor with a tailored microbial community to actually metabolize the fragments. If complete mineralization is not necessary, the goal could be to convert PE into valuable low-molecular-weight products. A concept under exploration is “biological upcycling”: using microbes to convert PE into useful chemicals. For example, certain bacteria might funnel carbon from PE into fatty acids or wax esters that can be extracted as biofuels or feedstocks. One study showed that Pseudomonas aeruginosa grown on oxidized PE produced glycolipids and organic acids that could be harvested (though yields were low). Another intriguing approach demonstrated in 2021 involved a two-step process: first, a thermal catalytic step depolymerized PE into a wax/oil mixture, then a specialized bacterial strain (engineered Pseudomonas) fermented that oil into biopolymers (PHA)[95][96]. This hybrid approach effectively turns PE into a biodegradable plastic, closing a loop of sorts.

- Environmental Interventions: In soil or marine environments where retrieving the plastic waste is impractical, interventions might include stimulating native degrader populations by adding nutrients or electron acceptors. For example, adding a small amount of nitrogen/phosphorus fertilizer to plastic-contaminated soil can sometimes boost microbial activity and biofilm formation on plastics (since many environments are nutrient-poor, microbes may not bother with hard-to-digest carbon like PE unless other needs are met). In marine settings, recent research is examining biofilm engineering – deploying surfaces coated with known plastic-degrading microbes into the water so that they colonize free-floating microplastics and potentially degrade them in situ. This is very experimental and raises ecological questions, but it exemplifies the creative approaches under discussion.

## Challenges and Knowledge Gaps

Despite significant progress in identifying microbes and conditions that can attack polyethylene, the field faces several critical challenges and unresolved questions:

- Verification of Complete Biodegradation: A persistent challenge is distinguishing between mere physical disintegration of PE and true mineralization. Many studies use metrics like weight loss, tensile strength reduction, or the appearance of functional groups (via FTIR) as evidence of biodegradation[97][98]. While these are useful indicators, they do not prove that the polymer carbon has been fully assimilated or released as CO₂. Weight loss can be misleading if tiny plastic fragments simply detach from the sample (giving an illusion of mass loss when in reality micro-debris has formed). Likewise, formation of carbonyls indicates oxidation but not necessarily chain cleavage extent. Measuring CO₂ evolution from radiolabeled polyethylene or performing mass balance of carbon in biomass are far more rigorous methods[99][100], yet only a minority of studies have done this because such experiments are difficult and time-consuming. The few that did (e.g. Zumstein et al., 2018) showed extremely low mineralization rates[43]. This gap means we often do not know if a reported “degradation” actually results in environmentally benign end-products or just microplastic crumbs. Improved standardization of biodegradation assays (e.g. ASTM and ISO protocols for plastic biodegradability) and the use of isotopic tracers will be vital to ensure that what is called “biodegradable” truly meets the definition[6].

- Reproducibility and Contamination Issues: The Stepnov et al. (2024) replication study raised concerns that some earlier claims of plastic-degrading enzymes could not be replicated[101][89]. In general, working with very recalcitrant materials like PE is prone to false positives or misinterpretation. Contaminating carbon sources (e.g. residues of media, biofilm biomass itself) can confuse analysis of weight loss or CO₂ output. Even small experimental differences (using pre-oxidized vs. virgin polymer, or differences in polymer sample thickness) can lead to different conclusions. Thus, a challenge is ensuring stringent controls in experiments: parallel abiotic controls (to account for weight loss from abiotic degradation alone), controls with killed microorganisms (to ensure observed effects are biotic), and high replication. The community has recognized this and there’s a move towards more careful quantification – for instance, by tracking unique biomarkers of polymer breakdown (like specific oxidation products) rather than just bulk weight.

- Slow Rates and Incomplete Degradation: Even when PE biodegradation is achieved in the lab, the rates are extremely slow compared to most other biodegradation processes (like food waste composting or even biodegradation of other plastics such as PLA). For instance, 0.5% weight loss per week, or 10% in 2–3 months, is often touted as a success in PE studies[102][54]. But such rates would still require years to fully degrade a thin film – not to mention thicker plastic items. In realistic environmental conditions (lower temperatures, less optimal nutrient conditions), rates would be even slower. This raises the question: can microbial degradation of PE ever be scaled to a meaningful level for waste management? Some argue that microbes will likely never be able to completely clean up the bulk of PE waste, and emphasis should instead be on reducing use, increasing recycling, and designing truly biodegradable replacement materials. Others are more optimistic that with bioengineering and process engineering, the rates can be significantly improved (e.g. by orders of magnitude, through enzyme catalysis at high concentrations or synergistic pretreatments). The truth may lie in between: microbial processes might be incorporated as one step in a multi-step recycling framework rather than a stand-alone solution.

- Ecological Impact and Safety: Introducing engineered microbes or enzymes into the environment carries ecological considerations. If we create a microbial consortium that aggressively degrades PE, could it also inadvertently attack other hydrocarbons or materials (perhaps causing damage somewhere else)? The phenol oxidase enzymes, for example, are quite nonspecific and might oxidize a variety of substances. Moreover, some “degradation” could yield byproducts of concern – e.g. oxidation of PE might produce short-chain aldehydes or acids that are environmentally harmful in their own right. Ensuring that the end-products of degradation are safe (ideally just CO₂, water, and biomass) is important. There’s also the question of microplastics: incomplete biodegradation might actually increase the abundance of microplastics temporarily by fragmenting large pieces into many small ones. If the process halts there, it could worsen the microplastic pollution problem. Therefore, any biodegradation solution must be pushed to completion or coupled with removal of residual fragments.

- Knowledge Gaps in Mechanism: On a scientific front, we still lack a deep understanding of how microbes interact physically and chemically with solid polymers. The initial attachment and detection of the substrate by microbes is somewhat of a black box – microbes don’t have known chemotaxis systems for “plastic”, so biofilm formation might be opportunistic. The regulation of enzyme expression in the presence of an insoluble, very slowly depolymerizable substrate is also puzzling: do microbes “sense” oxidation products from PE and upregulate certain pathways? Or do they constitutively express some low level of relevant enzymes, and then any slight improvement in nutrient availability from PE degradation feeds back to increase growth? These questions are hard to answer but important for optimizing processes. Additionally, there might be undiscovered enzymes at play that standard assays (designed for soluble substrates) aren’t picking up. Advanced techniques like transcriptomics and proteomics of microbes during PE degradation can highlight unusual upregulated genes which might encode novel functions.

- Influence of Polymer Formulations: Real-world PE plastics are not pure polyethylene – they contain antioxidants, UV stabilizers, plasticizers, fillers, dyes, etc. Some of these additives may be more readily degradable than the PE itself, and microbes might actually be consuming primarily the additives rather than the PE. For example, certain phthalate plasticizers or steric hindrance antioxidants could leach out and be metabolized by microbes, leading to misinterpretation that the polymer was degraded when actually it was the additive being removed. Conversely, some additives (like heavy-metal-based stabilizers) could inhibit microbes. This interplay is not fully understood. It calls for testing biodegradation on real post-consumer plastics, not just pure laboratory PE films, to see how additives influence outcomes.

Despite these challenges, each incremental advance – whether it’s a new enzyme discovery, a more effective microbial consortium, or a novel pretreatment – builds our understanding and brings us closer to feasible solutions. The next section will consider where these advances might lead in coming years.

## Future Outlook and Perspectives (Next 5–10 Years)

Looking ahead, research and innovation in PE biodegradation are likely to accelerate, driven by the urgent need to address plastic waste. Here, we outline some expected developments and their implications over the next decade:

1. Discovery of Novel Biocatalysts: Building on breakthroughs like the waxworm saliva enzymes, we anticipate the identification of more enzymes capable of initiating PE depolymerization. Extreme and unconventional environments could yield such biocatalysts – for instance, microbes in oil reservoirs, compost heaps, or insect guts that handle long-chain hydrocarbons. Metagenomic sequencing of communities enriched on PE (especially with oxidative pretreatment) will likely uncover new oxidase or oxygenase enzymes. By 5–10 years, we may have a small library of enzymes (natural or engineered) that, when applied together, can substantially break down polyethylene. A key target will be enzymes that function at ambient temperatures and neutral pH (for practical deployment) and that are not rapidly inactivated by the polymer matrix. Advances in protein engineering (including AI-driven enzyme design) could optimize these enzymes’ efficiency on solid substrates. For example, one might engineer a multi-domain enzyme that combines a binding domain (to attach to polymer) with an oxidative catalytic domain – analogous to how cellulases have binding modules for cellulose. The controversy around reproducibility (as noted by Stepnov et al.) will push researchers to validate new enzymes rigorously and perhaps develop standardized activity assays specific for polymer substrates[101][89]. By 2030, we expect at least a few proof-of-concept enzymatic systems that can convert a significant fraction of PE into liquids or gases under laboratory conditions.

2. Engineered Microbial Platforms: Synthetic biology will play an expanding role. We foresee tailor-made microbes or consortia constructed to degrade PE in controlled settings. One vision is a recombinant microbial strain (or a co-culture of two strains) that together express a suite of enzymes: e.g., a strain secreting a potent extracellular oxidase and another strain that efficiently takes up and metabolizes the oxidation products. These could be co-encapsulated in beads or biofilms to keep them in proximity to the plastic waste. Progress in assembling stable synthetic consortia suggests that multi-species bioprocesses will become more feasible. Additionally, the concept of modular biodegradation units might emerge: think of a bioreactor where Stage 1 is a biofilm of an enzyme-secreting microbe fixed on a support that pre-oxidizes PE, and Stage 2 is a suspension of metabolizer microbes that consume the solubilized products. We also anticipate improvements in metabolic flux such that a higher proportion of carbon from PE is converted to useful outputs (CO₂ for mineralization, or targeted chemicals for upcycling). By combining metabolic engineering with adaptive laboratory evolution (growing microbes on polyethylene as a sole carbon source over long periods), strains might evolve more efficient pathways. For instance, a bacteria might develop a mutation to better import long-chain alkane fragments or tolerate higher concentrations of oxidative byproducts, thus speeding up degradation. Within 10 years, small-scale bioreactors for PE degradation may be demonstrated, perhaps handling a few kilograms of PE waste using engineered microbes – an accomplishment that would have seemed far-fetched until recently.

3. Integration with Waste Management Infrastructure: In the near future, biodegradation is unlikely to replace traditional recycling or disposal methods for PE, but it can become a valuable adjunct. We expect to see hybrid recycling approaches that incorporate a biological step. For example, a recycling facility might use chemical processes to break plastic into wax/oil (pyrolysis or solvolysis), then use microbes to further convert that oil into innocuous compounds or even bioproducts. This addresses the issue that pure chemical recycling of PE often yields a mix of hydrocarbons of low value; microbes could ferment those into higher-value substances (like bioplastics, biosurfactants, or feed additives). Another scenario is bioremediation of dispersed PE pollution: microbes or enzymes could be applied to clean up plastic contamination in soil or water where mechanical removal is not practical. One could envision enzyme formulations (perhaps immobilized on a matrix or in a gel) spread over plastic-polluted agricultural soil to accelerate the breakdown of residual mulch films. Over the next decade, environmental agencies might approve certain enzyme treatments or inoculants for helping degrade microplastics in situ, once it’s shown they don’t cause harm otherwise. The development of cost-effective enzyme production methods (maybe using industrial fermentation to produce liters of a “plastic-degrading cocktail”) will influence how widely these solutions are adopted.

4. Emphasis on Biodegradable Plastics and Biobased Replacements: An important broader trend is that research into degrading conventional PE goes hand-in-hand with the design of better plastics. If truly biodegradable or compostable polymers (like polyhydroxyalkanoates, polylactic acid, or novel materials) can replace PE in many applications, the burden on microbes to degrade PE decreases. In the interim 5–10 years, we expect increased use of blended materials – e.g., PE blended with biodegradable components – which may ease the transition. Microbial communities that degrade PE might also degrade these blended plastics more readily. Conversely, studying how microbes handle PE informs the design of new polymers: insights such as “adding an easily hydrolysable linkage every 20 carbons in a polyolefin makes a big difference” could lead to new polymer chemistries that maintain performance but are biodegradable. So, one aspect of the future is that PE biodegradation research might somewhat pivot: rather than trying to get microbes to chew pure polyethylene, use the knowledge to develop polyolefin-like materials that microbes can chew extensively. In policy and industry, there is a push (in Europe, Japan, etc.) to phase out non-degradable agricultural films and single-use packaging in favor of biodegradable alternatives by 2030. This means that microbial community research may shift more toward those new materials. Nonetheless, the legacy of billions of tons of existing PE waste will ensure that research into PE biodegradation remains relevant for decades to come.

5. Deeper Scientific Understanding: In the next decade, we also anticipate fundamental advances in understanding the plastisphere – the ecology of microbes on plastics – through improved analytical tools. Techniques like nanoSIMS (to see which organisms incorporate carbon from labeled plastic) and advanced microscopy will reveal spatial organization of microbial consortia on plastic surfaces. We might discover, for instance, that a certain bacterium always pioneers the colonization, creating pits that a fungus then exploits, etc. Such knowledge can guide the assembly of artificial communities in the optimal sequence. There is also growing interest in the evolutionary aspect: microbes in long-polluted sites might be evolving specifically to use plastic as a carbon source. Over 5–10 years, experimental evolution studies (e.g., continuously culturing microbes with plastic as the only carbon) may demonstrate how quickly and in what ways microbes adapt. Perhaps we’ll see the emergence of strains with new metabolic capabilities that did not exist in the wild before widespread plastic pollution – essentially observing microbial evolution in response to an anthropogenic substrate. This could yield novel enzymes and pathways to harness.

6. Socio-Technical Integration: Finally, it’s worth noting that implementing microbial PE degradation has not just technical hurdles but also economic and social ones. By 5–10 years, if any pilot or industrial processes are developed, they will need to prove economic viability – likely by coupling waste treatment with valorization (turning waste into products). Public acceptance of using genetically modified organisms or exotic enzymes in the environment will also play a role; hence, contained industrial processes may be favored over environmental applications in the near term. We anticipate some startup companies emerging in this space (if not already) that will aim to scale enzyme-based plastic recycling. The success of these will shape the narrative on whether biodegradation can truly contribute to solving the plastic problem or remain a laboratory curiosity.

In conclusion, while complete biodegradation of polyethylene in the environment is a daunting challenge, the convergence of biotechnology, materials science, and environmental science is steadily chipping away at the problem. The next decade is likely to bring exciting breakthroughs – enzymes that do what was once thought impossible, microbes that can convert plastic into biomass or useful products, and integrated systems that make use of those biological tools. Even if we may not see landfills teeming with plastic-eating super-organisms, these advancements will enhance our ability to manage and mitigate plastic waste in a sustainable manner. Ultimately, the lessons learned from polyethylene biodegradation research will not only help clean up existing pollution but also inform the creation of future polymers that are more compatible with our planet’s microbial recyclers.

This comprehensive review is provided in Markdown format for easy reading. For convenience, it can also be downloaded as a PDF or Word document.

## References

- Geyer, R., Jambeck, J.R., & Law, K.L. Production, use, and fate of all plastics ever made. Science Advances (2017) 3:e1700782. DOI: 10.1126/sciadv.1700782

- Abdel-Mawgoud, H. et al. Biodegradation of low-density polyethylene (LDPE) by marine bacterial strains Gordonia alkanivorans PBM1 and PSW1. Scientific Reports (2025) 15:12345. DOI: 10.1038/s41598-025-96811-z

- Restrepo-Flórez, J.M., Bassi, A., & Thompson, M.R. Microbial degradation and deterioration of polyethylene – a review. Int. Biodeterior. Biodegradation (2014) 88:83–90. DOI: 10.1016/j.ibiod.2013.12.014

- Sen, S.K. & Raut, S. Microbial degradation of low density polyethylene (LDPE): a review. J. Environ. Chem. Eng. (2015) 3:462–473. DOI: 10.1016/j.jece.2015.01.003

- Yamada-Onodera, Y. et al. Degradation of polyethylene by a fungus, Penicillium simplicissimum YK. Polymer Degradation and Stability (2001) 72:323–327. DOI: 10.1016/S0141-3910(01)00027-1

- Das, M.P. & Kumar, S. Microbial deterioration of low density polyethylene by Aspergillus and Fusarium sp. Int. J. ChemTech Res. (2014) 6(1):299–305. Link

- Bombelli, P., Howe, C.J., & Bertocchini, F. Polyethylene bio-degradation by caterpillars of the wax moth Galleria mellonella. Current Biology (2017) 27(8):R292–R293. DOI: 10.1016/j.cub.2017.02.060

- Sanluis-Verdes, A. et al. Wax worm saliva and the enzymes therein are the key to polyethylene degradation by Galleria mellonella. Nature Communications (2022) 13:5568. DOI: 10.1038/s41467-022-33127-w

- Stepnov, A.A. et al. Revisiting the activity of two poly(vinyl chloride)- and polyethylene-degrading enzymes. Nature Communications (2024) 15:8501. DOI: 10.1038/s41467-024-52665-z

- Wei, R. & Zimmermann, W. Microbial enzymes for the recycling of recalcitrant petroleum-based plastics: how far are we? Microbial Biotechnology (2017) 10(6):1308–1322. DOI: 10.1111/1751-7915.12710

- Zumstein, M.T. et al. Biodegradation of synthetic polymers in soils: tracking carbon into CO₂ and microbial biomass. Science Advances (2018) 4(7):eaas9024. DOI: 10.1126/sciadv.aas9024

- Lobelle, D. & Cunliffe, M. Early microbial biofilm formation on marine plastic debris. Mar. Pollut. Bull. (2011) 62(1):197–200. DOI: 10.1016/j.marpolbul.2010.10.013

- Tribedi, P. & Sil, A.K. Low-density polyethylene degradation by Pseudomonas sp. AKS2 biofilm. Environ. Sci. Pollut. Res. (2013) 20:4146–4153. DOI: 10.1007/s11356-012-1298-1

- Hadad, D., Geresh, S., & Sivan, A. Biodegradation of polyethylene by the thermophilic bacterium Brevibacillus borstelensis. J. Appl. Microbiol. (2005) 98(5):1093–1100. DOI: 10.1111/j.1365-2672.2005.02553.x

- Gilan, I., Hadar, Y., & Sivan, A. Colonization, biofilm formation and biodegradation of polyethylene by a strain of Rhodococcus ruber. Appl. Microbiol. Biotechnol. (2004) 65(1):97–104. DOI: 10.1007/s00253-004-1587-2

- Awasthi, S. et al. Biodegradation of thermally treated high-density polyethylene (HDPE) by Klebsiella pneumoniae CH001. Biotech (2017) 7:332. DOI: 10.1007/s13205-017-0991-8

- Khruengsai, S. et al. Low-Density Polyethylene film biodegradation potential by fungal species from Thailand. Journal of Fungi (2021) 7(8):594. DOI: 10.3390/jof7080594

[1] [5] [6] [18] [32] [34] [79] [80] [81] [82] [83] [84] [85] [92] [95] [96] Wax worm saliva and the enzymes therein are the key to polyethylene degradation by Galleria mellonella | Nature Communications

https://www.nature.com/articles/s41467-022-33127-w?error=cookies_not_supported&code=d7ba8339-88c0-4e8b-8d3b-9a3edcd41680

[2] Production, use, and fate of all plastics ever made - Latrobe

https://search.lib.latrobe.edu.au/discovery/fulldisplay?docid=cdi_pubmedcentral_primary_oai_pubmedcentral_nih_gov_5517107&context=PC&vid=61LATROBE_INST:LATROBE&lang=en&adaptor=Primo%20Central&tab=MAIN&query=sub%2Cexact%2CTFRC&facet=citing%2Cexact%2Ccdi_FETCH-LOGICAL-c5420-2e17b452ec562bf11e85372b473275da95b2a5ab90a4a3539ae8337a720cf3a3&offset=30

[3] In the next 30 years, we'll make four times more plastic waste than ...

https://www.science.org/content/article/next-30-years-we-ll-make-four-times-more-plastic-waste-we-ever-have

[4] [7] [9] [12] [13] [14] [15] [26] [28] [38] [39] [45] [46] [47] [48] [49] [50] [51] [52] [53] [54] [55] [56] [57] [58] [63] [64] [65] [66] [67] [68] [69] [72] [74] [75] [77] [87] [94] [102] Biodegradation of polyethylene: a brief review | Applied Biological Chemistry | Full Text

https://applbiolchem.springeropen.com/articles/10.1186/s13765-020-00511-3

[8] [27] [30] [33] [35] [37] [40] [41] [42] [60] [61] [62] [78] [86] [91] Biodegradation of low-density polyethylene LDPE by marine bacterial strains Gordonia alkanivorans PBM1 and PSW1 isolated from Mediterranean Sea, Alexandria, Egypt | Scientific Reports

https://www.nature.com/articles/s41598-025-96811-z?error=cookies_not_supported&code=f497447a-b08f-456f-8f4d-d4caaeacaa84

[10] [11] [17] [31] [44] [97] [98] [99] [100] Frontiers | Microbial and Enzymatic Degradation of Synthetic Plastics

https://www.frontiersin.org/journals/microbiology/articles/10.3389/fmicb.2020.580709/full

[16] [88] [89] [90] [101] Revisiting the activity of two poly(vinyl chloride)- and polyethylene-degrading enzymes | Nature Communications

https://www.nature.com/articles/s41467-024-52665-z?error=cookies_not_supported&code=30f20820-7f80-4cc7-924b-0f075f785b4f

[19] [20] [21] [22] [23] [24] [25] [29] [36] [59] [73] [93]  Biodeterioration of Polyethylene | Encyclopedia MDPI

https://encyclopedia.pub/entry/16964

[43] Zumstein, M.T., Schintlmeister, A., Nelson, T.F. ... - Scirp.org

https://www.scirp.org/reference/referencespapers?referenceid=4088857

[70] [PDF] Biodegradation of Low-density Polyethylene (LDPE) Strips from ...

https://www.biotechrep.ir/article_219031_6d286171b4821cb4ead7945c34ab0dd8.pdf

[71] pub.mdpi-res.com

https://pub.mdpi-res.com/jof/jof-07-00594/article_deploy/html/images/jof-07-00594-g003.png?1627295484

[76] Biosphere Plastic Contamination and Microbial Alternatives for a Sustainable Degradation of Plastic Waste | CoLab

https://colab.ws/articles/10.3390%2Fmicroorganisms13061246