# Polyethylene Plastic Biodegradation by Microbial Communities

## Introduction

Plastic pollution has become one of the most pressing environmental challenges of our time. Polyethylene (PE), a polyolefin polymer consisting of a long aliphatic carbon backbone, is the most widely produced plastic globally – accounting for roughly 38% of plastic demand[1]. Its extensive use in packaging, bags, and containers has led to enormous accumulation of PE waste in landfills and natural habitats. Unlike biopolymers or certain polyesters, PE’s chemically inert C–C chain structure confers extreme resistance to biodegradation[2][3]. In fact, the estimated environmental half-life of PE ranges from decades to centuries[4][5]. This persistence, combined with low recycling rates, means that PE waste is now ubiquitous in soil, oceans, and even remote ecosystems, fragmenting into microplastics that further infiltrate food webs.

Conventional disposal methods like landfilling and incineration are problematic: landfilling merely sequesters plastic for future generations, while incineration generates greenhouse gases and toxic residues[6]. Mechanical recycling of PE is also limited by material degradation and contamination[7]. Biodegradation, the breakdown of plastics by living organisms, offers a tantalizing sustainable alternative. If naturally occurring or engineered microbes can mineralize PE into biomass, CO₂, water, and other harmless products, this could close the loop on plastic life-cycles[8][9]. However, achieving effective biodegradation of polyethylene has proven extremely challenging. The polymer’s high molecular weight, hydrophobicity, crystallinity, and lack of readily hydrolyzable bonds all impede microbial attack[10][11]. Only in recent years have researchers begun to identify microbes – bacteria, fungi, and even insect gut symbionts – with the remarkable ability to colonize and slowly decompose PE materials[12][13].

In this review, we examine the state of the art in PE plastic biodegradation by microbial communities. We first discuss the unique challenges of PE degradation and the general mechanisms by which microbes overcome its recalcitrance. We then survey the diverse microorganisms known to attack PE, including specialized bacteria, filamentous fungi, and symbiotic consortia (e.g. in insect guts). A critical analysis of microbial community strategies – natural “plastisphere” communities on plastic debris and artificial consortia designed in the lab – is provided, highlighting how synergistic interactions can enhance PE breakdown. Throughout, we compare single-organism approaches with community-based degradation, noting controversies (such as the true extent of biodegradation vs. mere fragmentation) and knowledge gaps (e.g. unidentified key enzymes). Finally, we offer a perspective on emerging trends and future directions, including omics-guided consortium design, enzyme discovery, and the integration of biodegradation with plastic upcycling. Our goal is to provide a comprehensive and critical overview for advanced researchers in biotechnology and environmental microbiology, charting the progress and prospects in this challenging field.

## Challenges and Mechanisms of Polyethylene Biodegradation

Why is polyethylene so difficult to biodegrade? Several material properties of PE confer its recalcitrance. First, PE’s backbone is a long, saturated hydrocarbon chain lacking functional groups (e.g. esters, amides) that typical depolymerase enzymes recognize[11]. The C–C bonds have high bond dissociation energy and are not prone to hydrolysis. Second, PE is highly hydrophobic and often partially crystalline, so water and enzymes have trouble accessing the polymer chains[10][11]. High crystallinity regions (common in high-density PE) are tightly packed and impermeable, leaving only amorphous regions for microbial attack[14]. Third, the molecular weight of PE (often hundreds of kDa) is far above what microbes can directly assimilate; polymer chains must be depolymerized into oligomers (~C_10–C_50_) or smaller before transport into microbial cells[15]. These factors mean that under natural conditions, unassisted PE degradation is extremely slow – on the order of decades – and usually requires prior environmental weathering (UV exposure, thermal oxidation, etc.) to introduce oxidation sites[11][16].

Stages of microbial PE degradation: Despite these challenges, certain microbes can colonize and degrade PE by a sequence of steps[17][18]. The generally accepted stages are:

- Surface Colonization – Microbes initially attach to the inert PE surface, often forming a biofilm. They may secrete extracellular polymeric substances (EPS) or biosurfactants to help adhere to the hydrophobic plastic[19]. Biofilm formation is critical; it not only anchors the microbes but can also create microenvironments (e.g. local pH changes, redox conditions) that promote subsequent steps[20]. Notably, biofilm growth on PE surfaces can cause pitting and micro-cracks, as observed via electron microscopy[21][22].

- Biodeterioration – Once attached, microbes begin to physically and chemically deteriorate the polymer surface. They secrete enzymes (e.g. lipases, oxidative enzymes) and metabolites that initiate bond cleavage or weaken the plastic matrix[23]. Filamentous fungi and actinomycetes can also exert mechanical forces; fungal hyphae penetrating into polymer crevices can break the material apart[24]. Metabolic byproducts like organic acids or peroxides may further erode the polymer surface[25]. This stage creates surface defects and introduces oxygen-containing functional groups (e.g. carbonyls), “priming” the PE for fragmentation. Indeed, oxidative pretreatments that create carbonyl groups greatly enhance subsequent biodegradation[11][16].

- Biofragmentation – The actual depolymerization of PE occurs via biofragmentation, where extracellular oxidative enzymes or free radicals cleave the long polymer chains into shorter oligomers, dimers and monomers[26]. Because microbes cannot directly ingest high-MW polymers, fragmentation is a prerequisite to further metabolism[26]. Polyethylene, being an alkane polymer, lacks a specific depolymerase (unlike PET which has PETase, for example). Instead, oxidative enzymes play the key role. Laccases (multicopper oxidases) and peroxidases from certain microbes can attack the C–C backbone by abstracting electrons to form free radicals, leading to chain scission[13][27]. Alkane hydroxylases, such as monooxygenases in hydrocarbon-degrading bacteria, can initiate oxidation at polymer chain ends or at accessible points in amorphous regions[28][29]. This yields alcohol or acid chain-ends. Repeated oxidative attacks can shorten PE molecules progressively. It is thought that PE must be broken down to ~500 Da oligomers (tens of carbons long) or smaller to permit microbial uptake[26]. Biofragmentation is often the rate-limiting step and may proceed only slowly without abiotic aid. For instance, pure cultures often achieve only a few percent of PE weight loss over months (see Table 1 below), indicating incomplete fragmentation in most laboratory tests.

- Assimilation – Once the polymer is depolymerized into oligomers and monomers (e.g. long-chain alkanes, fatty acids, etc.), these small molecules can be transported into microbial cells[30]. The microbes then assimilate these carbon products as substrates for metabolism. Common metabolic pathways come into play: for example, β-oxidation for fatty acids or alkanotroph pathways for alkanes. In many PE-degrading bacteria, genes for alkane degradation and fatty acid β-oxidation are upregulated when grown on PE, suggesting they assimilate oxidized fragments similarly to natural hydrocarbons[31][32]. During assimilation, the carbon from PE fragments is incorporated into microbial biomass or funneled into central metabolism (e.g. as acetyl-CoA units).

- Mineralization – Finally, the assimilated carbon is fully metabolized to inorganic end products (mineralized). Under aerobic conditions, the ultimate products are CO₂ and H₂O; under anaerobic conditions, CH₄ may also be produced[33]. True biodegradation is often defined by substantial mineralization (e.g. >50% conversion to CO₂ in standard tests). However, few studies achieve complete mineralization of PE. More commonly, partial breakdown yields biomass plus some residual oligomers. Verifying mineralization is a key challenge – CO₂ evolution tests or isotopic tracing are needed to confirm that carbon in PE ends up as CO₂. Many early studies relied on weight loss or the appearance of carbonyl groups as evidence of degradation, which can be inconclusive (e.g. weight loss can result from micro-fragmentation or loss of additives rather than complete carbon utilization). We return to this issue in Controversies.

Figure 1. Stages of microbial polyethylene biodegradation. Microbes first attach to the PE surface and form biofilms (i), then secrete enzymes/metabolites that cause surface deterioration (ii). Oxidative enzymes fragment the polymer into oligomers (iii), which are assimilated into microbial cells (iv) and ultimately mineralized to CO₂, H₂O (and CH₄ under anoxic conditions) (v)[17][26]. Environmental weathering (UV, heat) can augment microbial action by introducing reactive functional groups on PE (shown at top). (Adapted from Gu 2003 and recent studies)[17][18]

## Microorganisms Involved in PE Degradation

Over the past two decades, researchers have isolated a variety of microorganisms – across different taxa and environments – that can attack polyethylene to some extent. Initially, many studies focused on single strains from soils or landfills enriched with plastic. More recently, attention has shifted to complex communities (discussed in the next section). Here we summarize the key microbial players: bacteria, fungi, and symbiotic organisms (e.g. insect gut microbes) known to colonize and degrade PE, along with their distinctive mechanisms.

### Bacteria

Bacteria are the most frequently reported PE degraders, thanks to their metabolic diversity and ubiquity in plastic-polluted sites. Many belong to genera well-known for hydrocarbon or xenobiotic degradation. Commonly reported PE-degrading bacteria include Bacillus, Pseudomonas, Rhodococcus (and related actinomycetes), Arthrobacter, Acinetobacter, and Enterobacter, among others[34][35]. These typically come from soil, compost, landfill leachate, or marine biofilms where plastic waste is present. Table 1 provides representative examples of bacteria and their PE biodegradation performance.

Table 1. Representative polyethylene-degrading microbes and their biodegradation performance. (Selected studies demonstrating weight loss or other evidence of PE degradation by isolated strains and consortia.)

| Microorganism (Source) | PE Substrate & Conditions | Degradation Observations | Reference |
| --- | --- | --- | --- |
| Brevibacillus sp. strain 707 (soil) | LDPE film; 50 °C; 30 days | ~11% weight loss of PE film | Hadad et al. 2005[36][37] |
| Pseudomonas aeruginosa (acidic hot spring soil) | LDPE film; pH 5, 44 °C; 30 days | ~6.3% weight loss; surface oxidation observed | Mouafo Tamnou et al. 2021[36] |
| Enterobacter sp. D1 (waxworm gut isolate) | Polyethylene film; 28 °C; 31 days | ~10% weight loss; biofilm with pits on PE surface | Ren et al. 2019[38][39] |
| Consortium: Bacillus + Paenibacillus (landfill) | PE microparticles; 30 °C; 60 days | ~14.7% of PE (by mass) degraded | Park & Kim 2019[40][41] |
| Consortium: Marine plastisphere bacteria (mixed) | LDPE film; seawater; 120 days | 47 ± 7% weight reduction (substantial fragmentation) | Joshi et al. 2022[42][43] |

Data: Weight loss refers to reduction in mass of PE samples after incubation. Conditions are simplified; many studies use additional nutrients or pretreatments.

These examples illustrate that single bacterial strains typically achieve modest PE degradation (a few percent weight loss over 1–2 months), whereas tailored consortia or naturally adapted communities can yield much higher breakdown (tens of percent in similar timescales)[44][42]. Notably, thermophilic bacteria like Brevibacillus have shown relatively high degradation (11%) presumably because higher temperatures increase polymer chain mobility and enzyme activity[37]. Likewise, acidophilic conditions in the P. aeruginosa study improved degradation – acidity can help hydrolyze oxidized bonds or swell the polymer[36].

A recurring theme is that many PE-degrading bacteria are also competent at degrading hydrocarbons or other plastics. For instance, Bacillus and Pseudomonas species appear frequently and are also key degraders of PET, polyurethane, polypropylene, etc.[45]. These genera produce a variety of catabolic enzymes and are readily enriched in waste environments. Actinomycetes (e.g. Rhodococcus, Streptomyces) are another important group[46]. As filamentous bacteria, actinomycetes form branching hyphae and resilient biofilms, aiding surface penetration. Rhodococcus ruber strain C208 is a classic example that can grow on polyethylene films; intriguingly, it was found to secrete an extracellular laccase enzyme that significantly enhanced PE oxidation and depolymerization (especially in the presence of copper ions as cofactor)[46][47]. Rhodococcus and related actinomycetes also possess cytochrome P450 alkane monooxygenases and other oxidative enzymes that likely participate in attacking PE’s C–C bonds[28][29].

It is important to stress that no bacterium isolated to date completely mineralizes PE on its own under laboratory conditions – degradation is usually partial. Many isolates rely on co-metabolism (degrading PE only in presence of another easier carbon source) or require pre-oxidized PE to show activity[48][49]. Still, the discovery of new strains continues. For example, Acinetobacter (often known for oil degradation) and Paenibacillus from landfill soils have been identified that cling to PE and cause slow erosion[50][51]. Extremophilic bacteria (thermophiles, halophiles, etc.) have also been tested, given that extreme conditions (heat, salt) might help break PE’s structure; some extremophiles indeed show potential for PE degradation at high temperature or salinity[52]. As isolation techniques improve (e.g. high-throughput culturing, metagenomic screening), we expect more diverse bacteria to be identified.

### Fungi

Fungi are nature’s expert decomposers and have a special role in plastic biodegradation. Several features make fungi particularly effective against recalcitrant polymers: they grow as mycelia that can physically penetrate and break up materials, and they secrete a broad arsenal of extracellular enzymes (including oxidative enzymes) that can depolymerize complex substrates[53][13]. In soils, fungi are key in degrading lignin and other durable biopolymers, so researchers have long hypothesized they could tackle synthetic polymers like PE. Indeed, numerous fungi have been reported to colonize and biodeteriorate PE films, especially Aspergillus, Penicillium, Fusarium, Cladosporium, and related genera[54][55]. These tend to be common soil or saprophytic fungi known for versatile metabolism.

One advantage of fungi is their ability to adhere to and grow across hydrophobic surfaces. Fungi produce hydrophobins and other proteins that improve attachment to hydrophobic materials[56]. Once attached, fungal hyphae can wrap around and crack plastic surfaces, as observed under microscopy[24]. The mechanical disruption by hyphae increases the surface area accessible to enzymatic action. Furthermore, many fungi excrete ligninolytic enzymes (like laccase, manganese peroxidase, lignin peroxidase) that generate reactive radicals capable of attacking C–C bonds in polyethylene[13][57]. For example, white-rot fungi (such as certain Penicillium and Phanerochaete species) have been shown to cause oxidation and partial depolymerization of PE, evidenced by the formation of carbonyl groups on the polymer after fungal treatment[13][27].

Studies have isolated fungi from plastic-rich sites and demonstrated their abilities: Aspergillus niger and Aspergillus tubingensis are frequently cited for growing on polyethylene films and causing weight loss or surface erosion over a few months[54][58]. Fusarium species isolated from soil have also degraded PE thin films; one report documented Fusarium solani colonizing LDPE mulch film and inducing ~5–10% weight loss after 8 weeks, accompanied by visible cracks on the film surface (indicative of polymer chain scission)[59][55]. Mixed fungal communities or consortia of multiple fungi have achieved higher degradation than single strains[60][61]. D’Souza et al. (2021) showed that a consortium of three Aspergillus spp. could synergistically degrade LDPE with greater efficacy than any single fungus alone[62] – presumably different enzymes from each fungus complement each other.

While fungi clearly can break down polyethylene to some extent, their activities are often quantified in indirect ways (e.g. decrease in tensile strength, production of CO₂ in a respirometry test, or FTIR spectral changes) because complete mineralization is rarely achieved in lab timescales. One recent study focusing on Cladosporium fungi reported up to ~20% reduction in molecular weight of an LDPE sample after several months, along with secretion of cutinase-like enzymes[58][63]. Another found that Meyerozyma yeast (isolated from waxworms, discussed below) combined with bacteria could metabolize some PE oligomers[64]. Despite modest results, these findings underscore that fungi are indispensable in any discussion of PE biodegradation. They not only directly attack plastics but can also partner with bacteria: fungal breakdown of the polymer can generate fragments that bacteria further consume, and fungal hyphae can carry bacteria into otherwise inaccessible plastic interiors[65]. This brings us to the concept of mixed communities and symbioses.

### Insect Gut Microbiomes and Other Symbioses

A striking discovery in recent years is that certain insect larvae can ingest and “digest” plastics, seemingly with the aid of their gut microbes. The poster-child example is the waxworm – the caterpillar of the wax moth (Galleria mellonella). In 2017, Bombelli et al. reported that waxworm larvae chewed holes through polyethylene plastic bags and that some chemical breakdown occurred, with claims of ethylene glycol detected as a byproduct[66][67]. This report caused a media sensation as it suggested a biological solution to the plastic waste problem. Subsequent research showed that the waxworm’s ability likely stems from its natural diet of beeswax (a complex mixture of long-chain alkanes and lipids somewhat analogous to polyethylene) – the larvae and their gut bacteria have evolved alkane-degrading capabilities that are cross-acting on PE[68][69]. Specifically, two strains identified from waxworm guts, Enterobacter asburiae and Bacillus sp., were found to colonize and depolymerize polyethylene films in laboratory tests[70]. Yang et al. (2014) isolated an Enterobacter sp. D1 from waxworm intestines that showed clear biofilm formation and ~10% weight loss on a PE film in one month, as noted earlier[38][39]. This bacterium, along with others from the waxworm gut consortium, is thought to be responsible for breaking PE into shorter compounds that the larvae can then metabolize or excrete.

The waxworm findings, however, have not been without controversy. Did the caterpillars truly biodegrade PE, or just masticate it into tiny pieces? A follow-up study by Weber et al. (2017) questioned the original evidence for ethylene glycol production[67][71]. Their re-examination suggested that the reported chemical signatures could be explained by residual caterpillar proteins and lipids on the plastic rather than true oxidative breakdown products[72]. They argued that rigorous controls were lacking and that mechanical shredding might have been the primary effect. Thus, the extent of actual enzymatic depolymerization in waxworms remained uncertain[73]. This debate highlighted the need for careful controls (e.g. using frozen/crushed insect guts vs. live chewing, and spectroscopic confirmation of breakdown products) when assessing insect-driven biodegradation.

Since then, research has continued and expanded to other “plastivorous” insects. In 2020–2022, studies on mealworms (Tenebrio molitor, which eat polystyrene) and waxworms consistently found distinct shifts in the gut microbial community when larvae are fed plastics vs. normal diet[74][70]. For waxworms on a PE diet, next-generation sequencing revealed enrichment of certain bacteria (notably Pseudomonas and Serratia species) in the gut[75][76]. Serratia marcescens was isolated from waxworm guts and shown to degrade PE in vitro, especially when co-cultured with a waxworm-derived fungus (Meyerozyma guilliermondii yeast)[64]. These two organisms together could slowly depolymerize PE, each contributing different enzymes (bacterial oxidases and fungal esterases)[64]. Another study found that feeding waxworms on PE or polystyrene for 7 days led to an increase in gut Pseudomonas populations, though the overall degradation was hard to quantify over such short time[76][77].

Most recently, Cassone and colleagues (2023–2025) examined waxworms more deeply. They confirmed that waxworms can indeed metabolize PE into energy storage molecules (lipids) in their bodies within a few days – effectively converting plastic carbon into insect fat[78][79]. Remarkably, about 2,000 waxworms were reported to completely chew up a standard plastic bag in ~24 hours[80]. However, they also found a twist: on a diet of only plastic, the waxworms quickly became malnourished and died, indicating that plastic alone is not a nutritionally sufficient or balanced food[79]. Co-feeding the worms with sugar or other nutrients is necessary to keep them alive while they consume plastic[81][82]. This underscores that the insect-microbe system can break down PE, but it is an inefficient process biologically – likely a form of co-metabolism rather than a preferred pathway. Still, the work shows the potential of leveraging insect–microbe symbioses: either by mass-rearing such insects with supplemental feed to treat plastic waste, or by isolating and engineering the enzymes from their saliva or gut microbes for industrial use[83]. In fact, a very recent report announced the identification of several novel enzymes in waxworm saliva that can oxidize PE at room temperature[84], hinting that some part of the degradation may start even before ingestion (through saliva contact).

Beyond insects, other symbiotic systems have been noted. For example, some marine invertebrates harbor microbes that may degrade plastics; one study suggested certain worms and amphipods ingesting microplastics could have gut microbes aiding breakdown (though evidence is scant compared to insects). Another example is ruminants: a 2021 study found that cow rumen fluid (loaded with microbes used to breaking down plant waxes) could also slowly decompose polyethylene film, presumably by similar alkane-degrading bacteria present in the rumen[85]. These findings collectively emphasize a general principle: natural ecosystems and host animals that encounter recalcitrant polymers (waxes, lignin, etc.) have evolved microbes and enzymes that by chance or adaptation can act on synthetic polymers like PE. Mining these systems for potent microbes or enzymes is a promising avenue.

## Enzymatic and Metabolic Pathways for PE Degradation

A critical bottleneck in polyethylene biodegradation is the lack of specialized depolymerase enzymes that cleave the polymer backbone. Unlike PET or polyurethane, where specific hydrolases (PETase, urethanases, etc.) have been identified[86][87], PE degradation seems to rely on a suite of more generalist oxidative enzymes and pathways. Research to date indicates that PE-degrading microbes use enzymes from their hydrocarbon degradation arsenal to attack polyethylene. Key enzyme classes implicated include:

- Oxidative enzymes (laccases and peroxidases): These enzymes, common in fungi and some bacteria, generate reactive radical species. Laccases (multi-copper oxidases) can remove electrons from polymer chains, leading to random scission of C–C bonds. Peroxidases (like manganese peroxidase, MnP, and lignin peroxidase, LiP) use peroxide to oxidize substrates and have been shown to oxidize polyethylene’s methylene groups to carbonyls[13][88]. For example, the actinomycete Rhodococcus ruber produced a laccase that significantly enhanced PE film degradation in the presence of Cu(II)[46]. Fungi such as Alternaria upregulate multiple peroxidases when grown on PE, indicating these enzymes are part of the attack strategy[88][89].

- Alkane hydroxylases (monooxygenases): Many PE-degrading bacteria are known petroleum hydrocarbon degraders. They often possess alkane monooxygenase systems (e.g. the AlkB family and cytochrome P450 enzymes) which catalyze the addition of an oxygen atom to aliphatic hydrocarbons[28][29]. In the context of PE, these enzymes likely perform terminal or sub-terminal oxidation of the polyethylene chain ends[90]. When PE chains (or long-chain alkanes derived from PE) are oxidized at the end, the result is a primary alcohol, which can be further oxidized to an aldehyde and then to a fatty acid. Pseudomonas aeruginosa E7, for instance, was shown to have two AlkB monooxygenases; one of them (AlkB2) was significantly upregulated in presence of low-molecular-weight PE and could oxidize PE wax (C_44_ polymer)[28][91]. Likewise, Rhodococcus and Bacillus strains often carry P450 enzymes that can initiate oxidation on solid hydrocarbons like paraffin and are thought to do the same on polyethylene surfaces[29][92].

- Accessory catabolic enzymes: Once initial oxidation introduces functional groups, a cascade of other enzymes take over. These include alcohol dehydrogenases (ADH) and aldehyde dehydrogenases (ALDH) to convert alcohols to aldehydes to acids[93]. Baeyer-Villiger monooxygenases (BVMO) can cleave ketones or cyclic structures to esters, which might play a role if ketonic groups form on oxidized PE[93]. Esterases and lipases might help if any oxidative cross-linking creates ester-like bonds or if small esterified additives in plastic are present[94][95]. Essentially, after the initial oxidation by monooxygenases, the breakdown of resulting metabolites likely follows the well-trodden pathways of fatty acid β-oxidation (for linear alkane oxidation products)[31]. The end result of these pathways are central metabolites (acetyl-CoA, succinate, etc.) feeding into the TCA cycle.

Figure 2. Proposed pathway for microbial oxidation of polyethylene. Long-chain PE molecules (solid line) undergo initial oxidation at chain ends (or at random points after some abiotic pre-oxidation) via alkane monooxygenases (AlkB, P450, etc.), yielding primary alcohols and then aldehydes. These are further oxidized by alcohol and aldehyde dehydrogenases to fatty acids. Depending on chain length, intermediate carboxylic acids can enter β-oxidation to yield acetyl-CoA for microbial metabolism. Some sub-terminal oxidation may produce secondary alcohols/ketones that undergo Baeyer–Villiger oxidation (BVMO) to esters and then hydrolysis. Laccases and peroxidases (mostly from fungi/actinomycetes) can act at any stage to introduce radicals (●) and break C–C bonds randomly, complementing the terminal oxidation pathway[28][29]. (Simplified from references[28][29].)

Notably absent so far is a “polyethylene hydrolase” – an enzyme analogous to cutinases or PETases that could directly depolymerize PE. This likely reflects the fundamental chemistry of PE; hydrolytic cleavage is ineffective on a purely hydrocarbon chain. Evolutionarily, there has been little pressure to evolve enzymes for breaking synthetic polyolefins which have only existed for ~80 years. Instead, microbes repurpose their existing enzymes for analogous natural substrates (waxes, alkanes) to slowly attack PE. A major goal for the field is to identify or engineer a catalyst (enzyme or chemical) that can cleave the C–C bond efficiently under mild conditions. Some researchers are exploring engineered enzymes or combinations thereof: for example, using a laccase to introduce oxidation and a monooxygenase to further cleave, etc., effectively mimicking an “enzyme cocktail” akin to how multiple cellulases synergize in cellulose degradation[86][87].

Laboratory studies using omics techniques have been illuminating in this regard. Transcriptomic analyses of bacteria grown on PE have revealed upregulation of genes in alkane degradation, fatty acid metabolism, and stress response[96][31]. For instance, Rhodococcus ruber cultured with polyethylene showed 158 genes upregulated, mainly related to alkane catabolism and β-oxidation, consistent with the pathway in Figure 2[96]. Metagenomic sequencing of a community enriched on PE found numerous hits for alkB-like genes and oxidative stress enzymes, suggesting these functions are crucial for communal PE degradation[32][97].

In summary, microbes employ a multi-step enzymatic attack on polyethylene: initial oxidation (slow) followed by routine catabolism of the oxidation products (faster). The overall rate is constrained by the initial breaking of the polymer chains. To accelerate PE biodegradation, research is focusing on boosting these initial oxidative steps – through enzyme discovery, protein engineering, or coupling with abiotic pretreatments (e.g. UV, chemical oxidation to “pre-weather” the plastic).

## Microbial Consortia and Community Synergy in PE Degradation

Given the complexity of attacking PE, no single microbe has all the necessary tools to efficiently degrade it alone. This recognition has driven growing interest in microbial consortia – mixtures of microorganisms that work in concert to break down polyethylene. In natural environments, plastics are never encountered by isolated microbes; they are immediately colonized by diverse communities (the “plastisphere”)[98][99]. These communities often show a division of labor: some members initiate polymer oxidation, others digest the byproducts, and some produce biofilm matrices or surfactants that facilitate the process[100][101]. Synthetic consortia (intentionally combined strains) attempt to replicate or enhance this synergy.

Advantages of consortia: Compared to single strains, mixed communities are often more efficient, robust, and resilient in degrading plastics[102][44]. Advantages include: (i) Enzymatic complementarity – different species contribute different enzymes (e.g. a fungus produces laccase to break polymer chains, a bacterium beta-oxidizes the fragments[65]). (ii) Complete metabolism – one microbe’s metabolite is another’s food, so intermediate products (e.g. long-chain acids) get fully mineralized rather than accumulating. (iii) Biofilm formation and stability – multispecies biofilms can be more stable and effective; some bacteria excel at forming biofilms while others provide the degradative power within that biofilm[103][104]. (iv) Environmental tolerance – a consortium can survive a broader range of conditions; for example, some members might fix nitrogen or supply vitamins that others need, enabling the community to thrive on a nutrient-poor plastic surface.

Evidence of consortial superiority is found in numerous studies. As shown in Table 1, a two-member bacterial consortium from a landfill (Bacillus + Paenibacillus) degraded ~14.7% of PE in 60 days, outperforming what either strain likely could do alone[44][41]. Skariyachan et al. combined multiple plastic-degrading bacteria from soil and cow dung; their consortium degraded PE films significantly more (by weight and by formation of carbonyl groups) than any isolate alone[44][105]. Interestingly, they also observed that PE films (thin sheets) lost more weight than PE pellets under the same treatment[105]. This highlights a practical point: increased surface area and biofilm-friendly geometry (a thin film) enhance degradation – a consortium can only act on the surface accessible to it[106]. Thus, physical form factors (like using thin films, powdering the plastic, or using microplastics) can influence outcomes.

Mixed consortia can be cross-domain as well. Fungal–bacterial consortia have shown noteworthy results. Esmaeili et al. (2013) inoculated soil with both an Aspergillus fungus and a Lysinibacillus (a bacterium) and found that LDPE films buried in this soil degraded more than in soil with either microbe alone[65]. The hypothesis is that the fungus’s hyphae helped transport and attach bacteria deeper into the plastic, and possibly partially digested the plastic to make it more accessible[65]. Such cross-kingdom facilitation is well known in wood decay (fungi soften wood, bacteria fully mineralize it), and a similar cooperation seems to benefit plastic degradation[107]. A recent study by Massot et al. (2022) systematically investigated bacteria–fungi interactions on plastics and found numerous positive interactions, for example, certain Aspergillus species significantly enhanced the growth and activity of Pseudomonas on PE by providing anchoring hyphae and extra enzymes[108][109].

Another intriguing consortium is the natural one within insect guts discussed earlier. The waxworm gut community is a prime example of a multi-kingdom consortium: it includes bacteria (e.g. Enterobacter, Serratia), possibly yeasts (Meyerozyma), and the host’s own enzymes (salivary enzymes that soften plastic)[64][79]. Together, they achieve a feat (complete breakdown of a PE bag in days) that no isolated microbe has matched. The trade-off is the host’s health – highlighting that this consortium is not optimized for plastic degradation per se, but it nevertheless shows the power of a complex, co-evolved system to tackle PE. Researchers are looking at ways to externalize such consortia, for instance by culturing the key gut microbes together in bioreactors to digest PE without the insect, or by transferring the pathway into a more industrially hardy consortium.

### The Plastisphere: Natural Communities on Plastics

Whenever plastic debris enters the environment, microorganisms begin colonizing its surface, forming what has been termed the “plastisphere” – a distinct ecological niche on the plastic[110]. Studies have found that the community composition on plastic surfaces often differs from the surrounding water or soil microbiota, suggesting selection for organisms that can utilize the plastic or the nutrients accumulating on it[111]. The plastisphere is composed of various trophic types: heterotrophs that may degrade the plastic or biofilm organic matter, autotrophs (phototrophs) that find a surface to grow on, and even predators (protists) grazing on the bacteria[112]. Over time, a mature biofilm develops which can change the properties of the plastic – for instance, it can reduce hydrophobicity and introduce pits and grooves[113]. These biofilm-induced changes often precede any significant biodegradation and might actually facilitate subsequent polymer breakdown by making the surface more amenable to enzyme penetration[113].

Environmental studies have catalogued plastisphere communities in various settings: marine (ocean, coastal)[114], freshwater (rivers, lakes)[115], and terrestrial (agricultural soils, landfill sites)[111]. Some common trends emerge. In marine plastisphere samples, bacteria from genera like Alcanivorax, Marinobacter, Vibrio, Hyphomonas are frequently found attached to PE or PP fragments[116]. Notably, Alcanivorax is a known alkane degrader, suggesting it might be feeding on polymer leachates or initiating oxidation of the polymer[116]. Kirstein et al. (2019) found that Alcanivorax borkumensis proliferated on PE pieces incubated in seawater and hypothesized it as a “key player” in marine PE degradation[116]. In soil plastisphere communities, one often finds actinobacteria (as in landfills, where Rhodococcus and Nocardia are reported on plastic surfaces[117]) and diverse Bacillales. Zettler et al. (2013), who coined the term plastisphere, observed clear evidence of biodegradation (etch marks and surface erosion) on ocean plastic debris and correlated that with the presence of potential degraders in the biofilm[99][110]. This naturally leads to the idea that the plastisphere can be “mined” for effective degraders.

Researchers are now using metagenomics and metatranscriptomics to delve into plastisphere communities. By sequencing DNA/RNA extracted from plastic biofilms, they identify enzymes and pathways that are enriched. For example, Pinto et al. (2022) analyzed biofilm on PE after a 2-year seawater incubation and found that genes for alkane hydroxylases (alkB) became more abundant over time, indicating adaptive enrichment of alkane-degrading microbes on the plastic[32][118]. Similarly, Wang et al. (2022) compared microbial communities on plastic versus surrounding soil and found unique taxa and higher expression of oxidative stress and hydrocarbon degradation genes in the plastisphere. Such studies reinforce that prolonged exposure of a community to PE can select for a functional consortium capable of partial biodegradation[119][120]. In other words, nature is slowly evolving its own “solutions” in the form of specialized communities.

### Constructing Synthetic Consortia

Inspired by the plastisphere, scientists are attempting to construct optimized consortia in the lab that can outperform natural communities. Two general strategies exist[121]:

- “Top-down” enrichment: Start with a mixed environmental sample (soil, compost, marine biofilm) and culture it with PE as the primary carbon source, under controlled conditions. Through serial transfers and adjusting conditions, the community shifts and ideally becomes more efficient at degrading PE[122][102]. This approach leverages natural selection to yield a functional consortium. Key degraders from the enrichment can later be identified via sequencing (16S/ITS or metagenomics). For instance, Joshi et al. (2022) used this method with coastal seawater samples – after successive enrichment on LDPE, they isolated a marine consortium that achieved ~47% weight loss of LDPE in 120 days[42]. The enriched community could then be partially reconstructed with a few culturable strains that were dominant (in their case, Oceanobacillus, Bacillus, and Brevibacterium were among those reported, though the full detail is in their publication). Top-down approaches have the advantage of starting with robustness and complexity, but the end consortia can be hard to reproduce exactly and may still contain “passenger” microbes that don’t contribute to degradation.

- “Bottom-up” assembly: Select a set of known degraders (isolated pure cultures, possibly from different sources) and combine them in specific ratios to form a consortium[123]. The idea is to cover all necessary functional roles by design – e.g., include a fast-growing biofilm former, a strong oxidative degrader, a specialist that eats byproducts, etc. Bottom-up design allows more control and reproducibility. However, it faces challenges too: the strains might not cooperate naturally and could even inhibit each other (competition, incompatible growth conditions)[124]. Trial-and-error is often needed to find combinations that are synergistic rather than antagonistic[125]. An example is the artificial consortium by Putcha & Kitagawa (2024), who chose several bacteria each expressing key enzymes (laccase, alkane monooxygenase, lipase, etc.) and co-cultured them on PE pellets[94][95]. Over ~200 days, their consortium formed a multilayered biofilm on the plastic and caused obvious pitting and erosion of the PE surface[21]. Notably, one member (Rhodococcus erythropolis) became dominant in the biofilm – a reminder that even in designed consortia, a succession can occur where the most effective degrader takes over[126][127]. The authors reported that the consortium degraded a significant amount of the PE (though exact mineralization data were not given, surface analysis confirmed polymer chain oxidation). This kind of rational assembly combined with monitoring via sequencing is a promising route to engineer robust PE-degrading consortia.

Increasingly, researchers see that top-down and bottom-up are complementary rather than opposing. A proposed strategy is to enrich a natural community (top-down) to get a pool of candidates, use omics to identify key players and genes, then isolate or engineer a refined set of strains (bottom-up) that together recreate the degradation network[128][129]. This hybrid approach can compensate for limitations of each: the top-down step discovers novel unculturable helpers and real-world interactions, while the bottom-up step simplifies the community for easier control and optimization[128]. Modern multi-omics (metagenomics, metatranscriptomics, metaproteomics) provide a treasure trove of data from enrichment cultures, guiding which species and pathways to focus on[130][32]. For example, Gilmore et al. (2019) combined selective enrichment with deep sequencing to identify a minimal community that could degrade a model hydrocarbon polymer; similar efforts are now underway for polyethylene[131][132].

One must also consider population dynamics in consortia. Over time, species composition can shift (as seen in the Putcha consortium where Rhodococcus dominated)[126]. Ensuring stability and preventing collapse of function (say, if one key strain is outcompeted and the degradation stalls) is a challenge. Techniques like controlled inoculum ratios, periodic reinforcement of certain members, or even encapsulating cells to prevent direct competition are being explored. Spatial organization might matter too: biofilm consortia can be spatially structured such that outer layers perform initial oxidation and inner layers consume resulting molecules, etc. Engineering such spatial structure (e.g. in a bioreactor with support matrices) could improve efficiency.

In summary, microbial communities – whether naturally evolved on plastics or artificially constructed – clearly outperform most single microbes in degrading PE. The best results so far (approaching 50% conversion of PE in a few months[42]) have come from consortia. The field is moving toward rationally designing such consortia, informed by natural plastispheres and powered by genomics. The ultimate goal would be a stable, well-characterized community (or a synthetic microbe with a “consortium” of engineered pathways) that can be deployed in an environmental or industrial setting to biodegrade polyethylene reliably.

## Current Controversies and Knowledge Gaps

Despite significant progress in identifying PE-degrading organisms and consortia, several controversies and open questions remain:

- Extent of True Mineralization vs. Partial Degradation: One major debate is how far the reported “degradation” actually goes. Many studies measure weight loss, formation of carbonyl groups (by FTIR), reduction in polymer molecular weight, or changes in mechanical properties as evidence of degradation. But these do not necessarily equate to mineralization. Skeptics point out that weight loss could mean fragmentation into micro- and nano-plastics that escape detection (e.g. tiny particles slough off the film and are lost during washing)[85][133]. Similarly, observing carbonyls indicates oxidation of the polymer, but the chain fragments might still persist in the environment as waxy residues. Only a few studies have rigorously demonstrated conversion of PE carbon to CO₂ (e.g. by incubating with ^13C-labeled PE and capturing ^13CO₂). The waxworm saga exemplified this controversy: the initial claim of ethylene glycol production was challenged as possibly misidentified, leaving doubts about how far the polymer was broken down[133][71]. Resolving this requires standardized biodegradation tests, such as ASTM or ISO protocols (e.g. ASTM D5511 anaerobic digestion test, or CO₂ evolution in respirometric tests) to quantify mineralization. So far, complete mineralization of PE in laboratory conditions is seldom reported. Most consortia still leave some portion of the plastic unassimilated (which might be fine if the goal is just to weaken it for further processing, but not if we want full elimination).

- Environmental Relevance: Another point of debate is whether the lab demonstrations of PE biodegradation translate to meaningful rates in the environment. Critics note that many studies use pretreated plastics – e.g. thermo-oxidized PE (which has surface cracks and functional groups) or very thin films or powders – to get measurable degradation in a feasible time[134]. In the environment, plastics might not have those pretreatments (though weathering does act over longer times). Additionally, lab strains are often tested with additional co-substrates (like yeast extract, dextrose, or emulsifiers) to support microbial growth[135][134]. In a nutrient-poor environment (open ocean or subsoil), plastic might not support enough microbial activity to matter. Some argue that plastic biodegradation in nature is currently so slow as to be negligible – essentially, that any observed degradation is on timescales (many decades) that are not useful for remediation purposes[4]. On the other hand, optimists point to evidence of adaptation: for example, discovery of pits on decades-old buried plastic suggesting that microbes have been eating away at it slowly[112][114], or the rise in specific enzyme genes in polluted habitats (a sign of evolutionary response to plastic as a substrate). This remains an active area of research, requiring long-term field studies (e.g. burying labeled plastic in situ and monitoring over years) to gauge real-world biodegradation rates[5].

- Identity of Key Enzymes: As discussed, no dedicated “PEase” enzyme has been isolated. The field still lacks definitive proof of which enzyme (or enzyme system) is most responsible for cleaving the PE backbone. Is it laccase-generated radicals? Or alkane monooxygenase repeatedly truncating chain ends? Or perhaps unknown enzymes like rubber oxygenases (which cleave polyisoprene) that might act on PE? The uncertainty persists. Efforts to extract and characterize enzymes directly from cultures grown on PE have met with difficulty, partly because activities are low and product analysis is tricky. Some reports of enzyme activity do exist – for example, Jeon et al. (2016) partially purified an alkane monooxygenase from Pseudomonas that could degrade a synthetic analog of PE (alkane mixture)[28][91]. And the waxworm saliva enzymes reported in 2022 (tentatively named “demetra” enzymes) are a new candidate class, though their mechanisms are still being unraveled[84]. The controversy here is whether a breakthrough enzyme will be found naturally, or if we need to create one via protein engineering (for instance, by mutating enzymes that act on similar substrates to accept solid PE). No consensus exists yet, making this a ripe area for discovery.

- Safety and Ecological Impact: As we engineer microbes or consortia to degrade plastics, a practical consideration (sometimes debated) is safety. Releasing engineered microbes into the environment is fraught with regulatory and ecological concerns. Some have argued for containment – using these microbes in controlled facilities (e.g. bioreactors or composting systems) rather than in open nature. Others note that if a microbe truly can degrade PE quickly, introducing it in landfills might help mitigation. However, careful risk assessment is needed: a microbe that breaks PE might also attack other hydrocarbons (maybe even structural materials or living tissues, although that seems unlikely for a specialized degrader). There is also the issue of microplastic byproducts – incomplete degradation could transiently increase the load of microplastics in soil or water, possibly having toxic effects on organisms before full mineralization. While not a “controversy” in the scientific sense, these considerations drive some debate about how to deploy biodegradation technologies responsibly.

- Reproducibility of Results: As with any emerging field, reproducibility has been a challenge. Different labs sometimes report different extents of degradation for similar organisms. Factors like the type of PE (LDPE vs HDPE, additives present, surface area available), the method of sterilizing the plastic (which can alter its chemistry), and measuring techniques can all influence outcomes. For example, one lab might use tensile strength loss as a proxy for degradation, whereas another uses CO₂ evolution – these are not directly comparable. The community is moving toward standardized assay conditions, but until those are widely adopted, one must interpret claims of “degradation” case-by-case. There have been instances where initial optimistic reports (like the 2017 waxworm study) were tempered by later investigations[73], which is a normal part of science self-correcting but also highlights the need for careful validation.

Addressing these controversies requires interdisciplinary collaboration – microbiologists, polymer chemists, environmental scientists, and engineers working together. Advances in analytical chemistry (to track minute degradation products), in situ imaging, and high-throughput sequencing will help answer many of these questions. Meanwhile, funding agencies and journals are increasingly emphasizing that new claims of plastic biodegradation should include rigorous evidence (mineralization data, enzyme identification, etc.) rather than just surface analyses. This scrutiny will ultimately strengthen the field and separate the truly promising leads from the artifacts.

## Future Perspectives (Next 5–10 Years)

The coming decade is poised to be an exciting period for research into microbial plastic degradation. Building on the foundational knowledge we now have, researchers are charting several promising directions:

1. Omics-Driven Discovery of Enzymes and Pathways: High-throughput sequencing and -omics analyses will continue to play a central role. By analyzing genomes and metagenomes of plastic-associated microbes, scientists aim to identify novel enzymes that nature may have already evolved for tackling polyethylene. It is conceivable that within diverse plastisphere communities or extremophiles, there exist undiscovered oxygenases or radical-generating enzymes with higher activity on PE than known ones. Metaproteomics (identifying proteins expressed in a community when fed PE) could directly pinpoint which enzymes are active during degradation. Any enzyme candidates can then be produced recombinantly and tested in isolation – a faster route than trying to culture the original organism. Machine learning and protein engineering might also contribute: for example, by analyzing structures of alkane monooxygenases or laccases, researchers may design mutants with greater ability to bind and attack solid polyethylene. In the PET field, a few rounds of protein engineering dramatically improved PETase’s efficiency[86]; a similar effort could emerge for polyethylene-degrading enzymes, once clear targets are identified. The ultimate dream would be an enzyme or enzyme cocktail that one could sprinkle on shredded PE to depolymerize it in days – while that remains distant, the rapid progress with other plastic-degrading enzymes suggests we shouldn’t rule it out in the long run.

2. Synthetic Biology and Metabolic Engineering: Hand-in-hand with enzyme discovery, metabolic engineering will come to the forefront. One could envision engineering a microbial strain (or a synthetic co-culture) with a tailor-made pathway for PE degradation. For example, a bacterium could be engineered to overexpress a laccase on its outer surface (for initial polymer oxidation) along with multiple alkane degradation genes to catabolize the breakdown products. There has been proof-of-concept where E. coli was engineered with alkane-degrading pathways to tackle long-chain alkanes; extending this to solid PE by adding biofilm-forming capability and perhaps a few surface-active proteins is a plausible next step. CRISPR-based genome editing makes it easier to modify environmental isolates that already have some PE-degrading ability – boosting their key genes, knocking out competing pathways to channel more energy into degradation, etc. The future might see a consortium of engineered specialists, each performing a step in concert. For instance, a recombinant fungus aggressively oxidizes the polymer (but maybe can’t assimilate well), partnered with a recombinant bacterium that rapidly consumes the oxidized oligomers. This kind of division-of-labor engineering could substantially improve overall rates, as each organism can be optimized for its role without the need to do everything. Some researchers are already exploring genetic circuit designs where two bacteria communicate – one produces a signal when it has generated enough product, triggering the other to start consuming it, achieving a coordinated degradation process.

3. Combining Biodegradation with Upcycling: A forward-looking trend is valorization of plastic waste – not just breaking it down to CO₂ (which is environmentally helpful but yields no economic value), but converting it into useful products[136][137]. The concept of bio-upcycling is gaining traction[138][139]. Instead of mineralizing PE completely, the aim is to stop at intermediary chemicals that can serve as fuels or feedstocks. For example, if a consortium can efficiently convert PE into long-chain fatty acids, those could be harvested and turned into bio-diesel or lubricants. Or microbes could transform PE breakdown products into biopolymers or biosurfactants. Integration of chemical and biological processes is likely key here[140][137]. One scenario: use a mild thermo-oxidative pretreatment to turn PE into a mixture of oxygenated waxes, then feed that to a microbial community engineered to produce a specific product (say, medium-chain-length polyhydroxyalkanoates – biodegradable plastics – from those waxes). Another scenario: a two-step reactor where step 1 is a bioreactor of degrading microbes converting PE to short-chain acids, and step 2 is a fermentation where another microbe (like an engineered yeast or E. coli) consumes those acids to produce a commodity chemical (ethanol, acetone, bioplastics, etc.)[139][141]. Such integrated approaches maximize the value extracted from plastic waste and could make biodegradation more economically attractive. Recent reviews highlight that very few studies have addressed upcycling of polyolefins biologically[141] – this is expected to change with more interdisciplinary collaboration between microbiologists and chemical engineers. Over the next 5–10 years, we may see pilot processes that turn dirty PE waste into, for example, methane or other fuels via microbial consortia (some startups are already investigating landfill gas from plastics).

4. Enhanced Bioprocessing Strategies: On the applied side, expect advances in bioprocess engineering for plastic waste. This includes developing specialized reactors (maybe designs that increase surface contact between microbes and shredded plastic, like rotating drum bioreactors or slurry reactors with carriers that hold plastic particles in suspension). Bioaugmentation in waste facilities could become common – e.g. adding a custom consortium to a compost or landfill to speed up plastic decay. Another practical direction is pretreatment optimization: finding the sweet spot of inexpensive pretreatment (like a brief UV exposure or oxidative treatment) that makes plastic sufficiently biodegradable without too much cost. One interesting idea is using solar energy to assist – for instance, having a transparent reactor where sunlight both warms the culture and photo-oxidizes the plastic while microbes do their work. Additionally, surfactants or co-solvents might be employed to better disperse hydrophobic polymers into the aqueous phase for microbes to access (research has shown adding mineral oil or surfactants can improve PE degradation by increasing surface wettability[134]). In sum, engineering the environment around the microbes will be as important as engineering the microbes themselves.

5. Exploration of Terrestrial Plastisphere & Extremophiles: So far, more attention has been on marine plastics and a few terrestrial sites. In the next few years, expect intensive exploration of less-studied niches: landfill plastispheres, desert or Arctic plastispheres, and sites with long-term plastic burial. These could yield extremophilic microbes that work in conditions unsuited for usual life – e.g. a bacterium that degrades PE at 70 °C in a hot landfill (heat often speeds reactions), or a fungus that works at pH > 10 in alkaline soil. Atanasova et al. (2021) have already discussed extremophiles for plastic degradation[142]. The rationale is that extreme conditions could “activate” polyethylene and these microbes might have unusual enzymes to exploit that. Also, investigating terrestrial plastisphere diversity is crucial, as emphasized in a recent perspective calling for multi-omics of plastic-colonized soils and landfill sites[143][144]. The coming years will likely see global initiatives to sample and catalog microbes from long-standing plastic waste sites (akin to global metagenome surveys, but targeting plastic-rich environments). These efforts will feed back into points 1 and 2 (enzyme and strain discovery).

6. Lifecycle and Ecosystem Impact Studies: As biodegradation solutions become viable, researchers will concurrently study the ecosystem impacts and lifecycle implications. For example, what happens to the rest of the microbial community when you introduce a plastic-degrading consortium into a soil? Will it disturb the native ecology or perhaps beneficially reduce microplastics that would otherwise harm organisms? Also, a full life-cycle assessment (LCA) will be needed for any biodegradation-based recycling process: we must ensure that the process doesn’t emit more greenhouse gases or energy usage than it saves. If using insects, one might ask: can the insects (or their frass) be safely used as animal feed after they’ve eaten plastic? (Encouragingly, waxworms that convert plastic to fat might themselves be used as fish feed[22][83], suggesting a potential circular bioeconomy benefit). These interdisciplinary questions will become more prominent as lab successes move toward pilot scale demonstration.

Given the rapid growth of interest in environmental plastics, funding and innovation in this area are accelerating. We foresee that in 5–10 years, the field will transition from exploratory lab studies to translational research – developing actual biotechnologies to manage polyethylene waste. This could take the form of “plastic composting” facilities inoculated with special microbes, or small-scale devices for communities to degrade plastics sustainably. While it’s unlikely that microbes alone will solve the entire PE waste problem (the volumes are immense), they can become a key part of a multi-pronged solution, complementing improved recycling, chemical upcycling, and reduced plastic usage. In particular, microbes might be best suited to deal with microplastic pollution that is otherwise impossible to clean up – imagine microbe-based water treatment units that capture and digest microplastics in wastewater streams, preventing them from reaching oceans.

The holy grail remains a scenario where polyethylene and other recalcitrant plastics are no longer persistent pollutants but are simply another source of carbon that can be cycled by the biosphere. Achieving this will require bridging the gap between laboratory discoveries and field application, a challenge that the next decade of research is well-positioned to tackle with the tools of modern biotechnology and environmental science.

## Conclusion

Polyethylene’s durability, once celebrated as a material virtue, has become a liability in the era of plastic pollution. Tackling this inert polymer through microbial action is an ambitious goal – one that has driven the assembly of a growing toolkit of specialized organisms, enzymes, and engineered consortia. As we have reviewed, nature provides intriguing hints of solutions: bacteria that nibble at polyethylene in landfills and oceans, fungi that soften and oxidize it, and even humble insect larvae whose gut flora can chew plastic into metabolites. Each of these by itself falls short of a complete answer, but together they illuminate the path forward.

In the current state of knowledge, we have identified many of the players (microbes) and parts (enzymes) involved in PE biodegradation, yet we have not fully learned how to make them work in concert at a scale and efficiency that matches the enormity of the plastic waste problem. The lack of a definitive PE-destroying enzyme and the slow rates of degradation are key bottlenecks. However, the field is advancing rapidly on multiple fronts – from discovering communities in the plastisphere that naturally attack plastics, to designing synthetic consortia with ever-improving performance, to integrating those biological methods with chemical processes for better results.

It is clear that no silver-bullet organism exists (at least not yet) for polyethylene, so the emphasis is rightly shifting toward synergistic approaches. By combining the top-down wisdom of natural ecosystems with bottom-up innovation in biotechnology, scientists are inching closer to overcoming polyethylene’s recalcitrance. The next decade will likely witness the first viable bioprocesses targeting polyolefins, perhaps starting with niche applications (like treatment of agricultural mulch film waste or recovery of fuels from plastic via microbial routes). Success in these early applications will build confidence to tackle larger streams of waste.

In conclusion, while polyethylene biodegradation by microbes is still in its infancy compared to the biodegradation of more labile plastics, the progress to date offers a strong proof-of-concept that microbial communities can, given the right conditions, assimilate what was once thought to be “undegradable.” The challenge now is to boost and harness this ability to a level where it becomes not just a laboratory curiosity but a practical tool for environmental remediation and resource recovery. The convergence of microbiology, systems biology, and process engineering in this field gives reason for optimism. Through continued interdisciplinary research, the seemingly impossible (microbes eating plastic) may become a tangible part of a sustainable future, transforming polyethylene from a pollutant back into the biological carbon cycle.

For ease of reference and further reading, a list of cited works is provided below. Interested readers are encouraged to consult these sources for more detailed data and experimental methodologies.

## References

- Frontiers in Microbiology: “Assembly strategies for polyethylene-degrading microbial consortia based on the combination of omics tools and the ‘Plastisphere’.” Front. Microbiol. 14:1181967 (2023). DOI: 10.3389/fmicb.2023.1181967 – A comprehensive review discussing stages of PE biodegradation, known microbes and enzymes, and proposing combining top-down and bottom-up approaches for consortium development[145][146].

- Science of the Total Environment: “Degradation of conventional plastic wastes in the environment: A review on current status of knowledge and future perspectives of disposal.” Sci. Total Environ. 771:144719 (2021). DOI: 10.1016/j.scitotenv.2020.144719 – Summarizes current knowledge on how traditional plastics (including PE) degrade in nature and the microorganisms involved[5][66].

- International Biodeterioration & Biodegradation: Santo et al., “The role of the copper-binding enzyme laccase in the biodegradation of polyethylene by the actinomycete Rhodococcus ruber.” Int. Biodeterior. Biodegradation 84, 204–210 (2013). DOI: 10.1016/j.ibiod.2012.03.001 – Demonstrated that laccase production by Rhodococcus significantly enhanced PE film degradation, especially with copper present[46][47].

- Journal of Hazardous Materials: Joshi et al., “Unraveling the plastic degradation potentials of the plastisphere-associated marine bacterial consortium as a key player for low-density polyethylene degradation.” J. Hazard. Mater. 425:128005 (2022). DOI: 10.1016/j.jhazmat.2021.128005 – Reported a marine bacterial consortium (enriched from coastal plastic debris) that achieved ~47% weight loss of LDPE in 4 months, highlighting the high potential of naturally adapted communities[42][43].

- Chemosphere: Park & Kim, “Biodegradation of micro-polyethylene particles by a consortium isolated from a landfill site.” Chemosphere 222, 527–533 (2019). DOI: 10.1016/j.chemosphere.2019.01.159 – Combined two bacterial strains (Bacillus and Paenibacillus) to degrade ~14.7% of micro-PE in 60 days, illustrating improved degradation via mixed culture[102][44].

- Int. J. Environ. Res. Public Health: Ren et al., “Biodegradation of polyethylene by Enterobacter sp. D1 from the gut of wax moth Galleria mellonella.” IJERPH 16(11):1941 (2019). DOI: 10.3390/ijerph16111941 – Isolated an Enterobacter strain from waxworm intestines that formed biofilms on PE film and caused ~10% weight loss in one month, providing evidence of insect gut microbes contributing to PE degradation[38][39].

- Frontiers in Microbiology: Ruiz Barrionuevo et al., “The bacterial and fungal gut microbiota of the greater wax moth (Galleria mellonella) consuming polyethylene and polystyrene.” Front. Microbiol. 13:918861 (2022). DOI: 10.3389/fmicb.2022.918861 – Characterized changes in waxworm gut communities when fed plastic, identifying enriched Pseudomonas and Serratia and suggesting a multi-kingdom (bacteria + fungi) contribution to plastic degradation[74][75].

- ScienceDaily News: “Scientists question study about plastic-eating caterpillars.” (Sep 15, 2017) – A press release summarizing Weber et al.’s critique of the 2017 waxworm study. It explains doubts about evidence of PE actually being chemically degraded to ethylene glycol, and shows that mechanical shredding and contamination could explain the original results[66][67].

- ScienceDaily News: “These ‘plastivore’ caterpillars can devour a plastic bag in just 24 hours.” (Aug 27, 2025) – Reports new research by Dr. Cassone’s team on waxworms, confirming that waxworms metabolize PE into body fat within days and can chew through a bag in 24h (with co-feeding), but highlighting the worms’ health issues on a plastic-only diet[78][81].

- Journal of Applied Microbiology: Cowan et al., “Fungal bioremediation of polyethylene: challenges and perspectives.” J. Appl. Microbiol. 132(1), 78–89 (2022). DOI: 10.1111/jam.15203 – A focused review on the role of fungi in PE degradation, discussing fungal attachment, enzyme secretion (laccases, peroxidases), and the potential of fungi to synergize with bacteria in plastic bioremediation[56][13].

- Heliyon: D’Souza et al., “Fungal biodegradation of low-density polyethylene using consortium of Aspergillus species under controlled conditions.” Heliyon 7(5):e07008 (2021). DOI: 10.1016/j.heliyon.2021.e07008 – Demonstrated that a mix of Aspergillus strains could cooperatively degrade LDPE more effectively than single strains, highlighting fungal-fungal synergy in plastic biodegradation (performance details in text)[62].

- International Journal of Molecular Sciences: Atanasova et al., “Plastic degradation by extremophilic bacteria.” IJMS 22(11):5610 (2021). DOI: 10.3390/ijms22115610 – Reviewed how extremophiles (thermophiles, halophiles, etc.) contribute to plastic degradation. Suggests that extremophilic enzymes might be harnessed for polyolefin breakdown under harsh conditions where polymers become more labile[142].

- Applied and Environmental Microbiology: Danso et al., “Plastics: environmental and biotechnological perspectives on microbial degradation.” Appl. Environ. Microbiol. 85(19):e01095-19 (2019). DOI: 10.1128/AEM.01095-19 – A broad review covering microbial degradation of various plastics, including discussion on polyolefins and known species as of 2019, and the environmental distribution of plastic-degrading microbes[1][147].

- Current Biology (Correspondence): Weber et al., “Polyethylene bio-degradation by caterpillars?* Curr. Biol. 27(15):R744–R745 (2017). DOI: 10.1016/j.cub.2017.07.004 – The technical comment questioning the Bombelli 2017 findings. Provides evidence that the supposed ethylene glycol signals were likely due to residual protein/lipid, not true PE degradation, casting doubt on the extent of waxworm-driven biodegradation[133][71].

- Science of the Total Environment: Delacuvellerie et al., “From rivers to marine environments: a continuously changing plastisphere assemblage.” Sci. Total Environ. 787:147610 (2021). DOI: 10.1016/j.scitotenv.2021.147610 – Studied plastisphere microbial community succession from freshwater to marine environments, noting how community composition and potential plastic-degrading functions shift along the continuum (context for understanding plastisphere dynamics).

- Frontiers in Microbiology: Lou et al., “Serratia and yeast from waxworms degrade polyethylene.” Front. Microbiol. (2022) 13:839527. DOI: 10.3389/fmicb.2022.839527 – Isolated Serratia marcescens and Meyerozyma guilliermondii from waxworm guts; these, in co-culture, showed the ability to degrade PE (via weight loss and SEM observation), representing a cross-kingdom microbial consortium from an insect gut[64].

- ACS Sustainable Chem. Eng.: Chamas et al., “Degradation rates of plastics in the environment.” ACS Sust. Chem. Eng. 8(9), 3494–3511 (2020). DOI: 10.1021/acssuschemeng.9b06635 – Provided a comprehensive analysis of estimated degradation rates for various plastics. Notably estimates PE environmental half-lives on the order of decades to centuries, highlighting its recalcitrance[4].

- Chemistry and Biology (Cell Press): Bombelli et al., “Polyethylene bio-degradation by caterpillars of the wax moth Galleria mellonella.” Curr. Biol. 27(8), R292–R293 (2017). DOI: 10.1016/j.cub.2017.02.060 – The original report that waxworm larvae can ingest and metabolize PE, which sparked interest in insect-based plastic degradation. They reported holes in PE films and tentatively identified ethylene glycol as a breakdown product (which was later disputed)[66][67].

- Frontiers in Marine Science: Basili et al., “Major role of surrounding environment in shaping biofilm community composition on marine plastic debris.” Front. Mar. Sci. 7:262 (2020). DOI: 10.3389/fmars.2020.00262 – Found that the local environment (seawater chemistry, etc.) heavily influences which microbes colonize marine plastics, implying that different sites yield different plastisphere consortia (useful for understanding variability in degradation results).

- Microbes and Environments: Putcha & Kitagawa, “Polyethylene biodegradation by an artificial consortium: Rhodococcus as a competitive plastisphere species.” Microbes Environ. 39(3):2024 (2024). DOI: 10.1264/jsme2.ME24031 – Developed a synthetic bacterial consortium for PE degradation. Over 200 days, their consortium (enriched in Rhodococcus) formed biofilms and caused clear PE surface erosion, highlighting the dominance of Rhodococcus in the plastisphere and the effectiveness of multi-strain design[94][21].

(The above references are numbered in order of appearance in the text. All referenced articles are from peer-reviewed journals or reputable sources, and the links (DOI or URL) are provided for accessing the full publications.)

Download Options: This review is available for download in multiple formats. For convenience, you may download it as a PDF version or a Microsoft Word document for offline reading and reference.

[1] [2] [3] [4] [5] [6] [7] [8] [9] [10] [11] [12] [13] [14] [15] [16] [17] [18] [19] [20] [23] [24] [25] [26] [27] [28] [29] [30] [31] [32] [33] [34] [35] [36] [37] [38] [40] [41] [42] [43] [44] [45] [46] [47] [50] [51] [52] [53] [54] [55] [56] [57] [62] [65] [86] [87] [88] [89] [90] [91] [92] [93] [96] [97] [98] [99] [100] [101] [102] [103] [104] [105] [106] [107] [108] [109] [110] [111] [112] [113] [114] [115] [116] [117] [118] [119] [120] [121] [122] [123] [124] [125] [128] [129] [130] [131] [132] [136] [137] [138] [139] [140] [141] [142] [143] [144] [145] [146] [147] Frontiers | Assembly strategies for polyethylene-degrading microbial consortia based on the combination of omics tools and the “Plastisphere”

https://www.frontiersin.org/journals/microbiology/articles/10.3389/fmicb.2023.1181967/full

[21] [94] [95] [126] [127] Polyethylene Biodegradation by an Artificial Bacterial Consortium: Rhodococcus as a Competitive Plastisphere Species

https://www.jstage.jst.go.jp/article/jsme2/39/3/39_ME24031/_article

[22] [78] [79] [80] [81] [82] [83] These “plastivore” caterpillars can devour a plastic bag in just 24 hours | ScienceDaily

https://www.sciencedaily.com/releases/2025/08/250827010736.htm

[39] [48] [49] [134] [135] IJERPH | Free Full-Text | Biodegradation of Polyethylene by Enterobacter sp. D1 from the Guts of Wax Moth Galleria mellonella

https://www.mdpi.com/1660-4601/16/11/1941/review_report

[58] Mycodegradation of low-density polyethylene by Cladosporium ...

https://www.nature.com/articles/s41598-024-59032-4

[59] Biodegradation of synthetic plastics by the extracellular lipase of ...

https://www.sciencedirect.com/science/article/pii/S2666765724000814

[60] Fungal biodegradation of low-density polyethylene using consortium ...

https://www.sciencedirect.com/science/article/pii/S2405844021011117

[61] Fungal biodegradation of low-density polyethylene using consortium ...

https://www.academia.edu/97391270/Fungal_biodegradation_of_low_density_polyethylene_using_consortium_of_Aspergillus_species_under_controlled_conditions

[63] Fungal Enzymes Involved in Plastics Biodegradation - PMC

https://pmc.ncbi.nlm.nih.gov/articles/PMC9230134/

[64] Biodegradation of polyethylene by Meyerozyma guilliermondii and ...

https://www.sciencedirect.com/science/article/abs/pii/S0048969722057035

[66] [67] [71] [72] [73] [85] [133] Scientists question study about plastic-eating caterpillars | ScienceDaily

https://www.sciencedaily.com/releases/2017/09/170915144156.htm

[68] [69] [70] [74] [75] [76] [77] Frontiers | The Bacterial and Fungal Gut Microbiota of the Greater Wax Moth, Galleria mellonella L. Consuming Polyethylene and Polystyrene

https://www.frontiersin.org/journals/microbiology/articles/10.3389/fmicb.2022.918861/full

[84] Latest Trends on Insect Larvae, Their Enzymes and Their Gut ...

https://www.preprints.org/manuscript/202411.1632/v1