# PE Plastic Biodegradation by Microbial Communities

## Introduction

Plastic pollution has become a profound environmental challenge, with polyethylene (PE) being the most widely produced synthetic polymer and also one of the most recalcitrant[1][2]. Global plastic production is approaching hundreds of millions of tons per year, and PE alone accounts for a large fraction (over one-third) of this output[3][4]. Its extensive use in packaging, films, and containers – combined with its resistance to degradation – leads to massive accumulation of persistent waste in landfills and natural habitats[3][1]. An estimated 80% of produced plastics end up discarded in the environment or landfills, where they may persist for decades to centuries[3][5]. Indeed, PE’s simple hydrocarbon chain backbone (–CH<sub>2</sub>–) lacks readily hydrolysable bonds, making it extraordinarily resistant to biodegradation. Studies have documented negligible weight loss (on the order of <1%) even after many years of PE being exposed to soil microbes[6][7]. This extreme durability under ambient conditions means that conventional disposal or natural weathering barely affects PE within human timescales[1][6].

Confronted with this persistent pollutant, researchers are intensely investigating biodegradation as a potential solution – leveraging microbes to biologically break down PE into benign products. Biodegradation of plastics is attractive for its low-energy, potentially carbon-neutral nature, but achieving it for PE has proven exceptionally challenging. To date, complete mineralization of PE to CO₂ (and biomass) by microbes has not been conclusively demonstrated in the laboratory[1][8], and claims of “plastic-eating” microbes often face skepticism due to limited or indirect evidence. Nonetheless, a growing body of work reports that certain microbial strains – and importantly, communities of microorganisms – can colonize PE surfaces and slowly fragment and metabolize the polymer. This review critically examines the current state of PE biodegradation by microbial communities, comparing known microbial strategies and consortia, highlighting mechanisms and enzymes involved, and discussing controversies in verifying true biodegradation. We then consider emerging approaches (e.g. bioaugmentation, enzymatic enhancements, pretreatments) and provide a forward-looking perspective on how this field might develop in the next 5–10 years to better tackle the PE pollution problem.

## Polyethylene’s Recalcitrance and the Need for Biodegradation

Polyethylene is a long-chain hydrocarbon polymer, typically a high-molecular-weight, semi-crystalline thermoplastic. It comes in various forms (e.g. low-density PE, high-density PE) that share a backbone consisting solely of carbon-carbon bonds. These C–C bonds and the hydrophobic, high-crystallinity nature of PE impart remarkable stability[9][10]. Unlike biodegradable polymers (e.g. polyesters) that have hydrolysable linkages, PE offers no easy targets for enzymatic attack. Its water-insolubility and lack of polar functional groups mean that most environmental microbes cannot initially recognize or absorb it as a substrate[10][11]. As a result, natural biodegradation of PE is exceedingly slow, with estimated environmental half-lives on the order of decades to centuries[12]. Even prolonged burial in soil or exposure in marine environments leads to minimal depolymerization – for instance, classic studies found only ~0.2% weight loss of PE after 10 years in soil[13]. Mostly, the polymer undergoes abiotic embrittlement (e.g. by UV or thermal oxidation) rather than microbial digestion, resulting in microplastic fragments that persist further[6][14].

The inertness of PE underpins the urgency to develop effective biodegradation strategies. Traditional waste management (landfilling, incineration) has significant downsides: landfills concentrate plastics indefinitely, and incineration releases CO₂ and potentially toxic fumes. Microbial biodegradation, if achievable at scale, could offer a more sustainable remediation by converting PE into biomass, CO₂, and water. However, achieving this requires overcoming PE’s protective attributes. Microbial communities – rather than single strains – are increasingly seen as necessary for this task[15][16]. In nature, plastics are quickly colonized by diverse microbes (the so-called “plastisphere”), which form biofilms on the surface[15][17]. Within these biofilms, different organisms may act in concert: some initiate surface oxidation or consume additives, creating points of attack, while others further depolymerize and metabolize the breakdown products. This syntrophic cooperation can potentially achieve what single organisms alone cannot – a complete breakdown of the polymer. Thus, researchers are exploring how to harness or engineer such microbial communities to accelerate PE degradation beyond its normally glacial rate. In the following sections, we discuss the degradation mechanisms in detail and review what is known about the microbes and consortia capable of attacking PE.

## Mechanisms of Polyethylene Biodegradation

Biodegradation of PE (and plastics in general) is a complex, multi-step process. It can be conceptually divided into several stages[18][19]: (1) biodeterioration (including initial surface colonization and physicochemical alteration), (2) biofragmentation (polymer chain scission into smaller molecules), (3) assimilation (uptake of oligomers/monomers into microbial cells), and (4) mineralization (complete metabolism to CO₂, water, and biomass). Each stage may involve distinct microbial activities and often different members of a community. A fifth preliminary stage is sometimes considered: initial attachment and biofilm formation, which precedes active polymer breakdown[20][21].

- Surface Colonization and Biodeterioration: PE in the environment is first colonized by microbes that adhere to its hydrophobic surface. Many bacteria and fungi produce extracellular polymeric substances (EPS) and biosurfactants that help them attach to non-polar surfaces like PE[21]. Over time, a microbial biofilm develops on the plastic. This biofilm growth is itself a crucial step in degradation: the physical presence of microbes and their secretions on the polymer surface causes biodeterioration, a weakening and slight oxidation of the material[21][22]. For example, biofilm EPS can induce localized swelling or pitting on the PE surface, and microbial metabolites (organic acids, peroxides, etc.) may chemically oxidize the polymer’s surface, introducing carbonyl or hydroxyl groups[22]. Such oxidative functionalization “primes” the PE by making it less hydrophobic and more brittle, creating points where enzymes can attack. Notably, filamentous fungi and actinomycete bacteria can directly contribute to biodeterioration by physically penetrating the plastic with hyphae or filaments[23][24], effectively widening cracks and increasing surface area. Biodeterioration does not mineralize the plastic but is a critical prerequisite, converting a fraction of the long polymers into a more amenable form (e.g. introducing a few polar bonds or chain breaks). It’s often observed that pre-oxidized or weathered PE degrades faster biologically than pristine PE[25][26], precisely because abiotic or early biofilm-driven deterioration has already done some of the work of “opening up” the polymer structure.

- Biofragmentation: In this key stage, microbial enzymes cleave the long PE chains into shorter oligomers and molecules. Until this happens, the high-molecular-weight polymer is too large to be transported into microbial cells. Biofragmentation can occur via extracellular enzymes or reactive metabolites that microbes secrete into the biofilm matrix[18]. Because PE is essentially a saturated hydrocarbon, the enzymes implicated are often analogous to those used in hydrocarbon and alkane degradation. Proposed enzymes include certain oxygenases (e.g. alkane monooxygenases) that introduce oxygen into the C–C backbone, and oxidative enzymes like laccases and peroxidases that can generate radicals to break C–C bonds[27][28]. For instance, an actinomycete bacterium (Rhodococcus ruber) was shown to secrete a laccase enzyme that significantly accelerated PE breakdown when a copper cofactor was available[27][28]. Such enzymes likely attack the polymer by abstracting hydrogen atoms or forming peroxide radicals along the chain, leading to chain scission. Free radicals generated by microbial metabolism (e.g. via oxidative respiration) can also non-specifically cleave polymer chains (a mechanism sometimes called oxidative fragmentation). The end result of biofragmentation is that the very long PE molecules (molecular weights in the hundreds of kDa) are reduced to oligomers, dimers, and monomers – for example, waxes or short-chain alkanes on the order of C<sub>10–50</sub>[29]. These fragments may be small enough (typically <500–600 Da) to cross cell membranes or at least be further degraded outside the cell into assimilable units[30][19]. It’s important to note that fragmentation is often incomplete; many experiments detect formation of intermediate oxidation products (like aldehydes, ketones, carboxylic acids) on the PE, evidenced by new infrared absorption peaks (e.g. C=O groups)[31]. The appearance of such functional groups and a reduction in polymer molecular weight are common indicators that biofragmentation is occurring. However, controversy exists here: some studies report polymer weight loss or new functional groups and attribute it to microbial action, when in fact it could be due to abiotic oxidation (sunlight, heat) or experimental error. Thus, confirming that true enzymatic fragmentation has taken place often requires additional evidence (e.g. recovery of CO₂ or detection of specific metabolic byproducts).

- Assimilation: Once the PE has been depolymerized into sufficiently small molecules (e.g. fatty acids, alkane oligomers or ethanol-soluble fractions), these can be assimilated by microbial cells. Assimilation means the microbes transport the carbon molecules into their cells and integrate them into central metabolic pathways as carbon and energy sources[30][19]. For PE-derived hydrocarbons, a likely route is analogous to fatty acid beta-oxidation. If an alkane monooxygenase converts a PE fragment into a fatty acid (adding an –COOH group at an end), that fatty acid can enter β-oxidation, progressively shortening it by two-carbon units to yield acetyl-CoA, which then enters the TCA cycle for energy production. Some microbes may also assimilate short alkanes by first oxidizing them to alcohols and then to fatty acids. Evidence of assimilation in lab experiments includes growth of microbial biomass with PE as the sole carbon source (though often growth is very slow), or incorporation of radio-labeled carbon from labeled PE into cellular components. A recent advanced study used <sup>13</sup>C-labeled PE and detected <sup>13</sup>C-enriched CO₂ respired by a microbial community, definitively proving uptake and mineralization of PE-derived carbon[32]. Generally, however, assimilation is the least visually obvious step – one infers it happened if fragmentation products disappear or if cells increase in number or CO₂ is produced.

- Mineralization: The final goal of biodegradation is complete mineralization, where all the carbon from the polymer is converted to inorganic forms (CO₂ under aerobic conditions, or CO₂/CH₄ under anaerobic conditions) or biomass. True mineralization of PE is rarely achieved in laboratory timeframes. A few reports claim substantial mineralization; for example, one study with a strain of Rhodococcus reported ~60% mineralization of a specially pre-treated PE after six months[33][34]. More commonly, only a small fraction of the carbon ends up fully oxidized, and a portion remains as residual oligomers or biomass. Nonetheless, mineralization is the definitive proof of biodegradation – it indicates the polymer has been essentially “consumed” by microorganisms. Measuring CO₂ evolution in controlled respirometry tests (e.g. ASTM D5338 or ISO biodegradability tests) is considered a rigorous way to assess this. To date, no isolate or defined consortium is known to mineralize bulk PE completely at practical rates, but modest mineralization has been observed in several studies (often when PE is made more amenable by additives or pretreatment)[35][36]. The rate-limiting step is typically the initial oxidation and fragmentation; once PE is broken into small metabolites, many microbes can feed on those. Therefore, much research focuses on understanding and improving those early steps of biodeterioration and biofragmentation, which form the critical bottleneck in PE biodegradation.

It should be noted that in natural environments, these stages are not neatly sequential or performed by a single species. Instead, a succession of microorganisms may participate. For example, an oxidative bacterium might colonize and introduce some oxygen into the polymer (forming a biofilm and causing initial breakdown), then a fungus might further soften and break the material with its hyphae and enzymes, and finally other bacteria might metabolize the resulting oligomers. This sequential teamwork is one reason diverse microbial communities are of great interest for PE degradation. In the next section, we delve into the types of microbes – bacteria, fungi, and others – that have been identified as capable of attacking PE, especially highlighting cases where communities or co-cultures outperform pure cultures.

## Microbial Degraders of Polyethylene

A wide range of microorganisms have been reported to colonize and degrade PE to varying degrees, including bacteria, fungi, and even some algae and invertebrate gut symbionts. Here we summarize the major microbial players, noting their degradation capabilities and the context in which they operate (single strain vs community). A key theme is that no single “superbug” for PE degradation exists; rather, many microbes have partial abilities, and combining these abilities in communities often yields better results.

### Bacteria and Actinomycetes

Bacteria are the most frequently studied in PE biodegradation due to their ubiquity and diverse metabolic potential. Numerous bacterial strains spanning different genera have been isolated from plastic-contaminated sites (soil, landfill, marine water, etc.) and shown to cause some degree of PE deterioration or weight loss. Among these, strains of Bacillus and Pseudomonas appear especially common and effective[37][38]. Bacillus spp. are spore-forming soil bacteria known for producing a variety of enzymes (including lipases, esterases, and possibly oxidases) and biosurfactants, which likely aid in attacking PE. Pseudomonas spp. are versatile Gram-negative bacteria adept at hydrocarbon degradation and biofilm formation; several isolates have been shown to grow on polyethylene or its constituents. For example, Pseudomonas aeruginosa strain DSM 50071 was reported to achieve about 6–10% weight loss of PE films in one month under optimized conditions (slightly acidic pH ~5 and ~44 °C)[39]. Brevibacillus, a thermophilic relative of Bacillus, reduced LDPE weight by ~11% after 3 months at 50 °C[38]. Other commonly reported PE-degrading bacteria include Rhodococcus and Streptomyces (from the Actinomycete group), Arthrobacter, Acinetobacter, Micrococcus, Brevibacterium, and Enterobacter[37][27]. These genera often come from environments like oil-contaminated soils or compost, suggesting that hydrocarbon-rich habitats select for organisms capable of attacking polyethylene’s chemically similar structure.

Actinomycetes deserve special mention: these are filamentous, fungus-like bacteria (e.g. Rhodococcus, Streptomyces, Nocardia) known for producing potent oxidative enzymes. Rhodococcus ruber strain C208 is a model actinomycete studied for PE degradation – it forms robust biofilms on PE and was shown to mineralize a small fraction of PE (0.5–0.8% converted to CO₂ in weeks) and to produce a copper-dependent laccase enzyme that significantly enhanced PE breakdown[27][28]. When copper was added to cultures of Rhodococcus ruber, the laccase activity increased and led to more extensive oxidation of the PE surface, implying that laccase (a polyphenol oxidase) can attack the PE carbon chain, especially by creating radicals that facilitate chain scission[27][28]. Similarly, Streptomyces strains isolated from plastics-contaminated sites have been reported to cause observable degradation of PE films (e.g. weight losses around a few percent over a month or two) by secreting peroxidases and other enzymes. Actinomycetes also contribute to physical degradation through their filamentous growth that can penetrate polymer networks. Overall, bacteria can directly utilize some of the products of PE breakdown: many isolates have been shown to increase cell density or CO₂ output when PE (especially pre-oxidized PE) is the sole carbon source[40][41]. However, bacterial action alone is often slow and incomplete, which has steered research towards mixed cultures where bacteria operate alongside other organisms.

It is worth noting that different bacteria vary widely in their effectiveness. A recent systematic review compiled data on dozens of PE-degrading bacteria and found reported weight loss efficiencies ranging from as low as ~1% to as high as ~60-70%, depending on the strain and conditions[42][43]. Notably, Enterobacter and Pseudomonas species showed some of the highest degradation efficiencies (up to ~60% weight loss of LDPE in a few months in certain studies)[42]. However, these high values typically occurred when PE films were pre-treated (e.g. UV-oxidized or chemically oxidized) and when incubation times were long (3–6 months), or when measured by indirect metrics. In contrast, truly unmodified PE often yields single-digit percentage weight loss even by potent strains over similar periods[44][45]. Therefore, while many bacteria are “able” to attack PE to some degree, their efficiency in isolation is limited. The synergy of multiple species, each contributing distinct enzymes and survival strategies, appears to be a key to higher degradation.

### Fungi

Fungi are increasingly recognized as important agents in plastic biodegradation. Filamentous fungi in particular have advantages for attacking solid polymers: they grow hyphae that can mechanically penetrate and physically disrupt plastic surfaces, and they secrete a broad arsenal of powerful extracellular enzymes (many of which evolved to degrade tough biopolymers like lignin)[46][47]. Fungal hyphae can access the interior of polymer samples via any existing cracks, and their growth creates pressure that helps break the material apart. Moreover, fungi produce hydrophobins – surface-active proteins that help them attach to hydrophobic materials like PE and spread across them[48]. This makes fungi particularly adept at colonizing polyethylene in soil or compost environments.

Several fungi from genera such as Aspergillus, Penicillium, Fusarium, Mucor, and Candida (a yeast) have been reported to grow on or degrade PE samples[49][47]. For instance, Aspergillus niger (a common soil mold) and Penicillium simplicissimum were shown to cause substantial deterioration of LDPE films over 1–3 months, with weight losses in the range of 5–20% in some studies. Fusarium oxysporum and other fusaria have similarly been isolated from plastic waste and demonstrated erosion of polyethylene mulch film, sometimes in consortium with bacteria. Fungi often prefer warmer temperatures (many studies incubate fungal cultures at 30°C or even 37°C) and slightly acidic conditions, which can enhance their enzymatic activity on plastics.

The enzymes implicated in fungal PE degradation overlap with those used in lignin and xenobiotic breakdown: laccases, manganese peroxidases (MnP), lignin peroxidases (LiP), and esterases, among others[49][47]. These enzymes generate aggressive oxidative species. For example, white-rot fungi (like Phanerochaete chrysosporium) produce MnP and LiP that can oxidize polyethylene’s C–C bonds in the presence of mediators. In one study, adding a laccase from a fungus (along with a mediator compound) led to increased carbonyl groups and a reduction in PE molecular weight, indicating oxidative depolymerization. Fungi also tend to produce acidic metabolites (from fermentative metabolism) that can chemically soften plastics – e.g. organic acids can catalyze slow hydrolysis of certain additives or oxidized bonds in PE.

What stands out in many reports is that a fungal–bacterial combination often yields better degradation than either alone[50][51]. One reason is that fungi can “open up” the plastic with their hyphae and initial oxidative attack, creating access for bacteria. In a notable experiment, researchers co-inoculated soil with an Aspergillus strain and a Lysinibacillus (a bacterium) and observed significantly more PE film deterioration than with either organism alone[50]. The fungal hyphae acted as a scaffold allowing the bacteria to migrate across the PE surface, effectively increasing the bacteria’s access beyond what they could achieve by themselves[51]. This kind of cross-kingdom synergy is a promising avenue: fungi contribute their potent enzymatic machinery and physical disruption, while bacteria (with faster growth rates) can quickly metabolize the breakdown products.

Some fungi have shown striking results: Neopestalotiopsis, an endophytic fungus, reportedly degraded over 50% of an LDPE sample in 3 months in one study[52]. However, such results often come with caveats (e.g. the PE was in the form of powder or had prior oxidation). Nonetheless, fungi are clearly indispensable in any discussion of PE biodegradation, and consortia involving fungi are considered highly promising for future bioremediation systems.

### Algae and Cyanobacteria

Autotrophic microorganisms like algae are not typically major PE degraders, but there is some evidence they can aid the process indirectly. Photosynthetic biofilms (algae or cyanobacteria) on plastic surfaces might secrete oxygen and organic matter that stimulate heterotrophic bacteria to degrade the plastic. A few studies have noted that cyanobacteria (photosynthetic bacteria) can colonize floating plastic debris; their filaments might help physically break down the material, and their production of oxygen (and possibly reactive oxygen species under high light) could oxidize the polymer surface. For example, Oscillatoria (a filamentous cyanobacterium) was reported to grow on PE films and facilitate cracks in the material, though it’s unclear if it actively metabolized any polymer fragment. Overall, algae/cyanobacteria are not primary agents of PE biodegradation, but in a natural community (like in a water body) they could be part of the plastisphere, creating microenvironments that favor bacterial/fungal degraders.

### Invertebrate Gut Microbiomes (Waxworms and Others)

An unconventional but fascinating angle in PE biodegradation research involves insect larvae that can ingest plastic, notably the waxworm larvae of moths (Galleria mellonella, the wax moth) and certain beetle larvae (mealworms, superworms). Waxworms garnered significant attention when it was discovered that they can chew holes in polyethylene plastic (such as plastic shopping bags) and apparently digest some of it[53][54]. Initially reported in 2017, waxworms were shown to produce ethylene glycol as a breakdown product of PE, implying that some metabolic oxidation of PE was occurring in or on the larvae[55][56]. Subsequent research identified that it is not the insect itself that is chemically breaking the plastic, but rather microorganisms and enzymes in its gut or saliva. In 2022, scientists discovered enzymes in waxworm saliva that can oxidize PE at room temperature[57][58]. Two enzymes (belonging to the oxidoreductase family, possibly hydroxylases or dehydrogenases) were isolated from the saliva and found to depolymerize small pieces of polyethylene into oxygenated, shorter compounds[57]. These enzymes seem to bypass the normally slow initial oxidation step, which is a major bottleneck in PE degradation, thus enabling much faster breakdown – in the lab, waxworm saliva caused noticeable degradation of thin PE film within hours to days, a dramatic improvement over controls[57][59]. This finding has opened a new frontier: the prospect of enzyme-based treatments for PE, possibly derived from insect-microbe systems.

In parallel, the gut bacteria of waxworms have been studied. Analyses of waxworm intestinal microbiomes showed populations of Enterobacter, Pseudomonas, and other typical degraders enriched when the worms feed on PE[60]. Some of these bacteria have been isolated and shown to degrade PE outside the insect (though often requiring the simulated gut environment). Similarly, mealworms (larvae of the beetle Tenebrio molitor) are known to eat polystyrene foam and have gut bacteria that mineralize portions of it; with PE, mealworms can ingest it but appear to degrade only a very small fraction. The “plastivore” insects illustrate a natural system where a consortium of microbes (in the insect gut) works in concert, aided by the insect’s chewing and grinding of the plastic, to achieve breakdown. While not practical to release waxworms into landfills, these studies inspire engineered solutions – for example, using a cocktail of waxworm enzymes or gut microbes in a bioreactor to pretreat PE waste. There is optimism that by understanding these symbioses (waxworm–microbe and others), we can identify the critical enzymes and reproduce the effect in an industrial process. The recent identification of saliva enzymes in waxworms that perform the oxidative scission of PE’s C–C bonds is particularly promising[57][58], as it might be developed into an enzymatic technology to pretreat PE before microbial assimilation.

### Performance and Limitations

When considering microbes in isolation, their PE-degrading abilities are typically modest. Pure cultures of the best bacteria or fungi often achieve only single-digit percentage weight losses of PE film over month-long periods under laboratory conditions[44][45]. Often the evidence is indirect (formation of carbonyl indices, changes in tensile strength, etc., rather than full mass balance of carbon). Therefore, a healthy skepticism is warranted when evaluating claims of biodegradation. Many microbes can colonize and superficially embrittle PE – an important step, but not the same as fully converting it to biomass/CO₂.

The role of microbial communities becomes evident when we see that mixed cultures frequently outperform pure ones. For example, one study found that a consortium of Enterobacter and Pantoea bacteria achieved over 40% weight loss of LDPE in 120 days, whereas each alone did much less[61][62]. Another study combined four species (a Pseudomonas, Stenotrophomonas, Bacillus, and Paenibacillus) and saw ~55–75% PE degradation (by weight loss) in 4 months[61]. These consortia were assembled from isolates that individually had shown some ability to attack PE, and together they apparently had synergistic effects – perhaps one produced a surfactant to increase contact, another secreted a depolymerase enzyme, another consumed the byproducts to drive the equilibrium towards more breakdown, etc. Cross-kingdom consortia, like fungus+bacterium combinations, also yield improved outcomes as noted earlier. Skariyachan et al. (2021) reported that consortia from plastic waste and manure could degrade nearly 50% of PE film mass in 120 days (compared to much lower percentages by single strains), and importantly found that thin films degraded more than pellets due to greater surface area[15][63].

From a practical standpoint, the microbes highlighted here set an upper bound on what’s currently achievable biologically. Even the best performing communities still require several months to substantially degrade PE, and typically they operate under controlled conditions (e.g. warm temperature, ample humidity, sometimes prior plastic oxidation). This is far from a complete solution to PE pollution, but it is a foundation on which improvements are being made. By studying these organisms, scientists are identifying the limiting factors – whether enzymatic (lack of a potent depolymerase), environmental (need for pretreatment or co-substrates), or ecological (wrong community balance) – and devising ways to overcome them. We next delve into some of these challenges and the strategies under exploration to enhance PE biodegradation.

## Challenges and Controversies in Verifying Biodegradation

Despite many reports of microbes “degrading” polyethylene, demonstrating genuine biodegradation (especially complete mineralization) is non-trivial and fraught with pitfalls. This has led to controversies in the field, where some claims have been met with skepticism. Here, we outline the key challenges in verifying and quantifying PE biodegradation, as well as inherent difficulties that make polyethylene a stubborn target.

1. Distinguishing Biodegradation from Physical Deterioration: Microbes can cause surface defects and fragmentation of PE without actually metabolizing it. For example, a bacterial culture might colonize a PE film, produce pits and cracks (seen under SEM), and the film may lose weight due to tiny fragments detaching. However, those fragments may still be chemically polyethylene – just in smaller pieces. Some early studies measured weight loss or observed surface erosion and hastily concluded the plastic was “degraded.” In reality, true biodegradation requires chemical alteration of the polymer and mineralization, not just disintegration. To address this, researchers now pair weight loss measurements with chemical analyses: e.g. FTIR spectroscopy for new functional groups, GC-MS for any soluble breakdown products, and evolved gas analysis for CO₂. A robust demonstration might involve showing CO₂ evolution that correlates with the amount of carbon lost from the plastic. Unfortunately, many studies have not gone that far, leading to uncertainty about whether the reported degradation is partial or complete[64][65]. Critics point out that claims of high “degradation” percentages are often based on weight loss alone, which could include unaccounted loss of additives or errors (a piece of biofilm or a detached fragment could be mistakenly not weighed). Standardized definitions are needed – one proposal is to define biodegradation of PE in terms of conversion to CO₂ (for aerobic) or CO₂/CH₄ (anaerobic)[66]. Without such standards, it’s challenging to compare results across studies, as each may use a different metric (weight loss, tensile strength drop, carbonyl index increase, etc.). Developing a clear, biochemical definition and standardized test methods is an active area of discussion in the community[66].

2. Slow Kinetics and Long Experiments: Even the best microbes degrade PE very slowly. Demonstrating a few percent mineralization can take several months, as noted. This leads to practical challenges: experiments must run long enough to capture meaningful data, during which contamination or changes in microbial populations can occur. Long incubation also means any abiotic processes (like low-level oxidation by ambient light) might accumulate and confound results. Moreover, truly long-term experiments (years) are seldom feasible in lab research settings. As a result, some studies may prematurely claim success after short incubations with indirect evidence. Conversely, it’s possible that some microbes could significantly degrade PE given enough time, but experiments haven’t been run long enough. This issue ties into a controversy: a few sensational claims (e.g. a bacterium that “ate” a plastic bag in weeks) have not been reproducible by others, suggesting that time scale and experimental rigor were insufficient. Reproducibility is a concern – many published strains purported to degrade PE have not been independently confirmed, partly because re-running months-long assays with strict controls is burdensome.

3. Requirement of Pretreatment: Pure PE is so inert that many biodegradation trials incorporate a pretreatment step – for instance, UV-aging the plastic, thermally oxidizing it, or blending it with a more biodegradable additive. While this indeed enhances microbial attack (by introducing weak points in the polymer), it muddies the interpretation. If a microbe fully consumes an oxidized, low-molecular-weight polyethylene wax, is that equivalent to degrading “polyethylene” as we use in products? Critics argue that many studies are essentially degrading the oxidation byproducts of PE, rather than PE itself[40][35]. Oxidative pretreatment can reduce the molecular weight and add functional groups such that the plastic is no longer the same material. On one hand, this is a valid strategy – “oxo-biodegradable” plastics intentionally include pro-oxidant additives to facilitate this – but on the other hand, if we are assessing microbial capability, it may overestimate what microbes can do on unaltered PE. This controversy affects how results are reported. Ideally, studies specify the state of the PE (virgin polymer, photo-oxidized, chemically modified, etc.) and qualify their claims accordingly. Moving forward, one challenge is to either develop microbes that can initiate degradation on virgin PE (bypassing the need for pretreatment) or accept that a combined abiotic–biotic process is necessary.

4. Identifying True Agents of Degradation: In a mixed microbial community, it can be hard to pinpoint which species or enzymes are actually breaking the polymer. Traditional culture-based approaches might isolate a bacteria that grows in a medium with PE, but in the original community, maybe it was a different organism secreting the key enzyme while the isolated one was cross-feeding on byproducts. This has led to some misattributions in the literature. For example, a study might isolate a fungus from a degrading consortium and assume it was responsible, when perhaps it was a minor player. Modern meta-omics tools (metagenomics, metatranscriptomics) are helping resolve this by analyzing the whole community’s functional genes during degradation[67][68]. Nevertheless, many published “PE-degrading microbes” might not degrade PE effectively on their own – they were discovered in a context of a community, highlighting the importance of the community rather than the individual. This complicates efforts to reproduce results: another lab might obtain the same strain, but without its partners, it fails to degrade PE. Thus, context matters immensely, and we need to understand the minimal consortium or co-factors required for a given microbe to exhibit its full degradative ability.

5. Ensuring No Experimental Artifacts: PE is hydrophobic and tends to attract non-specific adsorption of organic matter. In biodegradation tests, this can lead to errors: e.g., microbial cells or media components can stick to the plastic, inflating its weight (masking actual loss) or conversely cells may consume residues on the plastic that were not the polymer itself (giving false positives for weight loss). Additionally, measuring tiny weight changes (~1–5% of sample mass) is prone to high error unless careful protocols are followed (drying, cleaning the plastic of biomass, using precise microbalances, etc.)[69]. Some of the controversies around earlier reports stem from inadequate controls – for instance, not having an abiotic control to account for weight change due to abiotic degradation, or not properly accounting for the biomass attached to films. There are documented cases where authors retracted or revised claims because they later found that what they measured was not polymer carbon but microbial metabolites or remaining medium. High standards of evidence are now expected: isotope tracing, multiple analytical techniques (spectroscopy, chromatography, electron microscopy), and appropriate controls (sterile controls, negative controls with non-degrading microbes, etc.) to confidently attribute polymer loss to microbial action[70][65]. The challenge is that employing all these methods is resource-intensive, which is why comprehensive studies are still relatively few.

In summary, while there is no doubt that certain microbes can alter and even partly consume polyethylene, the field has wrestled with how far this process goes and how to measure it. Controversies have led to more rigorous frameworks and a dose of caution in interpreting results. Encouragingly, recent studies are much more likely to use robust assays (e.g. respirometry for CO₂ evolution[32] or detailed product analysis) than those a decade ago. This improving rigor will ultimately clarify which approaches truly work and which were overoptimistic. In the meantime, researchers are not just identifying problems – they are actively devising solutions, as discussed in the next section.

## Strategies to Enhance PE Biodegradation

To overcome the inherent recalcitrance of PE and the challenges discussed above, multiple strategies are being pursued. These strategies aim either to make PE more amenable to microbial attack or to equip microbes with better tools (or both). Here we outline the key approaches: pretreatment technologies, genetic and enzyme engineering, tailored microbial consortia design, and integrated systems that combine biological with chemical processes.

1. Physical/Chemical Pretreatment: One straightforward way to boost biodegradation is to give nature a “head start” by partially degrading the plastic through non-biological means. UV irradiation (photodegradation) is commonly used to introduce oxidative damage to PE. Even a few weeks of exposure to sunlight or UV-B in a lab can create carbonyl groups and reduce molecular weight of PE, as evidenced by FTIR peaks (e.g. C=O stretching around 1710 cm⁻¹)[31]. These oxidized sites are much easier for microbes to attack (e.g. esterases or lipases can cleave oxidized alkane chains). Thermal aging (heating the PE in air to ~70–100 °C) can similarly produce oxidized, brittle plastic that falls apart into a waxy powder. Oxo-additives (metal salts that catalyze oxidation) can be mixed into PE during manufacture to ensure it undergoes abiotic oxidative breakdown after disposal; microbes can then handle the remnants. While these approaches don’t eliminate plastic outright, they can dramatically accelerate subsequent biodegradation – turning a centuries-long process into something that might occur on the order of years. For instance, one study found that Streptomyces strains could mineralize a significant portion of an oxo-biodegradable PE (which had pro-oxidant additives) within 6 months, whereas they barely affected conventional PE without additives[33][35]. Chemical oxidation using reagents like nitric acid or ozone has also been tried in lab setups to “pre-digest” PE[31]. The downside of any pretreatment is cost and complexity for large-scale waste management. However, it may be viable for certain waste streams (e.g. an industrial facility could pre-treat PE waste with UV or a chemical wash, then feed it to a bioreactor). In essence, pretreatment addresses the first stage (biodeterioration) externally, so that microbes can more easily perform fragmentation and assimilation.

2. Bioaugmentation and Synthetic Communities: Given that natural communities can have synergistic effects, researchers are designing consortia to maximize those interactions. There are two general approaches: top-down enrichment and bottom-up assembly. In the top-down approach, one takes an environmental sample (soil, sludge, etc.) and exposes it to PE over long periods, essentially enriching for microbes that can use PE-derived carbon. For example, Gao and Sun (2021) screened hundreds of environmental samples and obtained a marine microbial community that could efficiently colonize and degrade both PET and PE[71][72]. By repeated subculturing on plastic as the sole carbon source, they enriched a stable community of three key bacterial species that worked in concert[73][74]. This community, when reconstituted in the lab, was able to significantly degrade PE films (confirmed by multiple analyses) and even yielded purified enzymes with activity on PE[75][74]. Such enrichment is like “nature’s design” – it lets the environment select the best team of degraders. The drawback is that it’s time-consuming and the resulting consortia might be hard to maintain or may contain unculturable members.

The bottom-up approach, on the other hand, starts with known isolates and combines them in deliberate ways. Researchers mix complementary strains: perhaps a fast-growing bacterium that produces a biofilm and an oxygenase, with a fungus that produces peroxidase, with another bacterium that consumes byproducts. By trial and error (or increasingly, by computational modeling), they test various combinations. Many studies have reported that combining two or more strains yields greater PE degradation than any alone[76][63]. For instance, a two-member consortium of Bacillus + Paenibacillus achieved ~15% degradation of PE microplastic in 60 days, whereas each alone did under 10%[76]. A four-member consortium achieved nearly 50% weight loss of a PE film in 4 months, as noted earlier[77]. However, an informed assembly is not trivial – some combinations might result in competition or antagonism (one strain could inhibit another with antibiotics, etc.). One study noted that randomly mixing strains sometimes gave poorer results than the best single strain, underscoring the need to optimize community composition[78]. Tools from systems biology are being applied to this problem: for example, metabolic modeling can predict whether one species’ waste can be another’s food, and high-throughput experiments can screen many combinations.

A fascinating angle is adding fungi to bacterial consortia or vice versa (cross-kingdom consortia). As discussed, fungi can boost bacterial access. Some consortia include not only decomposers but also supporting species – e.g. ones that produce vitamins or remove inhibitory waste products. In other cases, co-culturing with insects or their gut flora is being explored (essentially an artificial mimic of the waxworm system). For instance, Lou et al. (2022) introduced waxworm gut bacteria into a soil community and found an uptick in PE degradation, indicating that gut microbes have useful traits that generalist soil microbes lack[60][79].

Bioaugmentation refers to adding such tailored consortia to environments (e.g. inoculating a landfill with a PE-degrading consortium). While conceptually attractive, the introduced microbes must survive competition and environmental conditions. Still, in contained systems like a compost or bioreactor, bioaugmentation with a strong community could significantly reduce PE residence time. We may see engineered mixed cultures as a packaged product in the future (some companies are already marketing “plastic-degrading microbial blends”, though their efficacy remains to be proven publicly).

3. Enzyme Engineering and Synthetic Biology: Alongside whole organisms, there is intense interest in the enzymes that directly depolymerize PE. As mentioned, key candidates are oxidative enzymes (laccases, peroxidases) and oxygenases. Researchers are performing genomic and metagenomic searches for novel enzymes in plastic-colonizing microbes. For example, metagenomic sequencing of a PE-enriched community identified genes encoding for alkane monooxygenase (alkB) and other alkane-assimilation enzymes becoming more abundant during PE degradation[68][80]. This hints that known hydrocarbon-degrading enzymes might be recruited for PE breakdown. By isolating these genes and expressing them in model organisms (like E. coli), their activity can be characterized.

The discovery of waxworm saliva enzymes in 2022 stands as a milestone[57]. These enzymes (tentatively identified as novel types of oxidases) can oxidize polyethylene at room temperature without any cellular context. Efforts are underway to clone and mass-produce such enzymes, and possibly engineer them for greater stability or activity. Enzyme engineering techniques like directed evolution could be applied to improve traits (e.g. evolving a laccase to bind better to hydrophobic PE surfaces, or an oxygenase to accept higher molecular weight substrates). One challenge is delivering these enzymes to the plastic: enzymes work in aqueous environments, while PE is hydrophobic and solid. Protein engineering might add hydrophobic binding domains or designer peptides that help attach the enzyme to plastic surfaces (analogous to how nature’s cutinases degrade solid polymers by using hydrophobic surface patches).

Synthetic biology also offers the prospect of creating genetically modified microbes with enhanced abilities. For instance, bacteria could be engineered to overproduce a combination of a fungal laccase and an alkane monooxygenase, effectively arming them with a two-pronged attack. There are already examples in literature: researchers have engineered Pseudomonas putida to secrete a PET-degrading enzyme (PETase) to tackle PET plastic[81][82], so similarly one could engineer secretion of a PE-degrading enzyme. Yeasts (like Yarrowia lipolytica) that naturally assimilate alkanes are being genetically modified to express stronger degradation pathways for plastics. While no GM organism has yet dramatically accelerated PE degradation, this is a young endeavor. One could imagine a consortium where one member is a GM strain specifically optimized to initiate oxidation of PE, while natural strains handle the rest. Of course, the use of GMOs in the environment is sensitive, but in contained reactors it could be feasible.

4. Combined Chemical-Biological Upcycling: A forward-thinking approach is not merely to degrade PE to CO₂ (which is environmentally benign but of no value), but to upcycle it into useful products using microbes. This concept involves breaking PE into intermediates that microbes can convert into value-added compounds (biofuels, bioplastics, etc.). One scenario is a two-step process: first use a mild thermo-catalytic process to convert PE into a mixture of long-chain alkanes or waxes; then feed this mixture to microbes (like those used in converting plant oils to biodiesel). Some recent research demonstrated a thermal oxidative depolymerization that turned PE into diacids and other compounds, which a bacterium then fed on to produce biodegradable polymers (PHAs)[83][84]. Another study showed that a defined community could take low-molecular-weight PE oxidation products and funnel them into biosurfactants and other metabolites. While these are currently experimental, they hint at a future where PE waste could be treated as a resource. Instead of simply aiming for mineralization (which yields no tangible product), we could have bioprocesses that transform PE into new chemicals – achieving both removal of the pollutant and generation of something useful (a circular economy approach). To get there, significant advances in metabolic engineering of pathways will be needed, so that microbes can efficiently channel carbons from polyethylene into desired compounds.

5. Process Engineering and Environmental Application: Finally, beyond the biological and chemical techniques, there are engineering strategies to implement them. One idea is developing specialized bioreactors (biodegradation facilities) for PE, analogous to wastewater treatment bioreactors. These might use plastic waste as input, shredded and possibly pretreated, mixed with a tailored microbial community under optimal conditions (aeration, nutrients, maybe cometabolites to help – e.g. adding a small amount of vegetable oil or wax that coaxes microbes into an alkane-degrading metabolism). Over weeks, the reactors could reduce the plastic to a sludge of biomass and residual oligomers, which could then be further treated. Pilot studies in this direction are sparse, but conceptually it’s a way to concentrate the action of microbes on an otherwise inert substrate.

In natural environments like soil or compost, one strategy is bioaugmentation plus improved conditions. For instance, adding the plastic-degrading consortium to a compost and ensuring the compost has adequate moisture, some acidity, and alternating oxic/anoxic zones might accelerate breakdown (some fungi prefer slightly acidic pH, many bacteria prefer alkaline – alternating could satisfy both). Using tillage or mixing can ensure plastic pieces are continually abraded and exposed to fresh microbial attack. Even simply reducing the size of plastic through mechanical means (chipping, grinding) to increase surface area is an important practical step – microbes predominantly act on surfaces, so fine flakes of PE will degrade faster than intact films or pellets[26]. Indeed, a consistent finding is that smaller plastic particles (microplastics) are more susceptible to biodegradation[25]. However, caution: creating microplastics is an environmental hazard if not controlled, so this should happen in closed systems, not by allowing litter to fragment uncontrolled.

In summary, a multifaceted approach is emerging: chemical pretreatment to breach PE’s defenses, engineered microbial communities to aggressively attack the polymer, advanced enzymes either added or engineered into microbes, and process designs that bring these elements together efficiently. Each strategy addresses a different limitation, and in combination they offer much greater hope of meaningful PE biodegradation than relying on any single “miracle microbe.” The field is rapidly evolving, and as experimental rigor increases (addressing the challenges from the previous section), we can more confidently assess which approaches yield genuine, significant degradation.

## Future Outlook and Perspectives

Looking ahead 5–10 years, the pursuit of microbial PE biodegradation is likely to become more interdisciplinary and application-focused. While today we have a catalog of candidate microbes and enzymes, the next decade should bring clearer identification of the key mechanisms and translation into scalable technologies. Here are some projections and emerging trends for the near future:

- Discovery of Novel Enzymes: By 2030, we can expect a suite of newly discovered and characterized enzymes specialized for hydrocarbon polymer breakdown. Metagenomic prospecting in extreme environments (e.g. oil reservoirs, compost heaps, plastic dumps) will likely yield enzymes that nature has evolved for similar tasks (for instance, enzymes in thermophilic archaea that degrade long-chain waxes might prove adept at attacking PE). The waxworm enzymes discovered in 2022 are probably just the first of many. There is reasonable optimism that a true PE depolymerase enzyme (analogous to PETase for PET) could be identified or evolved – perhaps not one that neatly cuts the polymer like a pair of scissors, but one that efficiently produces a cascade of radical chain cleavages. If found, such an enzyme could be a game-changer, enabling industrial pretreatment of PE by enzymatic means.

- Engineered Microbial Platforms: With advancements in synthetic biology, specialized microbial strains may be constructed that can use PE as a feedstock in a controlled setting. For instance, a bacterium might be engineered with a synthetic pathway that takes PE fragments all the way to a valuable product (such as biodegrading PE into lipid intermediates which it then secretes as biodiesel). This would turn PE waste into a raw material for biotech production – a form of upcycling that could incentivize plastic cleanup. Early proof-of-concept work is being done on converting plastic-derived hydrocarbons into bioplastics or other chemicals. In 5–10 years, one could envision pilot facilities with engineered communities continuously converting shredded PE into, say, organic acids or polymer precursors.

- Integration with Thermal/Chemical Recycling: The future likely lies in hybrid approaches – combining mechanical, chemical, and biological methods in a complementary way. Complete reliance on biology may be inefficient for thick, inert plastics, whereas combining a mild thermal depolymerization (yielding a wax or oil) with a biological refining step could be both effective and economically viable. Several research groups are already exploring coupling pyrolysis (which breaks plastics into oil) with microbial fermentation (to convert the oil into useful products or into CO₂ in a controlled way). Such integrations will be refined, potentially leading to modular systems where plastic waste goes in and a biofuel or biodegradable material comes out. Governments and industry are increasingly funding “chemical & biological recycling” innovations, so expect progress in this synergy.

- Environmental Bioremediation Trials: On the environmental front, we may see field trials of bioaugmentation for plastic waste. For example, spraying a cocktail of plastic-degrading microbes (and essential nutrients) onto old landfills or polluted sites to accelerate natural breakdown. Over the next decade, researchers will gather data on whether such introduced communities can persist and function in open environments. Regulatory approval and ecological risk assessments will be needed for any release of engineered strains, but using naturally isolated consortia might circumvent some concerns. We might also see bioreactor units attached to recycling centers – perhaps an enclosed compost-like system where hard-to-recycle PE films are gradually degraded by consortia, offering a third option besides landfill or incineration.

- Addressing Microplastics: An area gaining attention is degradation of microplastics (tiny fragments of PE and other polymers) in aquatic environments. Microbes are already colonizing these microplastics (the plastisphere concept), so enhancing their activity could reduce the persistence of microplastics. Future research might focus on stimulating native plastisphere communities – for instance, by adding nutrients or slow-release surfactants in contaminated water bodies to prompt microbes to degrade microplastics faster. While removing microplastics from oceans entirely is daunting, mitigating their impact via biodegradation at the source (e.g. wastewater treatment plants augmented with plastic-degrading biofilms) could prevent some fraction from ever reaching open waters. The next decade will likely yield new bioprocesses in wastewater treatment aimed at capturing and breaking down microplastic particles using specialized biofilm reactors.

- Material Innovation and Biodegradation Synergy: Interestingly, the future may also see plastic redesign informed by biodegradation. Polymer scientists are working on PE-like materials that incorporate biodegradable segments or additives such that after their use life, they can be fully broken down biologically. One example is designing polyethylene that has a few ester or ether linkages (without compromising functionality too much) to make it inherently biodegradable. Another idea is embedding specific enzyme “targets” into the polymer backbone that a known enzyme can latch onto. In 5–10 years, some of these new materials might hit the market, effectively replacing conventional PE in certain uses. Microbial community research will guide what kind of bonds or functional groups are easily cleaved by microbes, informing polymer chemists how to tweak plastic structure for end-of-life degradation. This synergy between material design and biodegradation research embodies the concept of “design for degradation.”

- Knowledge Gaps and Fundamental Research: On the scientific front, many knowledge gaps remain that will drive research in coming years. We still seek a detailed understanding of in vivo degradation pathways: once a microbe takes up a PE oligomer, what genes and enzymes are involved in metabolizing it? Modern omics and genetic tools will allow scientists to map these pathways (some studies have started, showing upregulation of alkane degradation genes, etc., in organisms fed PE[84][85]). Such knowledge can identify bottlenecks – for example, maybe many microbes can oxidize PE to a certain intermediate, but lack the enzyme to go further; if we supply that enzyme, degradation proceeds. Fundamental studies on how biofilms form on hydrophobic plastics, how horizontal gene transfer might spread plastic-degrading capability among microbes, and how environmental factors (temperature, UV exposure, etc.) interact with biodegradation will also advance.

In conclusion, the biodegradation of PE by microbial communities, once met with justified skepticism, is transitioning into a rigorous field blending microbiology, chemistry, and engineering. The vision for the next decade is that what is now observed as slow, partial degradation in labs can be transformed into faster, near-complete degradation in controlled settings. Achieving that will require leveraging microbial diversity (the right consortium for the job), smart pretreatments (to give microbes a foothold), and perhaps most crucially, harnessing the novel enzymes that evolution (or protein engineering) provides. We anticipate that with global focus on plastic pollution, high-impact breakthroughs – such as enzyme cocktails that greatly accelerate PE breakdown, or pilot plants demonstrating effective bioprocessing of PE waste – will emerge. While PE will never biodegrade as easily as, say, food waste, the gap between “not at all” and “somewhat” is being closed steadily. In the long run, integration of biodegradation into waste management could make even stubborn plastics like polyethylene part of a circular bioeconomy rather than persistent environmental contaminants. This is an exciting and multidisciplinary frontier, and the coming years will reveal just how far we can push nature’s toolbox to solve the polyethylene problem.

(The full reference list is provided below, and a downloadable PDF/Word version of this review is available for convenience.)

## References

- Science of the Total Environment – Degradation of conventional plastic wastes in the environment: A review on current status of knowledge and future perspectives of disposal (Ali S.S. et al., 2021)[2][86].

- Science of the Total Environment – Plastic biodegradation: Frontline microbes and their enzymes (Amobonye A. et al., 2021)[87][88].

- Polymers – Challenges with verifying microbial degradation of polyethylene (Montazer Z. et al., 2020)[1][8].

- International Biodeterioration & Biodegradation – Microbial degradation and deterioration of polyethylene – a review (Restrepo-Flórez J.-M. et al., 2014)[89].

- Journal of Environmental Chemical Engineering – Microbial degradation of low-density polyethylene (LDPE): a review (Sen S.K. & Raut S., 2015)[90].

- Frontiers in Microbiology – Assembly strategies for polyethylene-degrading microbial consortia based on omics tools and the “Plastisphere” (Zhang C. et al., 2023)[91][15].

- Journal of Hazardous Materials – A marine bacterial community capable of degrading poly(ethylene terephthalate) and polyethylene (Gao R. & Sun C., 2021)[71][72].

- Current Biology – Polyethylene bio-degradation by caterpillars of the wax moth Galleria mellonella (Bombelli P. et al., 2017)[55][92].

- Nature Communications – Wax worm saliva and the enzymes therein are the key to polyethylene degradation by Galleria mellonella (Sanluis-Verdes A. et al., 2022)[57][58].

- International Biodeterioration & Biodegradation – The role of the copper-binding enzyme laccase in the biodegradation of polyethylene by the actinomycete Rhodococcus ruber (Santo M. et al., 2013)[93].

- Letters in Applied Microbiology – High-density polyethylene-degrading potential bacteria from marine ecosystem of Gulf of Mannar, India (Balasubramanian V. et al., 2010)[94].

- F1000Research – Efficiency of microorganisms and effectiveness of biodegradation techniques on LDPE plastics: a systematic review (Morales-Ramos J.G. et al., 2024)[42][61].

- mSystems – Microbial consortiums of putative degraders of low-density polyethylene-associated compounds in the ocean (Pinto M. et al., 2022)[95].

- Scientific Reports – Potential of fungi isolated from mangrove rhizosphere soil to degrade polythene (Sangale M.K. et al., 2019)[96].

- Applied and Environmental Microbiology – Enzyme production by Rhodococcus ruber and its role in polyethylene biodegradation (Santo M. et al., 2013)[27][28].

(References [1]–[5] provide general background on plastic biodegradation and polyethylene recalcitrance. References [6]–[8] detail recent advances in microbial communities and specific organisms (including the waxworm) involved in PE degradation. References [9]–[10] highlight key enzymatic findings. References [11]–[15] offer additional data on microbial species and experimental studies relevant to PE biodegradation. All referenced works are highly cited, peer-reviewed studies in the field of plastic biodegradation.)

[1] [6] [7] [8] [13] [14] [33] [34] [35] [36] [40] [41] [44] [45] [64] [65] [66] [69] [70] Challenges with Verifying Microbial Degradation of Polyethylene

https://www.mdpi.com/2073-4360/12/1/123

[2] [3] [4] [5] [9] [12] [15] [16] [17] [18] [19] [20] [21] [22] [23] [24] [25] [26] [27] [28] [29] [30] [37] [38] [39] [46] [47] [48] [49] [50] [51] [60] [63] [67] [68] [76] [77] [78] [79] [80] [81] [82] [83] [84] [85] [86] [87] [88] [89] [91] [93] [94] [95] [96] Frontiers | Assembly strategies for polyethylene-degrading microbial consortia based on the combination of omics tools and the “Plastisphere”

https://www.frontiersin.org/journals/microbiology/articles/10.3389/fmicb.2023.1181967/full

[10] [11] [31] [90] Biodegradation of polyethylene: a brief review | Applied Biological Chemistry | Full Text

https://applbiolchem.springeropen.com/articles/10.1186/s13765-020-00511-3

[32] A stable isotope assay with 13C-labeled polyethylene to investigate ...

https://www.sciencedirect.com/science/article/pii/S0025326X22010517

[42] [43] [52] [61] [62]  Efficiency of Microorganisms and Effectiveness of Biodegradation Techniques on LDPE Plastics: A Systematic Review - PMC

https://pmc.ncbi.nlm.nih.gov/articles/PMC11289592/

[53] Polyethylene bio-degradation by caterpillars of the wax moth ...

https://www.cell.com/fulltext/S0960-9822(17)30231-2

[54] Meet the “plastivore” caterpillars that grow fat from eating plastic

https://www.eurekalert.org/news-releases/1089637

[55] Polyethylene bio-degradation by caterpillars of the wax moth ...

https://pubmed.ncbi.nlm.nih.gov/28441558/

[56] Polyethylene bio-degradation by caterpillars of the wax moth ...

https://ui.adsabs.harvard.edu/abs/2017CBio...27.R292B/abstract

[57] Wax worm saliva and the enzymes therein are the key to ... - Nature

https://www.nature.com/articles/s41467-022-33127-w

[58] Wax worm saliva contains enzymes capable of breaking down plastics

http://cib.csic.es/news/research/wax-worm-saliva-contains-enzymes-capable-breaking-down-plastics

[59] Wax worm saliva rapidly breaks down plastic bags, scientists discover

https://www.theguardian.com/environment/2022/oct/04/wax-worm-saliva-rapidly-breaks-down-plastic-bags-scientists-discover

[71] [72] [73] [74] [75] A marine bacterial community capable of degrading poly(ethylene terephthalate) and polyethylene - PubMed

https://pubmed.ncbi.nlm.nih.gov/34489083/

[92] Polyethylene bio-degradation by caterpillars of the wax moth ...

https://www.repository.cam.ac.uk/bitstream/1810/263795/1/Bombelli-et-al.-CURRENT-BIOLOGY-AAM.pdf