# PE Plastic Biodegradation by Microbial Community

## Abstract

Polyethylene (PE) is one of the most ubiquitous and recalcitrant synthetic polymers, posing a major environmental challenge due to its resistance to biodegradation. This review examines the state-of-the-art in PE plastic biodegradation by microbial communities, emphasizing recent insights into the microbes, enzymes, and collaborative strategies involved. We first outline the unique properties of PE that confer its persistence and the stepwise mechanisms by which microbes can, albeit slowly, depolymerize and assimilate this polymer. We then discuss the diversity of microorganisms capable of attacking PE – from bacteria (e.g., Bacillus, Pseudomonas, Rhodococcus) to fungi (e.g., Aspergillus, Penicillium) – and the key enzymes (such as oxygenases and laccases) that initiate PE oxidation. A critical analysis is presented on microbial consortia and their synergistic advantages in PE degradation, highlighting how interspecies cooperation can overcome some limitations of single strains. We compare studies of individual isolates versus mixed communities, including cross-kingdom collaborations and microbiomes from insect guts, to illustrate how microbial communities enhance degradation efficiency. The review also addresses methodological challenges in confirming true biodegradation of PE and differentiating it from mere physical disintegration. Finally, we offer perspectives on emerging approaches – like bio-augmentation, pretreatments, enzyme engineering, and integrated chemical–biological upcycling – that are expected to accelerate PE biodegradation in the coming decade. This comprehensive analysis aims to provide advanced researchers a cohesive understanding of current progress, controversies, and future directions in microbial PE biodegradation, toward ultimately harnessing microbial communities for mitigating plastic waste.

(This document is formatted in Markdown for clarity and can be converted to PDF or Word for convenient reading.)

## Introduction

Plastic pollution has become a pervasive environmental issue, with polyethylene (PE) being a leading contributor due to its extensive production and use (hundreds of millions of tons annually)【1】. PE is a polyolefin polymer characterized by a backbone of strong C–C bonds; this chemical structure, while imparting desirable durability to plastics, renders PE highly resistant to natural biodegradation【2】. Indeed, polyolefin plastics like PE are among the most persistent synthetic materials in landfills and oceans, capable of lingering for decades with minimal degradation【2】【3】. Nevertheless, certain microorganisms have demonstrated the ability to slowly attack PE under specific conditions, sparking interest in harnessing biodegradation as an eco-friendly remediation strategy【3】【4】. Over the past two decades, researchers have isolated a variety of bacteria and fungi that can colonize and partially degrade PE, and more recently, complex microbial consortia have shown enhanced degradation compared to single species. This review provides a comprehensive analysis of PE biodegradation by microbial communities, examining how these communities work, what limitations they face, and how biotechnology might boost their efficacy. We begin by reviewing the inherent challenges of PE biodegradation and the general mechanisms by which microbes can break down this stubborn polymer.

## Polyethylene Structure and Recalcitrance

PE’s molecular structure is essentially a long, hydrophobic aliphatic chain with a high molecular weight and minimal functional groups. The polymer can be linear or branched (e.g., high-density vs. low-density PE), but in all forms it has a carbon–carbon backbone lacking hydrolysable bonds【4】. This structure leads to several factors impeding biodegradation: (i) extremely low solubility in water and high hydrophobicity, making the polymer inaccessible to most microbial enzymes; (ii) a high degree of crystallinity in many PE materials, where tightly packed crystalline regions are impervious to enzyme penetration; and (iii) the strength of the C–C and C–H bonds, which are not readily cleaved by the enzymes that microbes normally use to degrade natural polymers【2】. As a result, PE can persist for years or longer in the environment without significant biological breakdown【2】. Microbes generally cannot directly assimilate intact PE; they must first overcome an activation energy barrier to initiate depolymerization of this inert substrate【3】. Common environmental factors like ultraviolet (UV) light and heat can slowly oxidize PE (a process known as photo-oxidative aging), introducing carbonyl groups and causing some polymer chain scission. Such pre-oxidation can increase the material’s susceptibility to microbial attack by creating points of enzymatic entry【5】. In the absence of any pretreatment, however, the biodegradation of PE is exceedingly slow – often only a few percent of weight loss over several months in laboratory studies【5】. These challenges underline why PE was long deemed “non-biodegradable.” Yet, accumulated evidence now shows that given the right organisms and conditions, PE can undergo a degree of biodegradation, though achieving environmentally meaningful rates remains difficult. In the following sections, we describe how microbes engage in this process, step by step.

## Mechanisms of Microbial Polyethylene Biodegradation

Microbial degradation of PE (and plastics in general) is a multistage process (Figure 1). It begins with biodeterioration of the polymer’s surface, followed by biofragmentation of the polymer chains, and concludes with assimilation and mineralization of the breakdown products【4】. In the initial phase, microbial cells colonize the surface of the plastic. Many PE-degrading microbes form biofilms – communities of cells embedded in extracellular polymeric substances – on the hydrophobic PE surface【4】. The biofilm not only helps cells adhere to the otherwise non-wetting plastic, but also can cause surface pitting and micro-cracks, a form of biodeterioration that mechanically weakens the plastic (often visible via electron microscopy as etching or fragmentation of the surface). Once firmly attached, the microbes secrete a suite of extracellular enzymes or reactive metabolites that attack the polymer. During the biofragmentation stage, these enzymes cleave the long PE chains into smaller molecular units such as oligomers (e.g., tens of carbon atoms long), dimers, or monomers【4】. Because intact PE is too large to be transported into microbial cells, exo-enzymatic breakdown is a prerequisite to actual biodegradation. Oxidative enzymes introduce functional groups (e.g., alcohols or carboxylates) into the polymer, rupturing C–C bonds and yielding shorter, oxygenated fragments. At that point, the micro-oligomers (typically ≤C_15–C_40 in size) can be taken up by the cells – the assimilation phase – and metabolized through central pathways【4】. Once inside the microbial metabolism, these carbon compounds can be further degraded via β-oxidation and other enzymatic steps to yield basic metabolites. Finally, under aerobic conditions, the ultimate end products of complete mineralization are carbon dioxide, water, and biomass. (Under anaerobic conditions, methane or other fermentation products may be formed instead of CO_2.) It is important to note that incomplete biodegradation will result in transformation of the polymer into lower-molecular-weight residues (e.g., waxes, short hydrocarbons) without full mineralization, an outcome observed in many cases. The overall biodegradation process is thus complex and often rate-limited at the initial depolymerization step – breaking the highly stable C–C bonds of PE requires specialized biochemical capabilities.

Figure 1: Schematic representation of the polyethylene biodegradation process by microorganisms. Initially (i) microbes attach to the PE surface and form biofilms, aided by secreted biosurfactants and sticky extracellular polymers. Then (ii) biodeterioration of the plastic occurs as surface colonies etch and crack the polymer (for example, fungal hyphae can physically penetrate the material). Next (iii) biofragmentation takes place: extracellular oxidative enzymes (such as oxygenases, peroxidases) cleave the long PE chains into shorter oligomers or monomers. Once sufficiently depolymerized, (iv) the small fragments are assimilated into microbial cells and metabolized. Finally, (v) mineralization is achieved as the fragments are catabolized to CO₂, H₂O, and biomass. Adapted from reference [4].

In the context of these stages, the rate of overall PE biodegradation is typically very slow. Standard laboratory biodegradation tests (e.g., OECD 301 guidelines) require observing 60% mineralization within 28 days to classify a substance as “readily biodegradable,” a benchmark that no current PE-degrading microbe or consortium meets for un-pretreated PE【4】. Indeed, many experimental studies report only a few percent polymer weight loss after months of incubation【5】. This underscores that even when microbial degradation occurs, it tends to be an incomplete and protracted process for PE. However, even limited depolymerization is significant because it can convert PE into smaller molecules that might be further degraded by other organisms in nature. The next sections identify which microbes are capable of initiating these processes and how they accomplish the critical first steps of polymer attack.

## Microbial Players in PE Biodegradation

### Bacterial Degraders and Enzymes

A variety of bacteria have been reported to colonize and degrade polyethylene to some extent. Predominant among these are species of Actinobacteria and Proteobacteria. Notably, strains of Bacillus, Pseudomonas, and Rhodococcus are frequently isolated from plastic-contaminated soils or sludge as potential PE degraders【4】【5】. For example, Bacillus spp. and Pseudomonas spp. are not only common hydrocarbon-degrading bacteria but have also been shown to form biofilms on PE film and effect measurable weight loss of the polymer【4】. Rhodococcus ruber, an actinomycete, is a model PE-degrading bacterium; it can form a robust biofilm on PE surfaces and secrete oxidative enzymes that partly depolymerize the plastic. In one study, a Rhodococcus strain achieved roughly 0.8% weight loss of PE per week by continuous biofilm action【5】. Other notable genera include Arthrobacter, Acinetobacter, Streptomyces, Nocardia, and Mycobacterium, among others, which have been identified in enriched communities on disposed PE【4】. Many of these bacteria are known for their ability to degrade hydrocarbons or xenobiotic compounds, suggesting they leverage similar catabolic pathways to tackle PE’s long alkane-like chains.

Bacteria employ a range of enzymes to attack PE. Because PE lacks easily hydrolysable bonds, typical hydrolases (like those that cut polyesters or polyurethanes) are ineffective. Instead, oxidative enzymes appear to play a key role in initiating PE degradation【4】【7】. One group of such enzymes are laccase-like multicopper oxidases. Rhodococcus ruber strain C208, for instance, secretes a laccase that, in the presence of copper, significantly enhances PE oxidation and depolymerization【7】. Laccases can generate reactive radicals that abstract hydrogen from the PE chain, leading to peroxidation of the polymer. Another important set of enzymes are the alkane hydroxylases (often encoded by alkB genes in bacteria). These are membrane-bound monooxygenases that normally initiate the catabolism of aliphatic hydrocarbons (by adding an –OH to a terminal methyl group of an alkane). In PE-degrading bacteria, alkane monooxygenase systems are implicated in attacking the polymer chain ends or oxidized sites【6】. For example, in a Pseudomonas aeruginosa strain, two alkane monooxygenase isozymes (AlkB1 and AlkB2) were studied; AlkB2 showed higher activity on long-chain alkanes and was more strongly induced during growth on low-molecular-weight PE, suggesting it effectively kick-starts PE chain oxidation【6】. Once the polymer is oxidatively cleaved into shorter chemicals (such as fatty acids or dicarboxylic acids), these intermediates can enter common bacterial metabolic routes. Terminal oxidation of PE fragments yields compounds like octadecanoic acid, which bacteria can further degrade via β-oxidation pathways【4】. Enzymes such as alcohol dehydrogenases and aldehyde dehydrogenases would then convert alcohols (from initial oxidation) to fatty acids, which are progressively shortened to acetyl-CoA units feeding into the TCA cycle. Additionally, peroxidases (e.g., manganese peroxidase, lignin peroxidase) have been identified in some PE-degrading microbes, especially fungi; these can catalyze oxidative bond-cleavage in a manner akin to lignin degradation【4】【2】. Overall, while multiple enzyme classes are likely involved, a concerted oxidative attack is believed to be the primary mode by which bacteria start breaking PE’s long chains. It is worth noting that truly specialized PE-degrading enzymes (analogous to the PETase enzyme for PET plastics) have not yet been discovered – current evidence points to microbes repurposing broad-specificity enzymes from hydrocarbon degradation pathways to handle PE【3】. Identifying such dedicated enzymes remains a key research frontier.

### Fungal Contributions to PE Degradation

Fungi are increasingly recognized as important players in plastic biodegradation. Certain fungi can grow directly on PE surfaces and often outperform bacteria in initiating polymer breakdown【2】. The advantage of fungi lies partly in their mycelial growth form: filamentous fungi (molds) produce hyphae that can physically penetrate and spread across polymer surfaces, promoting biodeterioration. This mechanical action can pry apart the polymer structure, particularly in semi-crystalline plastics where fungi may invade the amorphous regions【4】. Fungi also secrete potent oxidative enzymes into their surroundings. Species of Aspergillus, Penicillium, Fusarium, Cladosporium, and Mucor have all been reported to colonize and cause slow degradation of PE films【2】【4】. Aspergillus niger and Penicillium simplicissimum, for example, have been shown to erode PE strips over the course of several weeks, with observable changes in the material’s surface morphology and slight weight reduction. Like bacteria, fungi rely on oxidative enzymes for depolymerization of PE. They possess extracellular peroxidases and laccases that can generate free radicals and oxidize inert polymers. In one study, a marine-derived fungus Alternaria sp. upregulated numerous oxidase and peroxidase genes when incubated with PE, indicating a broad enzymatic assault on the polymer【4】. Fungal laccases have been directly tested on PE: the laccase from R. ruber (though bacterial in origin) and similar multicopper oxidases from fungi can cause measurable oxidation of PE, introducing carbonyl groups into the polymer structure【7】. Fungi often also produce biosurfactants and hydrophobins – small proteins that help them adhere to hydrophobic surfaces【2】. These factors facilitate tight binding of fungal hyphae to the PE, effectively “wetting” the plastic with enzymes. Some research has shown that adding nutrients or co-substrates can stimulate fungal attack on PE, possibly by priming the production of necessary enzymes. While fungi alone seldom achieve high mineralization of PE, they are extremely valuable in consortia, where fungal activity can pre-condition the plastic for further bacterial degradation. For instance, fungi might soften or partially oxidize the polymer, after which bacteria in the community metabolize the resulting fragments. In summary, fungal isolates expand the range of biological tools for PE degradation and often initiate processes that bacterial enzymes alone struggle to begin.

### Notable Studies: Rates and Extents of Degradation

It is instructive to compare some outcomes from the literature to gauge what level of PE biodegradation has been achieved under laboratory conditions (Table 1). Early reports of single strains showed modest results – for example, a thermophilic Brevibacillus sp. isolated from soil was found to reduce the weight of an LDPE film by about 11% after several weeks of incubation【4】. Likewise, a Pseudomonas aeruginosa culture in an acidic medium achieved ~6% weight loss of PE in 30 days at 44 °C【4】. These values, while small, were significant at the time as proof-of-concept that bacteria can indeed depolymerize PE to a detectable degree. More recently, much higher degradation extents have been reported using enriched microbial consortia. Park and Kim (2019) isolated a two-species consortium (a Bacillus plus a Paenibacillus strain) from landfill soil; this consortium degraded nearly 15% of added PE micro-particles over 60 days【8】. In another study, a cross-domain consortium of an Aspergillus niger fungus and a Lysinibacillus bacterium was able to degrade ~16% of an LDPE film in 4 months (and up to 30% if the PE was first mildly oxidized by UV exposure)【10】. Even more striking, a marine plastisphere-derived consortium of four bacterial species reported by Joshi et al. (2022) achieved about 47% weight loss of LDPE film after 120 days【12】. Such high values likely benefit from both synergistic microbial interactions and the use of pre-treated or accessible forms of PE (e.g., microplastics or oxidized films). It must be noted that standard test criteria (60% mineralization in 28 days) are still far from reach for any of these systems, but the improvements are evident. Table 1 summarizes several representative cases of PE biodegradation to highlight the differences between single microbes and communities, as well as the effect of pretreatments.

Table 1: Selected examples of polyethylene biodegradation by microbes and consortia. (Outcomes refer to weight loss or other degradation metrics under the specified conditions.)

| Microorganism(s) | PE Form & Conditions | Degradation Outcome | Reference |
| --- | --- | --- | --- |
| Brevibacillus sp. (strain 707, thermophile) | LDPE film; ~50 °C; 30 days | ~11% weight loss | [4] |
| Pseudomonas aeruginosa (single isolate) | LDPE strips; pH 5, 44 °C; 30 days | 6.3% weight loss | [4] |
| Bacterial consortium (2 spp.) – Bacillus + Paenibacillus | PE microparticles; 30 °C; 60 days (no pretreatment) | 14.7% weight loss; reduced particle size | [8] |
| Fungal–bacterial consortium – Aspergillus niger + Lysinibacillus sp. | LDPE film buried in soil; 28 ± 2 °C; 4 months; (UV-pretreatment 25 days for some samples) | 15.8% weight loss (untreated PE); 29.5% with UV-pretreated PE | [10] |
| Waxworm gut community – Meyerozyma (yeast) + Serratia (bacterium) | PE film; 30 °C; 45 days (shaken culture) | 15.9% weight loss (consortium outperforming either strain alone) | [11] |
| Marine mixed consortium (4 bacteria from plastisphere) | LDPE sheet; 30 °C; 120 days (no pretreatment) | 47% weight loss; extensive surface pitting and oxidation detected | [12] |
| Engineered approach: PE pre-oxidation + microbial consortium | PE (powder form) first chemically oxidized, then fed to enriched culture; various species | Near-complete conversion of PE to oxidized metabolites and CO₂ (estimated >90% conversion) | [13] |

(Table 1 illustrates that multi-strain consortia generally achieve greater PE degradation than single isolates. Pretreatment (e.g., UV oxidation) can dramatically boost the extent of biodegradation. Engineered chemo-biological methods (bottom row) show promise for full conversion of PE into smaller molecules.)

## Synergistic Effects in Microbial Consortia

A central theme in recent research is that microbial communities – rather than isolated strains – are often necessary to achieve meaningful biodegradation of PE【4】. In natural environments, plastics become colonized by diverse microbial assemblages (the so-called “plastisphere”), wherein bacteria, fungi, algae, and others coexist on the plastic surface. These communities can collectively carry out decomposition steps that no single organism can accomplish alone. There are several reasons why consortia outperform pure cultures in PE degradation【4】:

- Enzyme and Metabolic Diversity: A consortium pools the catalytic capacities of multiple organisms, yielding a richer enzyme arsenal. Different community members may specialize in attacking different molecular weight fractions or oxidation states of the polymer. This breadth of enzymatic activity increases the likelihood of breaking down a complex substrate like PE【4】. For example, one bacterium might secrete a potent oxidase to introduce oxygen into the polymer, while another bacterium or fungus can further cleave the oxidized segments – a division of labor impossible for either alone.

- Sequential Metabolism: In a community, the metabolic byproducts of one organism can be nutrients for another. This is critical for plastics, where initial depolymerization often produces partially degraded molecules that might inhibit the original degrader if they accumulate. In consortia, such intermediates can be consumed by other members, preventing feedback inhibition and driving the degradation process forward【4】. This “cross-feeding” ensures that no buildup of toxic or growth-limiting metabolites stalls the overall process.

- Biofilm Architecture and Stability: Mixed communities often form more stable and thicker biofilms on PE surfaces than monocultures【4】. Some bacteria in the consortium may primarily produce extracellular polymeric substances that enhance biofilm cohesion and adhesion to PE, even if those bacteria do not directly degrade the polymer. These helper organisms facilitate the colonization by key degraders. The consortium as a whole can thus maintain a sustained attack on the PE, whereas a single strain might fail to remain attached or viable over long periods.

- Microenvironment Creation: Within a biofilm, micro-consortia can create localized environments (pH, redox conditions, etc.) that favor certain degradation reactions. For example, one microbe’s metabolism might consume oxygen rapidly, creating anaerobic niches where anaerobes can thrive and perhaps perform reductive degradation steps. Although PE degradation is generally an aerobic process, these subtle microenvironment effects can influence enzyme activity and community dynamics【4】.

- Quorum Sensing and Regulation: Communities engage in cell–cell signaling (quorum sensing) that can modulate gene expression for biodegradation pathways. The presence of multiple species can trigger synergistic regulation, turning on pathways that are silent in pure culture【4】. It has been observed that some bacteria upregulate alkane degradation genes more strongly when in co-culture, possibly because community signals or stress responses stimulate a more aggressive metabolic mode.

- Robustness to Perturbation: Mixed cultures tend to be more resilient to environmental fluctuations (temperature shifts, nutrient limitation, etc.). If one strain is inhibited, another can fill its role to some extent. This robustness means consortia can sustain degradation activity under conditions that might kill or deactivate a single strain【4】. In practical applications (like in soil or compost), this stability is crucial.

Concrete examples highlight these advantages. In one study, a defined two-member consortium of Arthrobacter and Streptomyces (both actinobacteria) degraded PE film more efficiently together by forming a better biofilm than either alone【9】. Streptomyces (a filamentous bacterium) created channels in the biofilm and perhaps secreted enzymes that Arthrobacter utilized; meanwhile Arthrobacter produced biosurfactants improving polymer contact. In another case, a fungus–bacterium pair (A. niger with Lysinibacillus) showed that fungal hyphae could serve as a “bridge” for bacterial colonization deep in soil, carrying the bacteria along its filaments to reach buried PE fragments【10】. Here the fungus provided physical access and initial oxidation, and the bacterium likely mineralized some of the oxidized residues – a clear mutualistic interaction. Even the gut microbiomes of plastic-eating insects can be viewed as consortia adapted to degrade polymers. For instance, the gut of waxworm larvae (caterpillars known to chew polyethylene) contains a community of bacteria and yeasts that work together to digest PE particles【12】. Lou et al. (2022) isolated two strains from waxworm guts that when combined degraded PE far more than either alone, attributing this to complementary enzyme production and possibly metabolite exchange【11】.

Overall, synthetic consortia design is an emerging strategy whereby researchers combine isolates with known desirable traits to create a super-degrader community. Approaches include “top-down” enrichment (starting from an environmental sample and selecting for PE degraders through successive subculturing) and “bottom-up” assembly (mixing known degraders and optimizing their ratios and interactions)【4】. Both approaches have yielded consortia with improved performance. For example, a top-down enrichment from marine plastic waste yielded a community that could depolymerize nearly half of an LDPE sheet in laboratory tests【12】. A bottom-up constructed consortium of three novel strains from cow manure achieved over 60% degradation of pre-oxidized PE in 160 days【9】 – a remarkable level compared to single strains. These successes underscore that harnessing synergy is key: no single “super-bug” has yet been found that can efficiently devour PE on its own, but the concerted action of multiple microbes offers a viable path forward.

## Enhancing Biodegradation: Pretreatments and Integrated Approaches

Given the intrinsic resistance of PE, researchers have explored ways to assist microbial communities in the degradation process. One proven method is polymer pretreatment by abiotic means. Mild thermal or UV pretreatment oxidizes the surface layer of PE, creating carbonyl and ester groups that microbes can latch onto. For instance, exposing PE films to UV light for a few days to weeks produces a thin oxidized film (an “oxo-degradable” plastic surface). Microbial consortia can then achieve significantly higher degradation on such pretreated PE – as shown by the ~2× increase in weight loss with UV-oxidized PE versus untreated in the fungal–bacterial consortium example (Table 1)【10】. Pretreatment effectively gives the microbes a “head start” by partially overcoming the initial energy barrier for depolymerization. Thermal aging or exposure to weathering in natural environments similarly makes PE more palatable to microbes over time【5】. Some studies have also used chemical oxidants (e.g., nitric acid or ozone) to generate a spectrum of functional groups on PE prior to biodegradation assays. While pretreatment is not a standalone solution (it fragments the plastic and may generate microplastics), it can be coupled with biodegradation such that the microbes then metabolize what would otherwise be persistent oxidized fragments【5】.

Another line of research focuses on genetic and metabolic engineering to improve microbial degradation capabilities. This includes engineering bacteria to overexpress certain oxidative enzymes or to secrete combinations of enzymes not found in nature. For example, efforts are underway to engineer E. coli or other tractable microbes with alkane monooxygenase pathways and robustness traits so they can attack PE more aggressively【3】. Directed evolution of enzymes – such as modifying laccases or peroxidases to better bind and act on polyethylene – is being explored to create more efficient biocatalysts for polyolefin oxidation【3】. Although no engineered “PEase” enzyme exists yet, advances in protein engineering (like those that yielded highly efficient PET-degrading enzymes) could eventually yield catalysts that break C–C bonds in polymers at useful rates. Synthetic biology also enables the design of synthetic microbial consortia with controlled composition and communication. Researchers can program consortia where one species might sense a polymer oxidation product and then upregulate a complementary pathway in another species (via quorum sensing signals), thereby optimizing the hand-off between depolymerization and mineralization steps.

A particularly promising approach is integrated chemo-biological upcycling of PE waste. In such processes, a first step uses chemical or thermochemical treatment to depolymerize PE into smaller hydrocarbons (for example, via pyrolysis or catalytic oxidation), and a second step employs microbes to convert those intermediates into valuable products【13】. Gregory et al. (2023) demonstrated a two-stage system in which PE was lightly oxidized by a catalyst into long-chain oxygenates (waxes and oils), and then a specialized microbial consortium metabolized those into triacylglycerols (a biofuel precursor)【13】. This combined approach yielded near-complete conversion of PE carbon into useful biomass and molecules, essentially “upcycling” the plastic into new materials. The synergy arises because chemical steps can rapidly reduce polymer length (something microbes alone do slowly), and then microbes can carry out selective and mild conversions of the chemical products into high-value compounds (something pure chemical processes struggle with, as they often yield complex mixtures). Such hybrid strategies play to the strengths of both domains and are expected to gain traction in coming years as the drive for a circular plastic economy grows.

From an application standpoint, any real-world use of microbial PE degradation will need to address scale and efficiency. Bioremediation approaches might involve bioaugmentation (adding tailored consortia to plastic-rich waste sites or composters) and ensuring those microbes have the necessary nutrients and environmental conditions to remain active. There is also interest in designing bioreactors or bio-digesters specifically for plastic waste: these could pre-treat the plastic (e.g., with heat or UV) and then expose it to a concentrated, enzyme-secreting microbial community under optimal conditions. While still conceptual, one could envision an industrial composter where shredded PE films are inoculated with a robust consortium, held at elevated temperature (to speed microbial metabolism) for several months, and periodically supplied with cofactors like copper or manganese (to boost oxidase enzymes). The end result would ideally be CO₂ and water or perhaps biodegradable microbial byproducts. Achieving this in practice will require continued improvements in degradation rates – likely via the avenues discussed: enzyme engineering, microbial community optimization, and smart integration of pretreatments.

## Challenges and Controversies

Despite notable progress, the field of microbial PE biodegradation faces several challenges and points of debate. One major challenge is proving that observed weight loss or changes in PE are due to biodegradation (breaking of polymer chains and mineralization) rather than mere biofragmentation or surface erosion. Many early studies measured slight weight reductions in PE after long incubation with microbes and claimed “biodegradation,” but critics pointed out that these small losses could be explained by loss of additives (plasticizers, fillers) or by microbes consuming low-molecular-weight impurities on the plastic【5】. Weight-loss measurements can also be confounded by biofilm biomass remaining on the plastic, which can either add to the weight or, if not cleaned off properly, be mistaken as polymer residue. To address this, current studies employ a combination of analytical techniques: FTIR spectroscopy to detect new functional groups (like carbonyls) forming in the polymer, GC–MS to identify any released oxidation products in the medium, and SEM/TEM imaging to visually confirm surface degradation【5】. The ultimate proof of biodegradation is the detection of mineralization (e.g., CO₂ evolution from radiolabeled plastic). Such tests have rarely been done for PE due to its recalcitrance, but one study with ^14C-labeled PE did show a small percentage of carbon converting to CO₂ in the presence of a Rhodococcus strain over many weeks【3】. The low rates, however, mean that experiments must run for very long durations to get clear mineralization data, which is practically difficult. This leads to a continuing controversy: how much of the “degraded” PE in any experiment has truly been assimilated and mineralized by microbes versus just converted into microplastic fragments or oxidized oligomers? It is possible, and even likely, that some methods touted as biodegradation actually stop at producing microplastics – which might be even more problematic pollutants.

Another challenge is the reproducibility and standardization of biodegradation assays. Different studies use different forms of PE (powder vs. film vs. pellets), different incubation times (30 days vs. 6 months), different growth media and microbial sources, making it hard to compare results or objectively rank the best strains/consortia【5】. There have been systematic reviews calling for more rigorous controls – for instance, including abiotic controls that undergo the same pretreatment to quantify purely abiotic weight loss, and testing whether the microbes can grow using the plastic as the sole carbon source (a strong indicator of true biodegradation)【5】. Some reports of PE degradation were later met with skepticism because the microbes may have been co-metabolizing the plastic only in the presence of an easier carbon source, meaning they weren’t actually using PE to support growth. Establishing clear criteria (such as no other carbon present, significant CO₂ evolution, etc.) is crucial to validate a claim of PE biodegradation. The field is moving toward adopting standard test methods from environmental engineering (like ASTM or ISO biodegradation tests) to benchmark microbial performance.

A practical controversy is whether focusing on PE biodegradation is the right approach at all. PE is so resistant that even the best natural biodegraders only make a dent in it. Some argue that efforts would be better spent on improving recycling technologies or developing biodegradable plastics to replace PE, rather than trying to make the inherently non-biodegradable PE go away biologically. However, given the massive amount of PE already in the environment, research into biodegradation is justified as part of a multi-pronged solution. A nuanced viewpoint is that complete biodegradation of PE in the open environment may not be achievable on reasonable timescales, but partial biodegradation could help manage plastic waste by, for example, breaking large debris into forms that can be more easily collected or that are less harmful (though microplastics pose their own risks). Another perspective is bio-upcycling: using microbes not necessarily to mineralize PE fully, but to convert it into something useful (like waxes or lipids) that can be harvested【13】. This shifts the goal from waste elimination to resource recovery, potentially changing how success is measured (e.g., yield of product vs. percent CO₂).

Lastly, there are biosafety and ecological questions. If one were to engineer a super-PE-degrading microbe or consortium, what are the risks of releasing it? Could it affect other petroleum-based materials or even living tissue? These are hypothetical concerns at this stage, as no such potent organism exists, but any future biotechnological deployment will need to ensure the microbes function only in the target context (e.g., contained reactors or specific waste facilities). The prospect of spreading microbes to tackle plastic in open environments (like an oil spill cleanup approach) is intriguing but fraught with uncertainties about ecosystem impact. To date, the in situ biodegradation of plastics (in soil or marine settings) appears to be extremely slow – there is scant evidence that native microbial communities significantly reduce environmental PE on short timescales. Enhancing those communities’ activity through biostimulation (adding nutrients, surfactants) or bioaugmentation is experimentally being tested, but whether it can noticeably accelerate natural plastic decay remains unresolved.

## Future Perspectives (5–10 Year Outlook)

The coming decade is likely to witness significant advances in our understanding and application of microbial communities for PE degradation. One anticipated development is the identification of novel microbes and enzymes from unexplored environments. As plastic pollution infiltrates even extreme habitats, microbes are evolving to exploit this new niche. Metagenomic surveys of the plastisphere (the biofilm communities on ocean plastic debris, landfill plastics, etc.) will continue to reveal genes and pathways that confer plastic-degrading abilities【4】. We can expect discoveries of new oxygenases or accessory enzymes that, while not fully “PEases,” enable more efficient depolymerization of recalcitrant polymers. These discoveries will be accelerated by omics tools – e.g., using stable isotope probing with ^13C-labeled PE to directly pinpoint which community members incorporate carbon from PE, then sequencing their genomes/transcriptomes to find the responsible genes. Such techniques could unearth currently uncultivable but important degraders and provide blueprints for engineering.

Speaking of engineering, the field of synthetic biology will likely make substantial contributions. Researchers are already experimenting with inserting hydrocarbon-degradation pathways into fast-growing hosts and improving enzyme secretion systems. In the next few years, we might see a synthetic microbial consortium that has been rationally engineered for PE degradation: for instance, a triculture where Microbe A is engineered to produce a cocktail of effective extracellular oxidases, Microbe B is engineered to robustly uptake and beta-oxidize fatty acid fragments, and Microbe C is a biofilm specialist that glues the consortium together on the plastic surface. By fine-tuning communication and metabolic hand-offs between these members, such a consortium could achieve orders-of-magnitude faster degradation than wild strains. Early steps in this direction are being taken with modeling and machine learning approaches to predict optimal community compositions for polymer degradation【14】.

Another area of progress will be the integration of biodegradation with waste management workflows. Rather than thinking of microbial degradation as an isolated end-of-pipe solution, future strategies might incorporate it as one stage in a multi-step recycling process. For example, one could envision a recycling plant where PE waste that cannot be mechanically recycled (e.g., films contaminated with food waste) is instead directed to a bioprocess. In such a facility, moderate heat or oxidative chemicals break the plastic into a wax, then a tailored microbial community ferments that wax into a commodity chemical or biofuel (as demonstrated in pilot studies)【13】. The economics of this bio-upcycling will drive adoption – if companies can turn waste into profit using microbes, investment will follow. With growing public and regulatory pressure to handle plastic waste sustainably, the next 5–10 years may see pilot plants employing these hybrid chemical–biological methods, especially for polyolefins which currently have poor conventional recycling rates.

Environmental deployment of plastic-degrading consortia might also be tested in contained systems, such as landfill bioreactors. Modern landfills sometimes include anaerobic bioreactor sections to hasten waste stabilization; these could be modified to include aerobic zones inoculated with plastic-degrading communities to break down polyolefin-rich layers. Another concept is the use of enzymatic additives: for instance, embedding slow-release enzyme capsules or pre-seeded microbial spores into plastic items at manufacture, so that when the item becomes waste, it more readily degrades. Some companies are already marketing additives claimed to make plastics biodegradable, but these remain controversial and not definitively proven in scientific studies. In the next decade, however, it’s plausible that engineered enzymes (perhaps immobilized on polymer surfaces) could significantly shorten the time needed for environmental breakdown of disposed PE items.

On the scientific front, key knowledge gaps that researchers will aim to fill include: (a) understanding the limits of biodegradation – e.g., what molecular weight of PE can actually be fully metabolized? Recent work using model alkanes suggests that microbes struggle to consume very long chains (>C_50) efficiently【3】. Determining whether there is a cutoff chain length beyond which biodegradation stalls will inform how we pre-treat plastics. (b) Community dynamics – we need better models to predict how introduced plastic degraders will compete or cooperate with native microbes in complex environments like soil or seawater. Not all introduced strains will survive outside the lab, and indigenous organisms might outcompete them for easier substrates. Research into microbial ecology and evolution in the presence of plastic pollution will shed light on how consortia can be sustained long-term. (c) Quantitative biodegradation assessment – developing standardized, high-throughput assays (perhaps using microplate respirometry or microfluidic devices with plastic samples and communities) will allow rapid screening of many microbial combinations and conditions to identify optimal setups.

In summary, while a fully biodegradable PE polymer may not yet exist, the tools to tackle PE waste biologically are rapidly maturing. Microbial communities, with their innate versatility and adaptability, will be central to any biotechnological solution. The next 5–10 years will likely bring prototype systems where engineered enzymes and microbes collaborate to upcycle polyethylene into useful products, turning our plastic waste problem into a resource opportunity. Concurrently, fundamental discoveries about how nature’s decomposers handle “unnatural” materials like PE will deepen our understanding of microbial evolution and catabolism. With interdisciplinary efforts bridging microbiology, enzymology, and process engineering, the vision of significantly mitigating PE pollution via microbial action moves from the realm of science fiction toward feasible reality.

## Conclusions

Polyethylene biodegradation by microbial communities, once thought unattainable, is now an active area of research with tangible, if incremental, successes. Advanced microbial consortia have shown the capacity to colonize and oxidize this stubborn polymer, especially when aided by pretreatments or metabolic engineering. Key takeaways from this review include the importance of synergistic interactions in consortia, the role of oxidative enzymes in initiating PE breakdown, and the value of integrating biological processes with chemical methods to enhance efficiency. Many challenges remain – notably, achieving higher rates of degradation and confirming complete mineralization – but the progress in the last few years is encouraging. By leveraging genomics, synthetic biology, and systems engineering, scientists are inching closer to microbial solutions for polyolefin waste. In an era where plastic pollution is ubiquitous, such innovations are not merely academic; they could form a cornerstone of sustainable waste management in the future. Harnessing microbial communities to safely biodegrade or convert plastics aligns with the broader goal of a circular economy, where waste is transformed rather than simply accumulated. Although we are not yet able to let a vat of microbes digest a heap of PE overnight, the groundwork is being laid for a new generation of biotechnologies that treat plastic not as indestructible trash, but as a feedstock for biological recycling. The coming years will reveal how far we can push nature’s decomposers to meet this modern challenge. The research reviewed here provides a roadmap and a rationale for continuing to explore and engineer the biodegradation potential of microbial communities – an effort that could ultimately help reconcile our use of durable plastics with the planet’s need for biodegradability.

## References

[1] Production, use, and fate of all plastics ever made. Science Advances, 3(7):e1700782 (2017). DOI: 10.1126/sciadv.1700782
[2] Polyethylene biodegradation: A multifaceted approach. Biotechnology Advances, 82:108577 (2025). DOI: 10.1016/j.biotechadv.2025.108577
[3] Microbial enzymes for the recycling of recalcitrant petroleum-based plastics: how far are we? Microbial Biotechnology, 10(6):1308–1322 (2017). DOI: 10.1111/1751-7915.12710
[4] Assembly strategies for polyethylene-degrading microbial consortia based on the combination of omics tools and the “Plastisphere”. Frontiers in Microbiology, 14:1181967 (2023). DOI: 10.3389/fmicb.2023.1181967
[5] Challenges with verifying microbial degradation of polyethylene. Polymers, 12(1):123 (2020). DOI: 10.3390/polym12010123
[6] Functional analysis of alkane hydroxylase system derived from Pseudomonas aeruginosa E7 for low molecular weight polyethylene biodegradation. International Biodeterioration & Biodegradation, 103:141–146 (2015). DOI: 10.1016/j.ibiod.2015.04.027
[7] The role of the copper-binding enzyme – laccase – in the biodegradation of polyethylene by the actinomycete Rhodococcus ruber. International Biodeterioration & Biodegradation, 84:204–210 (2013). DOI: 10.1016/j.ibiod.2012.03.001
[8] Biodegradation of micro-polyethylene particles by bacterial colonization of a mixed microbial consortium isolated from a landfill site. Chemosphere, 222:527–533 (2019). DOI: 10.1016/j.chemosphere.2019.01.159
[9] Novel consortia of Enterobacter and Pseudomonas formulated from cow dung exhibited enhanced biodegradation of polyethylene and polypropylene. Journal of Environmental Management, 284:112030 (2021). DOI: 10.1016/j.jenvman.2021.112030
[10] Biodegradation of Low-Density Polyethylene (LDPE) by mixed culture of Lysinibacillus xylanilyticus and Aspergillus niger in soil. PLOS ONE, 8(9):e71720 (2013). DOI: 10.1371/journal.pone.0071720
[11] Biodegradation of polyethylene by Meyerozyma guilliermondii and Serratia marcescens isolated from the gut of waxworms (larvae of Plodia interpunctella). Science of The Total Environment, 853:158604 (2022). DOI: 10.1016/j.scitotenv.2022.158604
[12] Unraveling the plastic degradation potentials of the plastisphere-associated marine bacterial consortium as a key player for the low-density polyethylene degradation. Journal of Hazardous Materials, 425:128005 (2022). DOI: 10.1016/j.jhazmat.2021.128005
[13] Polyethylene valorization by combined chemical catalysis with bioconversion by plastic-enriched microbial consortia. ACS Sustainable Chemistry & Engineering, 11(9):3563–3574 (2023). DOI: 10.1021/acssuschemeng.2c06392
[14] Cutting-edge developments in plastic biodegradation and upcycling via engineering approaches. Metabolic Engineering Communications, 19:e00256 (2024). DOI: 10.1016/j.mec.2024.e00256